## Slide 1: Impact of PTFE distribution on water transport in a gas diffusion layer of polymer electrolyte fuel cells
d.froning@fz-juelich.de
Institute of Electrochemical Process Engineering (IEK-3)
Dieter Froning1, JunLiang Yu1, Uwe Reimer1, Steven Beale1, Werner LEhnert1,2,3
1Forschungszentrum Jülich GmbH, Institute of Electrochemical Process Engineering (IEK-3), Jülich, Germany
2Modeling in Electrochemical Process Engineering, RWTH Aachen University, Aachen, Germany
3JARA-HPC, Jülich, Germany
Interpore, May 8, 2019, Valencia, Spain

## Slide 2: Overview
Motivation
Simulation setup
Results
Summary

## Slide 3: Polymer electrolyte fuel cell (PEFC)
Active area: 4 cm x 4 cm = 16 cm²
Water management affects cell performance
Contact angles and breakthrough point distance can support two-phase CFD simulations in GC
Anode :
Cathode :

## Slide 4: Stochastic Model of the GDL Structure Ulm University
2D SEM image of a GDL
Assumptions on paper-type GDL
Fibers are horizontally oriented straight lines.
GDL can be separated into thin layers
Cells are partially filled with binder
22 realizations
R. Thiedmann, F. Fleischer, Ch.Hartnig, W. Lehnert, V. Schmidt, Stochastic 3D Modeling of the GDL Structure in PEM Fuel Cells Based on Thin Section Detection, J. Electrochem. Soc. 155 (2008) B391-B399
3D model of a GDL
4

## Slide 5: Simulation setup
GDL
Empty Space
Inlet : Velocity
Outlet : Open
Periodic
Water velocity is defined with .
Water flow through GDL is a capillary dominated process (density ratio and viscosity ratio can be negligible)
PEMFC working region M≈18, Ca≈10-6~10-8 , average velocity used
Local contact angle: 110° (Water on PTFE)

## Slide 6: Apparent contact angle with the sub-pixel polynomial fitting method (SPPF)
Only the biggest droplet in every geometry is considered.
Only droplets not touching the boundary.
VA of cross sections: 90°, 60°, 30°, 0°
One of view angles ;
Asymmetric shape

## Slide 7: Apparent contact angle
Rotation of the view angle (VA)

## Slide 8: Comparison with idealized contact angles
with
Circle method
(symmetric drop) :
V : Volume
H : Height
A : Contact area
Geometry |  | 
1 | 132.9 | 136.7 ± 3.6
2 | 127.0 | 126.2 ± 5.3
3 | 122.1 | 135.5 ± 10.9
4 | 125.7 | 129.1 ± 8.5
5 | 122.4 | 125.8 ± 9.0
6 | 132.5 | 135.5 ± 8.9
7 | 122.3 | 127.7 ± 8.6
Average | 126.9 | 130.9 ± 7.8
Geometry |  | 
1 | 132.9 | 136.7 ± 3.6
2 | 127.0 | 126.2 ± 5.3
3 | 122.1 | 135.5 ± 10.9
4 | 125.7 | 129.1 ± 8.5
5 | 122.4 | 125.8 ± 9.0
6 | 132.5 | 135.5 ± 8.9
7 | 122.3 | 127.7 ± 8.6
Average | 126.9 | 130.9 ± 7.8

## Slide 9: PTFE distribution
Randomly distributed, total PTFE coverage given
Regions with or without PTFE
Local contact angle Water/PTFE: 120° to pronounce the impact
50% PTFE, random. Two layers.
Upstream.
Downstream.
Sandwiched.
0% PTFE
100% PTFE
100% PTFE
0% PTFE
0% PTFE
100% PTFE
100% PTFE

## Slide 10: PTFE distribution
50% PTFE coverage, random distributed.
50% PTFE coverage, Upstream
50% PTFE coverage, Downstream.
50% PTFE coverage, sandwiched.
4.8 ms
9.6 ms
14.4 ms
19.2 ms
Small through-pores in the GDL.
Through-pores available for gas transport.

## Slide 11: PTFE distribution
50% PTFE coverage, random distributed.
50% PTFE coverage, Upstream
50% PTFE coverage, Downstream.
50% PTFE coverage, sandwiched..
4.8 ms
9.6 ms
14.4 ms
19.2 ms
PTFE
Large through-pores in the GDL.

## Slide 12: PTFE distribution
50% PTFE coverage, random distributed.
50% PTFE coverage, Upstream
50% PTFE coverage, Downstream.
50% PTFE coverage, sandwiched.
4.8 ms
9.6 ms
14.4 ms
19.2 ms
PTFE
No through-pores in the GDL.

## Slide 13: PTFE distribution
50% PTFE coverage, random distributed.
50% PTFE coverage, Upstream
50% PTFE coverage, Downstream.
50% PTFE coverage, sandwiched.
4.8 ms
9.6 ms
14.4 ms
19.2 ms
Large through-pores in the GDL – but they get closed.

## Slide 14: Summary
Liquid water transport through GDL process are different in stochastic geometries and some droplets emerging on GDL surface
Droplet shapes are irregular and vary with different positions and geometries
Apparent contact angles are different from the idealized value and more accurate
Distribution of PTFE can induce additional effects.
PTFE is most effective in the upstream region of the GDL.
[1] J. Yu, D. Froning, U. Reimer, W. Lehnert, Apparent contact angles of liquid water droplet breaking through a gas diffusion layer of polymer electrolyte membrane fuel cell, Int. J. Hydrogen Energy, 43 (2018) 6318-30.
[2] J. Yu, D. Froning, U. Reimer, W. Lehnert, Liquid water breakthrough location distances on a gas diffusion layer of polymer electrolyte membrane fuel cell. J. Power Sources 389 (2018) 56-60.
[3] D. Froning, J. Yu, U. Reimer, W. Lehnert, Statistische Analyse des lokalen Wassertransportes einer Polymer-Elektrolyt-Brennstoffzelle. Chem. Ing. Tech., 91 (2019), https://doi.org/10.1002/cite.201800158.
[4] M. Andersson, S. B. Beale, D. Froning, J. Yu, W. Lehnert, Coupling of Lattice Boltzmann and Volume of Fluid Approaches to Study the Droplet Behavior at the Gas Diffusion Layer/Gas Channel Interface. ECS Trans. 86 (2018) 329-338.
[5] J. Yu, Lattice Boltzmann Simulations in Components of Polymer Electrolyte Fuel Cell, PhD thesis, RWTH Aachen University (2018), Aachen, Germany.
14

## Slide 15
Thank you for your attention!