## Slide 1: Supercritical Adsorption of CO2 and CH4 on Shales and Surrogate Porous Media
Humera Ansari, Martin Trusler, Geoffrey Maitland, Ronny Pini
humera.ansari10@imperial.ac.uk

## Slide 2: Shale Gas Production
Rising production rates of shale gas worldwide
Global shale resources = 36,000 trillion cubic feet
Transition Fuel
[1] Salehi et al., Oil and Gas Review, 7, 2009
[2] Edwards et al., Environmental Science & Technology, 49(15), 2015
Shale Gas Extraction
Fracking
Enhanced Shale Gas Recovery
CO2
CH4
CH4
CO2
Shale
Improved CH4 recovery
CO2 sequestration
Low recovery:
10 – 20%
Based on the New Albany Shale [1]
[2]
[3]
[3] Ansari et al., Fuel, 301, 2021

## Slide 3: Gas Storage in Shale
50% of GIP [3]
Adsorbed Gas
Organic Matter
Clay Minerals
Dissolved Gas
Oil
Water
Free Gas
Large Pores
Natural Fractures
[3] Rexer et al., Energy & Fuels, 27, 2013
[1] Ma et al., Energy & Environmental Science, 14, 2021
[2] Loucks et al., Journal of Sedimentary Research, 79, 2009
[1,2]

## Slide 4: Adsorption Measurements
Gravimetric Measurement:
Rubotherm Magnetic Suspension Balance
Supercritical Adsorption
Adsorption at subsurface conditions
Subcritical Adsorption
Characterisation of the adsorbent
Volumetric Measurement:
Quantachrome Autosorb iQ
Pressure | Temperature
0 – 300 bar | 40°C
Pressure | Adsorbates
0 – 1 bar | Ar (87 K), N2 (77 K) and CO2 (273 K)

## Slide 5: Adsorption Modelling: Lattice DFT Model
Same number of molecules in each layer
Adsorption occurs on a flat surface
Number of molecules changes in each layer
Adsorption occurs on a curved surface
[1] Hwang et al., Microporous and Mesoporous Materials, 273, 2019
[2] Ansari et al., Microporous and Mesoporous Materials, 308, 2020
Pore space is discretised into lattice sites
Slit pore[1]
Cylindrical pore[2]
Clay
Minerals
Organic
Matter

## Slide 6: Use of Surrogate Materials
Ansari et al., Energy & Fuels, 36(7), 2022

## Slide 7: Surrogate Materials
Mesoporous Carbon[1]
Activated Carbon[1]
Illite[2,3]
HP Measurements
+
PSD
+
LDFT Model
Hybrid LDFT Model Parameters
[2] Hwang et al., Microporous and Mesoporous Materials, 273, 2019
[3] Ansari et al., Energy & Fuels, 36(7), 2022
[1] Ansari et al., Microporous and Mesoporous Materials, 308, 2020

## Slide 8: Shales
[1] Delle Piane et al., International Journal of Coal Geology, 2021. 103880
[2] Marcellus Coalition, 2020
[3] British Geological Survey
Shale | TOC [wt%] | Clay [wt%]
Longmaxi (LG4) | 7.8 | 21.0
Marcellus (ML) | 6.1 | 47.0
Bowland (B6) | 3.6 | 23.4
Bowland (B8) | 0.9 | 25.5
Longmaxi Shale
Marcellus Shale
Bowland Shale
[1]
[2]
[3]

## Slide 9: Adsorption on Shale
LG4 model includes MC (60%) + AC (40%)
Carbon controls adsorption for LG4 and ML (ρb > 1 mol/L)
Ratio of adsorption between LG4 and ML is similar to the ratio of TOC
CO2/CH4 ratio is > 2
Longmaxi Shale
Marcellus Shale
Shale | TOC [wt%] | Clay [wt%]
LG4 | 7.8 | 21.0
ML | 6.1 | 47.0
Ansari et al., Energy & Fuels, 36(7), 2022

## Slide 10: Adsorption on Shale
Bowland (organic-rich) Shale
Bowland (organic-lean) Shale
Shale | TOC [wt%] | Clay [wt%]
B6 | 3.6 | 23.4
B8 | 0.9 | 25.5
LG4 and ML adsorb more than the Bowland shales
CO2/CH4 ratio is > 3
Increased contribution of IL
B8 model includes a larger contribution of IL than MC
Ansari et al., Energy & Fuels, 36(7), 2022

## Slide 11: Representative PSD for Shale
Three scaling factors:
wo – TOC (wt%)
wc – clay content (wt%)
t – fraction of AC
Shale | Experimental νptot [cm3/g] | Predicted νptot [cm3/g]
LG4 | 0.050 | 0.049
ML | 0.042 | 0.050
B6 | 0.020 | 0.028
B8 | 0.020 | 0.016
Pore volumes directly dependant on TOC
PSDs obtained based on kernels for either slit carbon pores or cylindrical silica pores (not both).
Ansari et al., Energy & Fuels, 36(7), 2022

## Slide 12: Gas-in-Place and CO2 Storage Potential
Excess Adsorbed
Amount
Volumetric Free Gas
Produced Volume:
Shale | OGIP [m3STP/m3] | CO2 Storage Potential [m3STP/m3]
LG4 | 20.0 | 30.3
ML | 17.8 | 26.3
B6 | 11.0 | 23.3
B8 | 11.3 | 25.7
Ansari et al., Energy & Fuels, 36(7), 2022

## Slide 13: Conclusions
Adsorption on shales is strongly dependent on TOC
Shale’s composition can be used to predict adsorption in shale, avoiding a heavy experimental burden
The validity of this approach extends from textural analysis to the quantification of the GIP
humera.ansari10@imperial.ac.uk