## Slide 1: Visualizing biofilms within porous media using contrast-enhancing staining agents
Laurenz Schröer, Tim De Kock, Tim Balcaen, Greet Kerckhofs, Karel Folens, Nico Boon and Veerle Cnudde - 31/05/2022

## Slide 2: Biofilms colonize the pore space affecting the material properties and water transport
Biofilms induce:
  Bioclogging
  Microbially induced precipitation
  Gas formation
  Dissolution
  Etc.
Their effect is often indirectly determined
or studied in 2D using microfluidics
Schematic example of a microfluidic setup
Valiei et al. 2012

## Slide 3: µCT can visualize the interior of opaque materials, but cannot distinguish biofilms from water
Biofilm = 99% water
Positive contrast agents
  BaSO4
  silver-coated microspheres
  1-chloronaphtalene
Drawbacks:
  Alters fluid properties
  Heterogeneous distribution
  Sedimentation
Aim: Identify other negative contrast agents to visualize biofilms in 3D with µCT.
Anozie Ebigbo, 2009
Schematic model biofilm
in porous medium
µCT cross-section
solid
Water/Biofim?
Water

## Slide 4: Biofilms were cultured on stones and within a sand column
Dripflow - Visualization “big” biofilms on stones
Flow - Visualization biofilms within pores
General workflow
Cultivate the biofilm
Add the contrast agent
Remove non-attached contrast agent with PBS
µCT scan

## Slide 5: Numerous contrast agent were tested and mono-WD POM Gave promising results
Tested, but less promising
KI
KBr
Iron-oxidation
Ba-absorption
PTA
Mono-WD POM: Dripflow experiment

## Slide 6: Visualizing biofilms inside the flow cell remains challenging

## Slide 7: five contrast agents were compared Isotonic lugol and Hf-WD POM were promising
Isotonic lugol
Hf-WD POM

## Slide 8: 3D visualization of the biofilm structure
Hf-WD POM
Isotonic lugol
Both contrast agents can be used complementary

## Slide 9: Isotonic lugol visualizes potential biofilms inside porous media but segmentation remains difficult

## Slide 10: Conclusions and future research
Negative contrast agents are able to stain biofilms allowing visualization with µCT
Hf-WD POM, Mono-WD POM and isotonic lugol are the most promising contrast agents
Visualization of biofilms inside porous media remains challenging
Future research should focus on how these contrast agents interact with the biofilm and how we can enhance absorption

## Slide 11
15 Institutions
9 Countries
Facilities:
  11 Electron microscopy
  14 X-ray Microscopy
Transnational access, joint research activities,
industry events, workshops, etc.
https://excite-network.eu/

## Slide 12: Laurenz Schröer Postdoctoral researcher and Facility manager for EXCITE Department of geology - pprogress E Laurenz.Schroer@ugent.be T +32 9 264 46 33 www.ugent.be
@GeologieUGent @ProgressU
UGCT