## Slide 1: Nanoparticle-based suspensions and emulsions for enhanced oil recovery
A. Strekla 1,2, Ch. Ntente 1,3, M. Theodoropoulou 1 and Ch. Tsakiroglou1,*
1 Foundation for Research and Technology Hellas, Institute of Chemical Engineering Sciences (FORTH/ICE-HT), 26504 Patras, Greece
2 University of Patras, Department of Physics, 26504 Patras, Greece
3 University of Patras, Department of Chemistry, 26504 Patras, Greece
* ctsakir@iceht.forth.gr

## Slide 2: Contents of presentation
Introduction
Overview
Synthesis of Fe NPs and characterization
Tests of enhanced oil recovery in porous media models
Conclusions

## Slide 3: Introduction
Energy consumption worldwide is expected to increase by 50% relative to current levels by the end of 2030.
This growth is unlikely to be met by renewable resources, and thus there is a strong and growing demand for oil as a predominant energy resource.
Problem
Objectives
Globally the overall oil recovery factors for primary and secondary recovery range from 35% to 45%.
A tertiary recovery method can enhance the recovery factor by 10-30%, which could contribute to energy supply
The use of nanoparticles in enhanced oil recovery (EOR) processes comprises an emerging and well-promising approach.

## Slide 4: Overview
Density , Contact angle
Surface – Interfacial tension
Size , z-potential
Rheology of emulsion
Synthesis of Fe NPs
Characterization of Fe NPs properties
Experiments into porous media
polyphenols from parsley leaves
FeCl3
transparent glass-etched pore networks

## Slide 5: Synthesis of Fe NPs
Polyphenols
(parsley leaves)
FeCl3 0.1M
Measurements of Fe NPs suspension |  | 
pH | 6,02 | 
Eh (mV) | 499,1 | 
Surface Tension(mN/m) | Wilhelmy plate 53.84 | DuNouy Ring 55.12
Interfacial Tension (mN/m) | 19.41 (with n-C12) | 
Size (nm) | 132,43 | 
Z-potential (mV) | -25,5 | 
Image : Solution of FeNPs

## Slide 6: Properties of FeNPs
Density:
fluids | Density d (g/mL)
Paraffin oil | 0.829
NaCl 0.25M | 1.002
Fe NPs 0.25(g/L) | 0.9931
Fe NPs 0.25 (g/L) – NaCl 0.25M | 0.9814
Fe NPs 0.25 (g/L) – NaCl 0.25M (Emulsion) | 0.833
Measurement ST and IT of suspensions:
The static surface/interfacial tension of aqueous phase/air and aqueous phase/oil was measured by using a tensiometer with DuNouy Ring.
suspension | Surface tension (mN/m) | Interfacial tension (mN/m)
NaCl 0.25M | 66.42 | 30.59
Fe NPs 0.25(g/L) | 52.87 | 27.93
Fe NPs 0.25 (g/L) – NaCl 0.25M | 50.03 | 20.72

## Slide 7: Contact angles:
Solutions | CA (°)/air | image | CA (°) / paraffin | Image
NaCl 0.25M | 53.85 |  | 54.45 | 
Fe NPs 0.25 g/L | 53.05 |  | 39.2 | 
Fe NPs 0.25 g/L – NaCl 0.25M | 55.0 |  | 43.95 | 

## Slide 8: The suspended nanoparticle size distribution was determined with dynamic light scattering (DLS), while the stability of the nano-colloids was confirmed by measuring the ζ-potential.
Size and z-potential:
solutions | Size (nm)
Fe NPs 0.25 (g/L) | 36.39
Fe NPs 0.25(g/L) – NaCl 0.25M | 35.26
Fe NPs 0.25(g/L) – NaCl 0.25M (Emulsion) | 220.2
Zeta potential of FeNPs 0.25 (g/L) is -22.1 mV.
Image : Dynamic light scattering

## Slide 9: Pickering Emulsion
With the aid of an ultrasound probe, the nano-colloids were mixed with oil (n-decane) to prepare Pickering emulsion of FeNPs 0.25g/L -NaCl 0.25M .
Suspension of FeNPs - oil (n-decane) Volume ratio 1:1
Ultrasound probe
Pickering emulsion

## Slide 10: Experimental setup of visualization tests on transparent pore networks

## Slide 11: Values of Ca and κ
Capillary number
Viscosity ratio
= 0.01246 Pa s
= 0.026 Pa s
= 0.001 Pa s
fluid | Flow rate(10-6/60) m3/s | U ( 10 -5 m/s) | μ (Pa s) | ΙΤ (mN/m) | Ca (10-6) | κ
paraffin | 0.08 | 0.94 | 0.026 | 30.5 | 8.0 | 26.0
NaCl 0.25M | 0.2 | 2.35 | 0.001 | 25.0 | 0.94 | 0.038
FeNPs 0.25 g/L | 0.2 | 2.35 | 0.001 | 25.0 | 0.94 | 0.038
FeNps 0.25 g/L – NaCl 0.25M | 0.2 | 2.35 | 0.001 | 25.0 | 0.94 | 0.038
FeNps 0.25 g/L – NaCl 0.25M (emulsion) | 0.2 | 2.35 | 0.01246 | 25.0 | 1.17 | 0.48
Ca pore scale -> CaL1=Ca*factor
Ca network scale -> CaLN=CaL1*LN/Lp
Drainage: CaL1=0.0324, CaLN=3.2
Imbibition: CaL1=0.0038, CaLN=0.38
Tsakiroglou et al., AIChE J. 49(10), 2472 (2003)

## Slide 12: Transient two-phase flow patterns
Primary Drainage
Displacement NaCl 0.25M by paraffin oil (red- colored)
κ= 26.0
Ca = 8x
Primary Imbibition
NaCl 0.25M
κ = 0.038
Ca = 0.94x10-6

## Slide 13: Transient two-phase flow patterns
FeNPs 0.25 g/L
κ≈ 0.038
Ca = 0.94x10-6
FeNPs 0.25 g/L – NaCl 0.25M
κ≈ 0.038
Ca = 0.94x10-6
FeNPs 0.25 g/L – NaCl 0.25M
Emulsion
κ=0.48
Ca = 1.17x10-6
Secondary
Imbibition
Tsakiroglou et al., J. Coll. & Interface Sci. 267, 217-232 (2003)
Tsakiroglou, J. Non-Newt. Fluid Mech. 117, 1–23 (2004)

## Slide 14: Plots of tests for EOR
Fe NPs 0.25 (g/L)
Fe NPs 0.25 (g/L) – NaCl 0.25M
Fe NPs 0.25 (g/L) – NaCl 0.25M Emulsion

## Slide 15: Results
Type of displacement | Displaced fluid | Displacing fluid | Flow rate (mL/min) | Injected volume (mL) | Oil saturation | Oil removal efficiency (%)
Drainage | NaCl 0.25M | Paraffin oil | 0.08 | 8.0 | 0.82 | -
Prim. Imbib. | Resid. paraffin oil | NaCl 0.25M | 0.2 | 8.0 | 0.45 | 46.25
Sec. Imbib. | Resid. paraffin oil | FeNPs 0.25 (g/L)-water suspension | 0.2 | 14.4 | 0.36 | 20.0
Drainage | NaCl 0.25M | Paraffin oil | 0.08 | 8.0 | 0.82 | -
Prim. Imbib. | Resid. paraffin oil | NaCl 0.25M | 0.2 | 8.0 | 0.41 | 50.0
Sec. Imbib. | Resid. paraffin oil | FeNPs 0.25 (g/L)-NaCl 0.25M suspension | 0.2 | 14.0 | 0.39 | 4.88
Drainage | NaCl 0.25M | Paraffin oil | 0.08 | 8.0 | 0.82 | -
Prim. Imbib. | Resid. paraffin oil | NaCl 0.25M | 0.2 | 8.0 | 0.44 | 46.34
Sec. Imbib. | Resid. paraffin oil | Emulsion | 0.2 | 12.0 | 0.09 | 79.55

## Slide 16: Conclusions
The potential to increase the residual oil recovery efficiency by injecting suspensions of iron oxide nanoparticles synthesized and stabilized by the polyphenols of parsley extracts is investigated with visualization tests on a glass-etched pore network.
The nanoparticles mobilize trapped oil by transferring it from upstream to downstream through a mechanism of successive steps of drainage (local increase of oil saturation) / imbibition (local decrease of oil saturation).
It seems that the oil recovery efficiency of secondary imbibition tests is favored when using low iron concentration Fe NPs suspension without the presence of NaCl . On the other hand, the oil recovery efficiency increases respectably when using Pickering emulsions stabilized by FeNP with NaCl.

## Slide 17
Acknowledgement