## Slide 1
Physicochemical Characterization of CO2-Activated Colloidal Silica Gels for Adaptive Subsurface Sealing
Simon Zougheib
Energy Resources and Petroleum Engineering
KAUST

## Slide 2: Problem Statement
Carbon capture, utilization, and storage (CCUS) reduces CO2 emissions by capturing CO2 and storing it in deep geological formations.
However, stored CO2 may leak through faults and fractures in the wellbore cement
Colloidal Silica is investigated as an adaptive sealant as it is initially an injectable liquid and gels after exposure to CO2
Treatment design requires understanding how CO2 interacts with colloidal silica dispersions
In this work, we analyze CO2 uptake, and the effect of particle size and dissolved CO2 concentration on the gelation response
Introduction
1. Sample Characterization
2. CO2 Uptake
3. Rheological Analysis
Conclusion

## Slide 3: How CO2 Activates Colloidal Silica
Stage 1: Stable colloidal silica dispersion
Stage 2: CO2 dissolution
Stage 3: Surface-charge reduction and double-layer compression
Stage 4: Aggregation and gelation initiation
Introduction
1. Sample Characterization
2. CO2 Uptake
3. Rheological Analysis
Conclusion
CO2

## Slide 4: Part 1: Particle size and zeta potential characterization
Commercial Name | Silica wt% | Average Particle Diameter [nm] | Zeta Potential [mV]
CS30 | 30 | 6.4 | -46.6
SM30 | 30 | 7.7 | -50.2
CS40 | 40 | 9.7 | -54.0
TM40 | 40 | 15.1 | -40.4
CS50 | 50 | 75.2 | -39.4
Particle-size range from 6.4 to 75.2 nm
Negative zeta potentials confirm electrostatic stabilization before CO2 exposure
Introduction
1. Sample Characterization
2. CO2 Uptake
3. Rheological Analysis
Conclusion
SEM images for visualization of different particle sizes (after gelation, dried)
CS40 – 9.7 nm
CS50 – 75.2 nm
TM40 – 15.1 nm
1 μm
1 μm
1 μm
Particle size (by Dynamic Light Scattering) and zeta potential were measured for different commercial samples:

## Slide 5: Part 2: CO2 Uptake
Use fixed-volume reactor to investigate CO2 uptake by pressure decay with time
Introduction
1. Sample Characterization
2. CO2 Uptake
3. Rheological Analysis
Conclusion

## Slide 6: Effect of Silica Loading
For all samples: fast initial uptake, then slower approach to equilibrium
Lower silica loading (higher water content) leads to higher cumulative CO2 uptake
Introduction
1. Sample Characterization
2. CO2 Uptake
3. Rheological Analysis
Conclusion
CO2 Uptake
Pressure Decay

## Slide 7: Effect of Particle Size
At fixed silica loading, the smaller particle samples show higher apparent CO2 uptake
Likely linked to higher surface area and more accessible silanol sites per unit silica mass
40 wt% Silica
30 wt% Silica
Introduction
1. Sample Characterization
2. CO2 Uptake
3. Rheological Analysis
Conclusion
The 40 wt% samples allow particle-size comparison at fixed silica loading

## Slide 8: Part 3: Rheological Analysis
Pre-saturate solution to the target dissolved CO2 concentration (at room temperature)
Measure solution pH
Transfer to rheometer for analysis at 80°C
15°
Introduction
1. Sample Characterization
2. CO2 Uptake
3. Rheological Analysis
Conclusion

## Slide 9: pH vs. Dissolved CO2 Concentration
Increasing dissolved CO2 lowers the pH and promotes gelation
Gelation occurs once the pH falls below an apparent threshold
Smaller particle size samples gel at lower dissolved CO2 concentration and smaller pH drop
15.1 nm
9.7 nm
Introduction
1. Sample Characterization
2. CO2 Uptake
3. Rheological Analysis
Conclusion

## Slide 10: Test 1: Dynamic Mechanical Analysis – Sol/Gel Transition
Sol/Gel Transition is the time when the sample becomes a gel
Measure the Storage (G’) and Loss (G”) moduli over time at 1% strain and 10 rad/s frequency
  G’<G” → liquid-like behavior
  G’>G” → gel-like behavior
  We extract the sol-gel transition time tSG when G’=G”
Introduction
1. Sample Characterization
2. CO2 Uptake
3. Rheological Analysis
Conclusion
Example: 9.7 nm, 0.075 mol/kg H2O

## Slide 11: Test 2: Viscosity Measurements – HVTT
Measure viscosity over time at constant shear rate (5s-1)
  We extract the High Viscosity Threshold Time (HVTT)1 - time at onset of rapid viscosity increase, at 100 mPa.s
Introduction
1. Sample Characterization
2. CO2 Uptake
3. Rheological Analysis
Conclusion
(1) Basilio, E.; Zougheib, S.; Sahu, Q.; Almohsin, A.; Alabdrabalnabi, M.; Hoteit, H. Predicting Gelation Kinetics of Colloidal Silica for Water Shut-off Treatments: A Novel Arrhenius-Based Model. Phys. Fluids 2025, 37 (4), 043110. https://doi.org/10.1063/5.0262437.
Example: 9.7 nm, 0.075 mol/kg H2O

## Slide 12: Results – Gelation Time
HVTT
Sol/gel Transition
Introduction
1. Sample Characterization
2. CO2 Uptake
3. Rheological Analysis
Conclusion
More dissolved CO2 makes gelation faster
For the same initial dissolved CO2, the 9.7 nm sample gels faster than the 15.1 nm sample

## Slide 13: Results – Gel Network Characterization
Maximum Viscosity
Introduction
1. Sample Characterization
2. CO2 Uptake
3. Rheological Analysis
Conclusion
The smaller particle size 9.7 nm sample reaches much higher maximum viscosity
This indicates a stronger final gel network under the tested conditions
CS40 – 9.7 nm
TM40 – 15.1 nm
1 μm
1 μm

## Slide 14: Conclusion
CO2 destabilizes silica dispersions and triggers gelation
Lower silica loading (higher water content) increases CO2 uptake
At fixed loading, samples with smaller particles take up more CO2
The samples with smaller particles (9.7 nm) gel faster and form stronger networks than the ones with larger particles (15.1 nm)
Introduction
1. Sample Characterization
2. CO2 Uptake
3. Rheological Analysis
Conclusion

## Slide 15
Thank you