## Slide 1
Interpore 2026, Nantes. MS05 (Physics of multiphase flow in diverse porous media)
22 may 2026
Fluid transfers through versatile dynamic NMR relaxometry
Benjamin Maillet (oral presenter), Philippe Coussot, Rahima Sidi-Boulenouar (Navier laboratory)
Rheology and Porous Media team building
Ecole des Ponts Paris Tech
Champs-sur-Marne
France
Main topic of Navier laboratory : Material for construction by plenty of approaches.

## Slide 2
Why understand the interaction between water and solid matrix ?
Plenty of approaches but often …
→ not temporally and/or spacially resolved (only 1 image or a set of global information)
→ not « multiscale »
→ not quantitative
→ not so versatile (only specific material)
→ needs to hydric equlibrium (in contrary to the « real life »).
Lehoux et al, Physical Review E, 2016
Using colloidal deposition to mobilize immiscible fluids from porous media
Joanna Schneider, Rodney D. Priestley, and Sujit S. Datta
Phys. Rev. Fluids, 2021
→ The « Dynamic NMR relaxometry » is an innovative and general approach to answer to all these limitations for porous media and complex fluids

## Slide 3
The most standard NMR setup at Navier laboratory…
B0
B1
Minispec Brüker 0,5 teslas
Gz
V(sample) ≈ 1 cm3 >> pore, particle,… size
Duration(exp) ≈ 10 min << drying duration
↗ dry air flux + ↘ distance [air tube – sample]
→ « more agressive » drying by the top surface
→ NMR of liquid proton (water at 20 °C by default)
→ Direct access to NMR observable evolution
CPMG sequence
Global information
→ T2 probability
density function
∫ A.exp(-t/T2) d( ln(T2) )
Loop process
Spin Echo sequence
Local information
(optional)
T2 : characteristic time of magnetization (transverse part) to come back at equilibrium

## Slide 4
The fast exchange theory as a key concept…
Fast exchange bulk – surface available if :
→ 1 molecule can explore surface and bulk several times during T2 duration
→ Surface residence time << Diffusion time inside the pore
Dynamic relaxometry easier to interpret if :
→ T2,ads. or r2 constant during the drying if stable roughness, chemical composition,…
→ No gradient of water content, isotropic swelling or shrinkage,…
→ No dewetting of the solid matrix
4
→ NMR relaxation = Surface interaction process
→ Shift of the relaxation efficiency according to Tarr and Browstein (1979):
= -
→ Aqueus solution : τ2 = .
Paste, suspension, gel,… (volume fraction): τ2 = . = .
Porous medium: τ2 = . (saturated) or τ2 = . (unsaturated)
→ T2,pure water = 2250 ms at 20°C (reference) > T2,pure surf and bulk water dries first
≈ water molecule size
r2 : transverse relaxivity higher if the solid matrix is a stronger relaxation process for liquid water → depends on the chemical composition
Julien, Maillet, Tocquer, Aime, Coussot
Langmuir, 2024
Log(T2)
NMR signal
SNMR α V(water)
T2,,measured
ANR Thermo NMR, Sidi-Boulenouar (> 2026)

## Slide 5
The reference power law… PL(t) = 1 ! Slow drying of a stable material
Adsorbed water
Adsorbed + non adsorbed water
T2,ads. water = 2 ms
T2,sat. pore = 12 ms
Constant drying rate
Falling drying rate
≈ 1
Dry air
τ2 = . . Vwater
log(τ2) = C + 1 . log(SNMR) → PL(t) ≈ 1
if Vparticle constant (robust particle), …
Slow drying of Ludox suspension 0,5 M
Slow drying of saturated Vycor
= pure fused silica glass by 3D network of interconnected tortuous isotropic monodisperse pores (size ≈ 4,6 nm).
τ2 = . . Vwater (for unsaturated porous medium)
log(τ2) = C + 1 . log(SNMR) → PL(t) ≈ 1
if Swet constant (no dewetting), …
Sidi-Boulenouar, Maillet, Carouge, Ayturk, Poulesquen, Langmuir, 2026
Maillet, Sidi-Boulenouar, Coussot. Langmuir, 2022
… , r2 constant (chemical stability), fast exchange available, homogenous hydric content during the most of the drying.

## Slide 6
Deviation of the power law PL(t) n° 1. Shrinkage with no desaturatrion (PL < or = 1).
Regime 1: LP(t) = 1/1
τ2 = . . Vwater
log(τ2) = C + 1 . log(SNMR) → PL(t) ≈ 1
τ2 and Vwater decreases by the same relative variation.
→ Constant wetted surface
Regime 2: LP(t) = 1/3
τ2 = . . Vwater
log(τ2) = C + 1/3 . log(SNMR) → PL(t) ≈ 1/3
→ Isotropic shrinkage
if τ2 α Vwater / Swet α [pore size]1 and Vwater α [pore size]3 , …
… , r2 constant (chemical stability), fast exchange available, homogenous hydric content during the most of the drying.
Regime 1: LP(t) = 1/1
τ2 = . . Vwater
log(τ2) = C + 1 . log(SNMR) → PL(t) ≈ 1/1
if Spore = 2. l . l’ is constant and Vpore = l . l’ . e(t) decreases.
τ2 and Vwater decreases by the same relative variation.
→ only thickness of water e(t) decreases
« layer by layer » of water, if …
(Regime 2: LP(t) ≈ 0 → next slide… )
Slow drying of
Humid cellulose
Maillet
Sidi-Boulenouar
Coussot. Langmuir
2022
Maillet
Sidi-Boulenouar
Keita
2026
First part of slow drying of
montmorillonite paste (shrinkage)
T2 pdf (ms)
Régime 1
Régime 2
≈ 1
Log(T2)(log(S))

## Slide 7
Deviation of the power law PL(t) n° 2. Desaturation with perfect dewetting (PL = 0).
Slow drying of green poplar (free water)
τ2 = . . Vwater ≈ cste
during the most of free water drying
log(τ2) = C + 0 . log(SNMR) → PL(t) ≈ 0
if Swet and Vwater decrease by the same relative variation
→ Full dewetting with the same meniscii in tracheid, …
… , r2 constant (chemical stability), fast exchange available, homogenous hydric content during the most of the drying.
Maillet
Sidi-Boulenouar
Keita
2026
Regime 1: LP(t) = 1
Regime 2: LP(t) ≈ 0
τ2 = . . Vwater ≈ cste
log(τ2) = C + 0 . log(SNMR) → PL(t) ≈ 0
if Swet and Vwater decrease by the same relative variation
→ In accordance with dewetting during the last layer drying between 2 clay waferers « molecule by molecule », …
First part of slow drying of
montmorillonite paste (shrinkage)
T2 pdf (ms)
Régime 1
Régime 2
≈ 1
Log(T2)(log(S))

## Slide 8
Generalization of the power law if stable chemistry and homogen water content:
Shrinkage or swelling of a saturated porous medium :
Saturation or desaturation of non deformable porous medium ;
Power law | Dimentionality of the deformation | 
1 / 1 | N = 1 Ex : Lamellar shape (only thickness changes) | 
1 / 2 | N = 2 Ex :Thin cylindric shape (only diameter changes) | 
1 / 3 | N = 3 Ex : Spherical pore (only diamter changes) | 
1 / ∞ | Thin cylindric shape (only height changes) | 
1 / N | N : Dimenssionality of the deformation | 
e
d
d
h
Power law | Wetability | 
1 | Pore wall remains totaly wet d(S(wet)/S(wet)) = 0 | 
]0 ; 1[ | 0 < d(S(wet)/S(wet)) < d(V(water)/V(water)) | 
0 | Stable meniscus : d(V(water)/V(water)) = d(S(wet)/S(wet)) | 
Glass sphere
Bridge water
Glass sphere

## Slide 9
log(Normalized NMR signal)
≈ 1
Hydric vertical profiles of the AlSi gel during fast drying
Deviation of the power law PL(t) n° 3. Hydric inhomogneity development.
Drying of aluminosilicate gel
Sidi-Boulenouar, Maillet, Carouge, Ayturk, Poulesquen.
Langmuir, 2026
Submitted
τ2 = . . Vwater
log(τ2) = C + 1 . log(SNMR) → PL(t) ≈ 1 (reference value)
if Vparticle constant (no shape or roughness modification), r2 constant (chemical stability), fast exchange available, homogenous hydric content
during the most of the drying.
Hydric vertical profiles of the AlSi gel during slow drying
τ2 = . . Vwater
log(τ2) = C + PL(t) . log(SNMR) → PL(t) not constant
… because of the too slow diffusion of particles that don’t ensure fast redistribution of particles during this fast drying.
Gradient of T2(z,t) and φ (z,t) ↔ Deviation of PL(t)
We need to take into account hydric gradient, contraction, reconfiguration of particle ability to predict the power law deviation
→ See Rahima Sidi-Boulenouar’s poster for more details based on simulatuion of profiles to predict PL(t) fully !
≠ 1

## Slide 10
Deviation of the power law PL(t) n° 4. Chemical instability
Slow drying (concentrations increase) of
Cu2+(aq) + SO42-(aq) solution (very stable)
… vs … Betol solution (gel AlSi precursor : Sin0mHp(aq) , Na+(aq) , HO-(aq) )
log(Normalized NMR signal)
τ2 = . . Vwater → r2(t) = r2(0) . ( Vwater(t)/Vwater(0) )1-PL(t)
if chemical instability only and homogeneous concentration, fast exchange available.
PL(t) = 1 for Cu2+(aq) + SO42-(aq) solution → r2(t) = r2(0) → Cu2+ very stable during all the drying.
PL(t) > 1 and increases more and more for Beteol solution → effective r2(t) increases more and more
→ Betol very unstable during all the drying in accordance more than 2 states Qi : Q0 → Q1 → Q2 → … if r2(i) increases.
Genralization ?
→ Innovative methodology to sort components (ion, particle, solide matrix,…) by degree of chemical unstabilty.
Normalized NMR signal
Slope of the cureve log(τ2) vs log(Normalized NMR signal)
i.e. PL(t)
Cu2+(aq) + SO42-(aq)
Betol(aq)
log(τ2) (in ms)
Cu2+(aq) + SO42-(aq)
Betol(aq)
≈ 1
PL(t) > 1
Normalized NMR signal
r2(t) / r2(0)
Cu2+(aq) + SO42-(aq)
→ Chemical « avalanche »
Q0 → Q1 → Q2 →…
→ Chemical stability
Betol(aq)
M’Homa
Chabane
Maillet
Sidi-Boulenouar
Poulesquen
2026 (in progress)

## Slide 11
Conclusion and perspective.
Shift of the relaxation efficinecy : = - = r2 . = « Chemical term x Physical term »
… always based on the fast exchange theory (surface and bulk water by diffusion and other…)
log( τ2 ) vs log( NMR S ) → power law evolution PL(t) during drying = innovative, very generalisable representation to catch all physical and chemical instabilites by a multiscale, temprally and non invasive approach:
dewetting of the solid matrix, inhomogneity of local water content, chemical instability, … and more ?
The Dynamic NMR relaxometry can scope all water state progressively and is available for hydric drying of plenty of material as porous medium, paste, suspension, gel, solution, granular media, … and also foam, emulsion, … ?
Generalizations should be possible for all water transfer (ex: imbibition) or other volatil protonic liquids,…
… or a chemicaly and physicaly unstable material (ex: setting of a fresh cement paste) ?
Do you want to see more NMR or MRI
from Navier laboratory ?
→ 4 other presentations
(P. Coussot, F. Gerony, E. Keita, O. Hbaieb)
→ 2 posters
(R. Sidi-Boulenouar, A. Samba)

## Slide 13
Sum up of the main expected aspects of the T2 pdf