## Slide 1: Foam confined in granular media: liquid distribution & consequences
A. Salamé, V. Langlois, O. Pitois

## Slide 2: Introduction
Foam in porous media – Applications
Applications for 50 years: Petroleum Operations (drilling fluid, sand cleanout fluid,…)
New applications:
  “In situ” soil remediation (hydrocarbur, heavy metals,…)
  Soil reinforcement (microbiologically induced calcite precipitation,…)
  Potential use of foam as binder of granular media (especially waste granular materials)
Foam + binders:
cement slurries,
geopolymer solutions,
calcined clay suspensions
Granular media

## Slide 3: Introduction
Foam: Dispersion of a large amount of gas in a liquid phase.
Characteristic parameters:
Liquid fraction
Bubble sizes (, polydispersity degree ,…)
For foam confined in granular media: Grain sizes (, polydispersity,…),
Questions raised for confined foams:
1. What’s the microstructure of a confined foam? How does the liquid distribute itself inside the pore space?
2. How are the properties of the foam affected by confinement?
Continuous liquid phase
Gas bubbles
Microstructure of bulk foam
Bulk foam
Confined foam
polydispersity:
Network of Plateau borders

## Slide 4: 1. Confined foam microstructure & liquid distribution
Model for the liquid distribution in porous space
Daisy shaped liquid bridges in foam-filled granular packings, Pitois O., Salamé A. et al., JCIS, 2023
Permeability of foam-filled granular packings: numerical modeling, Langlois V., Salamé A. et al., PRF , 2025
Assumptions:
Monodisperse spherical grains
Monodisperse bubbles
Perfect wetting
Foam at equilibrium with uniform capillary pressure (with surface tension)
Liquid fraction of the foam introduced in the granular medium
Effective liquid fraction of the foam filling the core of the pore space
5%
10%
15%
Numerical simulations (Surface Evolver)
Liquid bridges
Wall Plateau Borders
Core Plateau Borders

## Slide 5: 1. Confined foam microstructure & liquid distribution
Experiments: Measure the effective liquid fraction of the core foam
Höhler R. et al., Soft Matter, 2021
Effective liquid fraction of the core foam
Surface liquid fraction of the core foam at the column wall.
Monodisperse
Polydisperse foam
G
Bulk foam
mm
mm
mm
Example:
core foam
Column wall
liquid
Column wall
Camera
(to prevent gravity drainage)

## Slide 6: 2. Consequences on confined foam properties
Shear rate
Shear stress
(Pa)
Marze et al.,
J. Rheol. 2008
Experiment performed in the International Space Station
Foam properties
Rheology: Yield stress
Aging: Coarsening
Real time: 2h
1 mm
Pasquet M. et al.,
JCIS, 2023
Bulk foam
  For bulk foam, bubble growth in the stationary regime:
Coarsening rate,
Yield stress,
Rheometer
Foam
Herschel Bulkley (HB) model:
Bulk foam:
Notes: Now, to illustrate the effect of this redistribution of liquid on the properties of the foam, I will focus on two specific properties. The first concerns an ageing mechanism known as coarsening, and the second concerns the rheology of the foam.
Coarsening is caused by the difference in gas pressure within the bubbles, resulting from the dispersion of bubble sizes. As the gas pressure is higher in the small bubbles, this leads to a transfer of gas from the small bubbles to the large bubbles. The average bubble size increases over time. It is observed that the increase of the square of the bubble size is proportional to the time interval. This leads to the definition of a coarsening rate. It has been shown that the coarsening rate can be expressed as the product of a physicochemical constant and a decreasing function of the liquid fraction.
The second properties is the yield stress of the foam. This yield stress can be characterized by shearing a foam in a rheometer. The experimental relationship between shear stress and shear rate is usually described using a Herschel-Bulkley model. By fitting this relationship to the experimental results, we can determine the yield stress. For bulk foam, based on a dimensional analysis, the yield stress should take this form, where 𝛾 is the surface tension. Note that the function g is a decreasing function of the liquid fraction.

## Slide 7: 2. Consequences on confined foam properties
Aging: Coarsening
Confined foam
Foam properties
Rheology: Yield stress
Foam
Camera
Time
Apparent viscosity
Darcy’s law:
Equivalent
shear rate:
: intrinsic permeability
: sample length
: cross-section area
: Porosity
: Pore size
Apparent yield stress
Foam
Foam flow rate
Pressure drop
Omirbekov S. et al.,
Adv. in Water Resour. (2020)
Grains
Grains
Coarsening rate
Pore’s radius

## Slide 8: 2. Consequences on confined foam properties
Confined foam
Foam properties
Rheology: Yield stress
Aging: Coarsening
1500
1000
750
550
400
2500
At s
Total liquid fraction

## Slide 9: 2. Consequences on confined foam properties
Aging: Coarsening
Confined foam
Foam properties
Rheology: Yield stress
Bulk foam
Bulk foam
At s
1500
1000
750
550
400
2500
Determined independently under static conditions
We assume that the liquid distribution does not significantly differ under dynamic conditions
Effective liquid fraction of the core foam

## Slide 10: Conclusion & perspectives
Conclusion
  When liquid foam is injected in a granular medium, the liquid redistributes from the core foam towards the surface of the grains and the contacts between the grains. The core foam is therefore drier than the injected foam.
  We have determined the liquid fraction of the core foam at equilibrium and shown that its effective liquid fraction can be used to interpret several properties of confined foam involving non-equilibrium phenomena, such as coarsening and flow of foam through granular media.
  At first order, the coarsening rate and the apparent yield stress for confined foam can be evaluated from the values obtained for bulk foam, using the effective liquid fraction of the core foam instead of the total liquid fraction.
Perspectives
  Validation of our microstructure model with 3D imaging (Ultra-Fast X-ray tomography).
  To study the dynamics of the liquid redistribution during the foam coarsening or the foam flow.
Publications
Pitois O. et al., “Daisy shaped liquid bridges in foam-filled granular packings”, JCIS, 2023
Langlois V. et al., “Permeability of foam-filled granular packings: numerical modeling”, PRF , 2025
Salamé A., et al., “Rheology of liquid foam flowing through porous media”, Physics of Fluids, 2025
Salamé A., et al., “Enhanced coarsening induced by pore confinement”, PRE, 2025
Salamé A., et al., “Foam coarsening in granular packings”, PRE, 2026

## Slide 12: Foam production (coarsening)
Polydispersity index:
Foaming solution:
Non-ionic surfactant
AlkylPolyGlucosides (Glucopon® 225DK)
at 20 g/L in water
Salamé A., et al., “Enhanced coarsening induced by pore confinement”, PRE, 2025
Salamé A., et al., “Foam coarsening in granular packings”, PRE, 2026

## Slide 13: Foam production (foam flow)
Decreases strongly the coarsening rate
Cationic surfactant TTAB at 10 g/L in water.
+
Grains
Control of the distribution of the bubble sizes
Control of the liquid fraction
Perfluorohexane
Reduced length to limit compressibility effects
Salamé A., et al., “Rheology of liquid foam flowing through porous media”, Physics of Fluids, 2025

## Slide 14: 1. Confined foam microstructure & liquid distribution
Model for the liquid distribution in porous space
Daisy shaped liquid bridges in foam-filled granular packings, Pitois O., Salamé A. et al., JCIS, 2023
Permeability of foam-filled granular packings: numerical modeling, Langlois V., Salamé A. et al., PRF , 2025
Assumptions:
Monodisperse spherical grains
Monodisperse bubbles
Perfect wetting
Foam at equilibrium with uniform capillary pressure (with surface tension)