## Slide 1: Self similarity in salt creeping efflorescence crystallization
Rozeline Wijnhorst, Marc Prat and Noushine Shahidzadeh
Van der Waals-Zeeman Institute, Institute of Physics, University of Amsterdam, The Netherlands
Institut de Mécanique des Fluides de Toulouse (IMFT), Université de Toulouse, CNRS Toulouse, France
b
d
e
a
c

## Slide 2
Salt pillars
Salt creeping
Salt Crystallization in nature
Salt lake city
Dead sea

## Slide 3: Crystallization In nature
Saudi Arabia desert
Sand Roses
Gypsum CaSO4
Notes: crystal clusters of gypsum or baryte, which include abundant sand grains.[1][unreliable source?] The "petals" are crystals flattened on the c axis, fanning open in radiating clusters.
The rosette crystal habit tends to occur when the crystals form in arid sandy conditions,[1][unreliable source?] such as the evaporation of a shallow salt basin.
It grows in tropical and subtropical regions of Saudi Arabia

## Slide 4
Damage
Delamination
Mural Paintings
Roman Forum
Copyright-N.Shahidzadeh
Harmful effect of Salts
Efflorescence
Soil salinity
Gypsum effect on sodium soils modification - Everbright

## Slide 5: Understanding the dynamics of salt creeping
Solution level
crystals
Soil
salt
Solution level
Continuous crust made of many small crystallites beyond the solution boundary
University Of Amsterdam
Institute of Physics
Bulk crystallization
Crystallization from porous media
limestone
crystals
R. Hird et al, Proc. R. Soc. A Math. Phys. Eng. Sci. 2016, 472 (2186).
Notes: Besides being an interesting phenomenon, salt creeping is a big problem responsible having salt can be at at high heights in the wall
in walls,. Apart from buildings, creeping also is responsible for the migration of salt from saline regions of the soil to the other parts, thereby leading to sodification of more soil area.

## Slide 6
University Of Amsterdam
Institute of Physics
Mechanism of salt creeping? Quantitative description
Flat surface and rough surface
Internal microscale structure?
Role of Environmental conditions
Impact of salt properties :
solubility , crystal interfacial energy ?
Questions:
Madrid
Notes: Besides being an interesting phenomenon, salt creeping is a big problem responsible for bringing salt from the soil into the building structure, thereby leading to their deterioration. Apart from buildings, creeping also is responsible for the migration of salt from saline regions of the soil to the other parts, thereby leading to sodification of more soil area.
Similarity with the super film of liquid helium II which occurs at room temperature which a lower transfert rate.

## Slide 7: Experimental setup
University Of Amsterdam
Institute of Physics
Vertical creeping
Climatic chamber
T=21°C
RH= 6% and 45%
q
q
Qazi et al. Science Advances 2019
Contact angle and contact line analysis during evaporation up to creeping
Temporal evolution of mass with creeping.
Salt solution
Notes: Water droplet fast evaporation so difficult to study
So we used a vertical substrate with this setup
Climate box to control humidity ONLY CREEPING AT LOW HUMIDITY
Cameras for contact angle and crystal structures
Balance for mass

## Slide 8
General view: NaCl solution
RH=6%
T=21 ͦC
Creeping only at low relative humidity RH ≤30%
Crystal precipitation occurs in bulk prior to creeping
University Of Amsterdam
Institute of Physics
Qazi et al. Science Advances 2019
Notes: the film shows the general view of the process.In the previous experiment we saw the creeping preferentially starting at the sides of the glass slides, the sides of the glass slide are rough. we bring glass cylinder in contact with the salt soltion and let the solution evaporate under very low relative humidity. So, what do we see here is, firstly, the time when the creeping starts increases dramatically. And before creeping we already see the formation of crystals in the bulk. Which means that although the saturation is reached, the creeping doesn’t start right away.

## Slide 9
Evolution of Contact angle up to creeping
Different salts
University Of Amsterdam
Institute of Physics
NaCl
KCl
Na2SO4
                Creeping starts below a critical contact angle
                The lower solubility of the salt solution the lower the critical contact angle
Qazi et al. Science Advances 2019
Initiation of Salt creeping

## Slide 10
Salt creeping growth
University Of Amsterdam
Institute of Physics
Qazi et al. Science Advances 2019
Self amplifying process
Multiple crystals nucleation and growth from thin films
6mm
± 0.02 h-1
KCl
Na2SO4
NaCl
RH=6%
T=21 ͦC
 m(t) =
Notes: the film shows the general view of the process.In the previous experiment we saw the creeping preferentially starting at the sides of the glass slides, the sides of the glass slide are rough. we bring glass cylinder in contact with the salt soltion and let the solution evaporate under very low relative humidity. So, what do we see here is, firstly, the time when the creeping starts increases dramatically. And before creeping we already see the formation of crystals in the bulk. Which means that although the saturation is reached, the creeping doesn’t start right away.
Difference in creeping rates indicates difference in shapes and
surface to volume ratio of crystals
growth coefficient intrinsic property of the salt
Difference between salts : difference in surface to volume ratio of crystals
the film shows the general view of the process.In the previous experiment we saw the creeping preferentially starting at the sides of the glass slides, the sides of the glass slide are rough. we bring glass cylinder in contact with the salt soltion and let the solution evaporate under very low relative humidity. So, what do we see here is, firstly, the time when the creeping starts increases dramatically. And before creeping we already see the formation of crystals in the bulk. Which means that although the saturation is reached, the creeping doesn’t start right away.
Difference in creeping rates indicates difference in shapes and
surface to volume ratio of crystals
 growth coefficient intrinsic property of the salt
Difference between salts : difference in surface to volume ratio of crystals

## Slide 11: Salt creeping lead to efflorescence
Hydrophobic Glass beaker
University Of Amsterdam
Institute of Physics
From bulk solution
R. Wijnhorst et al. Physical Review Applied 2024
Spreading of thin film of salt solution on precipitated crystals
From porous media
R. Wijnhorst et al. arXiv preprint arXiv:2508.18779

## Slide 12
Dynamics of efflorescence formation
Efflorescence creates a porous structure:
Evaporation flux
Veran-Tissoires et al, PRL 2012
Pumping effect , act as sinks
screening effect
Desarnaud et al.J.App. Physics 2015
Notes: House of cards

## Slide 13
1 cm
SEM analysis
University Of Amsterdam
Institute of Physics
outer side
Cauliflowers structure
R. Wijnhorst et al. arXiv preprint arXiv:2508.18
Enhancement of capillary pumping leads to growth up to macroscopic size.
Notes: Salt creeping can initiate and grow on flat surfaces but also on top of porous materials such as soil or stones; this is called efflorescence (4,11,12). The microscopic analysis of the 3D network of such efflorescence reveals an internal porous structure of the crystalline salt network with a fractal structure characterized by a self-organized, self-similar arrangement of salt crystals. Scanning Electron microscopy (SEM) images of sodium chloride (NaCl) creeping efflorescence reveal a structure similar to cauliflowers, and show that this phenomenon covers many orders of magnitude in length scales so that it indeed appears fractal (13). The first precipitating large crystals create large pores between them, enabling smaller crystals to nucleate afterwards within these spaces, which in turn will forming smaller pores, and so on. Again, this porous structure, with different pore size distribution, allows salt water to be sucked in by capillary pumping and crystallization to continue even further.
outer side

## Slide 14: NaCl Crystal size decreases over height: self similar behaviour
3
2
1
Chart: sample 24
radius crystal | 9.773 | 4.6492 | 2.2842
radius pore | 2.7013 | 0.98602 | 0.54891
University Of Amsterdam
Institute of Physics
Fractal dimension of 1.7
complex structure with a high degree of irregularity or roughness
R. Wijnhorst et al. arXiv preprint arXiv:2508.18779
Notes: A good natural example with a fractal dimension close to about 1.7 is the network of blood vessels in the human retina. When measured as a branching 2D pattern, retinal vessel trees often have a fractal dimension around 1.7, meaning they are more complex than a simple line (dimension 1) but do not fully fill an area (dimension 2).

## Slide 15: 3D Micro-Ct scans
The 3D Micro-CT scans by using a z-stack of the Micro-CT slices and applying a box-counting method:
Fractal dimension of approximately 2.5
Branch-shaped structures in nature, such as real cauliflowers (2.8) and broccoli (2.7).
University Of Amsterdam
Institute of Physics
R. Wijnhorst et al. arXiv preprint arXiv:2508.18779

## Slide 16
Efflorescence as a hierarchical porous medium
h1 (level 1)
h2 (level 2)
h3 (level 3)
d1
d2
d3
Slit pore of
aperture ai
Pore structure in halite cubic block of level i
hi
level i
Top view
halite
halite
halite
halite
the thickness of a level can be greater than the level cube size in the model
(several cubes over the thickness)
Sketch for but in fact
1
2
3
1
capillary-viscous competition on efflorescence height?
University Of Amsterdam
Institute of Physics

## Slide 17
Permeability of level i:
Viscous pressure drop over level i (from Darcy’s law):
Viscous pressure drop over n levels:
Maximum capillary pressure on top of efflorescence (with n levels):
Efflorescence as a hierarchical porous medium
University Of Amsterdam
Institute of Physics
R. Wijnhorst et al. arXiv preprint arXiv:2508.18779

## Slide 18
(α = 2)
Computation performed for hi = 2 hi-1
(the thickness of level i is twice the thickness of
level i-1)
Data from cone experiment
d1: 11 microns a1: 3.88 microns
Evaporation flux: j = 8.5 x 10-5 kg/m2/s
Capillary pressure on top of efflorescence
Viscous pressure drop across efflorescence
Capillary pressure in porous substrate (computed for S = 0.11)
<<1
The efflorescence growth is not
limited by capillarity –viscous effect competition
h1 = 0.1 mm (about 10
level 1 cube sizes)
height of first level:
Height is only limited by the amount of salt present at the beginning of experiment.

## Slide 19
Salt creeping in evaporating droplets
Untreated glass slide
θ= 34 degrees
Plasma treated glass slide
θ= 15 degrees
RH=6%
T=21 ͦC
RH = 6%
T= 21 ͦ C
University Of Amsterdam
Institute of Physics

## Slide 20
University Of Amsterdam
Institute of Physics
Courtesay of
Romane le Dizes Castell
Self–organized structure : Sand Roses
CaSO4 crystals:
1 to 3 meters height
Notes: As different minerals have different crystalline structures reflecting the seven possible lattice structures, the macroscopic patterning is different between different salts. Desert roses typically consist of calcium sulfate (gypsum) or barium sulfate (Barite) with sand grains (SiO2) interspersed between the crystalline structures. When investigated in detail, desert roses reveal also a spectacular self-organized structure analogous to the NaCl but with a different shape: large petals, smaller petals in between these and even smaller ones between those, again reminiscent of a fractal organization. A close-up of the structure by SEM imaging reveals that each petal itself is composed of parallel smaller leaflets, emphasizing the universality of this pattern and the porous structure of the 3D salt network (13). Because of its self-similar porous nature, this assembly of crystals structure in nature can grow up to 1 to 3 meters height. Salt creeping is therefore both universal and self-amplifying, typically initiated by the presence of salt crystals or impurities. It hinges on the formation of numerous crystallites under low humidity conditions, with impurities often serving as nucleation centers or salt mixtures catalyzing this spectacular self-organized process.

## Slide 21
Micro-CT imaging
SEM imaging
University Of Amsterdam
Institute of Physics
Sand Roses
R. Wijnhorst et al. , under review
Porous internal structure on multiple length scales

## Slide 22: Conclusions
Salt creeping : Self amplifying process.
Efflorescence: results from salt creeping on precipitated crystals.
Efflorescence displays self-similarity; growth proceeds across multiple scale leading to fractal pattern.
Smaller versions of the same pattern within the larger formations.
Mechanism can occur at different scale from micro to macro
Fascinating Self-organized mineral deposits
University Of Amsterdam
Institute of Physics

## Slide 24: Box-counting method
Blue or highlighted boxes indicate those containing part of the fractal object.
This process is repeated for progressively finer grids.
The results are then used to plot log(N) vs. log⁡(1/r)
where N is the count of occupied boxes
R is the box size; the slope of this plot yields the fractal dimension.
The fractal shape is covered with a grid of boxes, and the number of boxes containing part of the shape is counted at multiple scales (box sizes) to assess how complexity scales with resolution
Notes: the fractal shape is covered with a grid of boxes, and the number of boxes containing part of the shape is counted at multiple scales (box sizes) to assess how complexity scales with resolution