## Slide 1
Adityra Sahoo, Dr. Raka Mondal
Associate Professor, Indian Institute of Petroleum and Energy, Visakhapatnam
Multiscale homogenization-based transport modeling of porous composite proton exchange membranes for maximum charge transport.
Abstract ID: 75

## Slide 2
(a) Commercial option ~ Poor ionic cluster
(b) Improved micro-phase segregation ~ Efficient ionic network ~ improved ion transport
Objective: Network of Bigger water channels without short-circuiting
The challenges:
  Theoretical: Optimized directive for size modulation.
  Experimental: Post-treatment optimization of pristine/ composite membrane.
  Attempt to achieve better alternative from Nafion
The route for solution: Microphase segregation
Image Source: https://skill-lync.com/student-projects/week-6-fuel-cell-powered-vehicle-model-34
Size of Ionic channels: 1-50 nm,
Walls (polymeric backbone) as obstacles
Transport mechanism
Water permeable region
Ref: DOI:10.1007/s12034-009-0042-8

## Slide 3
Fundamental insights of impact of size and orientation of micro-phase segregation
Macroscopic approach
proton vehicles in whole membrane
Solves for: effective flux
Limitation: membrane as continuum, effective properties considered, Localised variation ignored
Molecular simulation: Effective but requires very high computational load.
Segregation coefficient ()=
So, more segregation ~~~ less
Diffusive-convective-electroosmotic flux of proton through blue zones
Current approach:
Mesoscale: solution for momentum, mass and electrophoretic transport with localised variation; space averaging
Advantage:
Accurate prediction of conductivity with structural and operational changes
White areas – hydrophobic zones, impermeable to ions
Blue zones – water channel, the possible pathway of ions

## Slide 4: Background
Variables: velocity (), pressure (), concentration of proton (), Electric potential ( | Governing Equations
Governing Equations | 
Continuity equation | 
Momentum Balance (Navier Stokes equation) | 
Species balance (Nernst Planck equation) | 
Charge conservation (Poisson equation) | 
 | Governing Equations
Governing Equations | 
Continuity equation | 
Momentum Balance (Navier Stokes equation) | 
Species balance (Nernst Planck equation) | 
Charge conservation (Poisson equation) | 
2-dimensional zonal arrangement
For proton (valence of the charge carrier) ;
System parameters:
Velocity parameter: , Concentration parameter: ,
Reynold’s Number: Peclet Number:

## Slide 5
periodic
1,
1
,
R1 boundary:
Inlet of proton from
Anode side
R3
boundary:
Outlet/ sink of proton from
Cathode side
Flow of water + proton
(1,0)
(1,1)
(0,1)
(0,0)
periodic
Proton conductivity,
where
System conditions and proton conductivity
Variables:
velocity (), pressure (), concentration of proton (), Electric potential (

## Slide 6
Equivalent form of (for hexagonal arrangements)
Equivalent form of where
Composite Electrochemical membrane: application of homogenization theory
Situation: uniform/ non-uniform distribution of additives, charged obstacles in the proton flow-path
Strategy: Use of Homogenised Nernst-Planck-Poisson equation for composite PEM membranes
interfacial area
cell volume
Surface charge
Additive mass fraction ((location))
Homogenized Poisson equation
Homogenized Nernst-Planck-equation without convection
Before homogenization
Before homogenization

## Slide 7
Conductivity prediction for membranes without additives
Proton conductivity decreases along with segregation coefficient
Square pitch
Hexagonal pitch
Cubic pitch
Equivalent form of
Without additive,
Same all over the membrane
Additive dosage (mass/mass) which can be a function of

## Slide 8
More additive: higher conductivity
Hexagonal arrangement gives better at lower, comparable at high
Increasing additive dosage along x-axis: higher conductivity
At lower mean of higher additive gradient along gives same conductivity.
Effect of additive dosage (m/m),
Enhancement in along x-direction

## Slide 9
Parameter | Value | Units | Description
εr | 80 | – | Dielectric constant of water
q | 1.60 × 10⁻¹⁹ | C | Charge of a proton
εo | 8.854 × 10⁻¹² | F/m | Permittivity of free space
kB | 1.38 × 10⁻²³ | J/K | Boltzmann constant
ρ | 1000 | kg/m³ | Density of water
 | 0.001 | Pa·s | Viscosity of water
L | 160 × 10⁻⁶ | m | Membrane thickness
Dw | 1.30 × 10⁻¹⁰ | m²/s | Diffusivity of water
Experimental validation with SPEEK-Zirconium membranes
Excellent agreement between developed membranes and models

## Slide 10
Variation of proton conductivity for different geometries (a) Hydrophobic-square & filler-square (b ) hydrophobic-hexagonal & filler–hexagonal (c) hydrophobic–square & filler-hexagonal (d) hydrophobic-hexagonal & filler-square
Conductivity prediction for membranes with different orientation of additives
For maximum ionic conductivity hydrophobic-hexagonal & filler–hexagonal arrangement is best
Diffusive flux become nominal in this case, increasing the electromigration effect strongly
For futuristic membranes, choose the operating conditions based on these parametric behavior.
Velocity parameter: , Concentration parameter: , Reynold’s Number: Peclet Number:
Variation of average ionic conductivity

## Slide 11
Effect of surface charge and size of additive on ionic conductivity
By increasing the additive size with respect to additive enhances the conductivity, limited by experimental difficulty
Negative surface charge enhances the ionic conductivity manifold

## Slide 12
Mesoscale modelling successfully predicted proton transport in PEM membranes.
Optimized micro-phase segregation improved ionic conductivity.
Hexagonal arrangements showed the best transport performance.
Additive dosage, size, and surface charge enhanced conductivity.
Experimental results validated the developed model successfully.
Conclusion

## Slide 13
F1, Tech Horizon Building, Chemical Engineering,
IIPE, Visakhapatnam
+91-9932631600
rakam.che@iipe.ac.in/ rakamukherjee10@gmail.com