## Slide 1
2026.5
Micro-CT and SEM characterization on biochar-modified wellbore cement exposed to a CO2-rich environment
Liwei Zhang, Theogene Hakuzweyezu, Yan Wang, Manguang Gan

## Slide 2
Geologic Carbon Storage and Engineering Safety Research Center
The center was founded in 2004 and is one of the largest CCUS research centers in China.
40+ full-time researchers (including postdocs and employed engineers)
Research directions cover almost all fields of CO2 geological utilization and storage
Key research direction 1: Site selection and source-sink matching, system risks and cost analysis, regulation and commercialization
Key research direction 2: THMC coupling theory of CO2-water-mineral systems
Key research direction 3: Evaluation and monitoring of CO2 storage system integrity and mechanical stability
Key research direction 4: Characterization and control of CO2 corrosion processes

## Slide 3
Meeting with Prof. Michael Celia at Princeton University
Prof. Martin Blunt of Imperial College visited the center
Meeting with Prof. Sidney Green at the University of Utah
Visiting Institute for Modelling Hydraulic and Environmental Systems, University of Stuttgart
Visiting the CT center at University of Michigan
Visiting South Dakota School of Mines and Technology
One of the most active international collaboration hubs in China to promote CCUS research
Hosting the session of“Carbon Sequestration in Underground Reservoirs”at GSA Annual Meeting
Hosting the session of“Advances in Imaging Porous Media”at InterPore Annual Meeting

## Slide 4
2
3
1
Raw materials and experimental schemes
CONTENTS
4
Results and discussion
Conclusions
Background and research objectives
Notes: I will introduce the content from the following four parts, the first one is background and objectives.

## Slide 5
Background
01

## Slide 6
Reason for CO2 emissions: more than 80% of the world's primary energy supply is based on fossil fuels
U.S. Environmental Protection Agency (2022), Inventory of U.S. Greenhouse Gas Emissions and Sinks: 1990-2020
CO2 accounts for about 79% of the total greenhouse gas emissions, due to very significant global CO2 emissions from various sectors.
Call on reducing anthropogenic CO2 emissions and achieve net zero emission by 2050
CO2 data on Hawaii’s Mauna Loa constitute the longest record of direct measurements of CO2 in the atmosphere
Background
Reducing GHG emissions is an important strategic requirement for the world

## Slide 7
Zero-carbon emission
Carbon negative
The green development of traditional fossil energy and the use of low-carbon energy
The development of new zero-carbon energy and zero-carbon industrial process
Strengthening CO2 resource utilization and ecosystem carbon sequestration
Carbon emission reduction
Carbon utilization and removal
Pathways to net zero emissions
The global pathway to net zero emissions
A promising technology: CCUS (CO2 capture, utilization, and storage)
CCUS refers to the industrial process of separating CO2 from industrial emission sources and directly using or permanently storing it to achieve CO2 reduction
Background

## Slide 8
Background
Given that wellbores are globally distributed and are integral to CO2 geological utilization and storage projects, it is imperative to study their leakage risks.
Distribution of oil and gas wells worldwide
(Adopted from IPCC, 2005)
Distribution of Wellbores at the Weyburn
CO2-EOR Project Site in Alberta, Canada
(Adopted from Laumb et al., 2016)
Well no.：
~20000
Unknown leakage risk for most wells
For CCUS projects, CO2 leakage via wellbores is a big concern

## Slide 9
Casing-cement interface flow
Matrix flow and diffusion
Fracture/cement defect/mud channel flow
Cement-caprock interface flow
(Adopted from Viswanathan et al. 2008)
CO2 leakage from wellbores: a major CO2 leakage pathway for CCUS projects
(Adopted from Gasda et al. 2004)
CO2 leakage from wellbores impairs long-term safe CO2 storage of CCUS projects and causes environmental concerns.
Background

## Slide 10
Wellbore cement: An alkaline porous material serving as a protective layer for wellbore casing. Hydrated wellbore cement contains calcium hydroxide, calcium silicate hydrate, ettringite, calcium sulphoaluminate hydrate, etc.
CO2-rich environment
Permeability and porosity increase at the reaction zone
Most minerals in hydrated cement are prone to acid attack
Research needs
CCUS conditions: Low pH, high concentrations of CO2, H2S, SO42-, etc.
With large amounts of CO2 injection, the pH of the formation water can drop below 3.0 w/o buffering effect
Exposure of wellbore cement to CCUS conditions: Permeability and porosity increase and loss of cement integrity
(Zhang et al., 2013)
Background

## Slide 11
https://growingthegoodlife.net/
Applications of biochar
Soil Fertility Improvement and Agricultural Production
Carbon Sequestration and Climate Change Mitigation
Background
Introduction to biochar
This study shows that biochar can also be utilized as a wellbore cement additive to mitigate CO2 alteration to wellbore cement
Production of biochar
Soil and Water Pollution Remediation
Livestock Waste Management and Circular Agriculture
Enhancement of Ecological Restoration and Reforestation
Biochar is a stable carbon-rich and porous material produced by heating organic biomass under oxygen-limited conditions. It has a high surface-to-volume ratio, porous structure, and enriched functional groups on the surface (such as –OH and –COOH).

## Slide 12
Research objectives
Build cement degradation testing system under THMC coupled conditions and conduct cement degradation experiments for RF, BC and supercritical CO2-treated biochar (SCBC) samples
Conduct CT, SEM and QEMSCAN characterization of cement samples after CO2 reaction experiments to visualize cement integrity loss, and validate the CO2-resisting performance of BC and SCBC samples
Study the mechanisms of BC and SCBC additives to resist CO2 alteration
Research objectives

## Slide 13
Raw materials and experimental schemes
02

## Slide 14
Dispersant
Cement
Water reducer
SCBC
Water
BC
Slurry Mixer
Sample molding
1 wt.% NaCl
Curing and CO2 reaction vessel
(a)Raw materials
(b)Slurry and sample preparation
(c) Sample curing and CO2 exposure
CO2 cylinder
Water
Raw materials and experimental schemes
Materials and testing method
Batches of cement slurries were prepared, and different tests were performed to evaluate their mechanical properties and physicochemical characteristics
Group | Cement | Water | Dispersant | Superplasticizer | Biochar | ScCO2 treated biochar
RF | 200 | 88 | 3 | 4 | 0 | 0
SCBC | 200 | 88 | 3 | 4 | 0 | 4
BC | 200 | 88 | 3 | 4 | 4 | 0
Mix proportions of control and biochar added cement mixes
Notes: I will introduce the content from the following four parts, the first one is background and objectives.

## Slide 15
Raw materials and experimental schemes
A schematic diagram illustrating the components of a HPHT curing/carbonation vessel
Experimental parameters
Curing temperature: 62 oC
Curing pressure : 17MPa
Solution: 1wt% NaCl
Curing time: 14 d
Reaction temperature: 62 oC
Reaction time with CO2: 14d
Reaction pressure : 17MPa
Solution: 1wt% NaCl
Curing and reaction devices used at IRSM-CAS
HPHT curing/carbonation process
Reaction
Curing
Notes: I will introduce the content from the following four parts, the first one is background and objectives.

## Slide 16
Zeiss Xradia 410 micro-CT scanner
The pore size in cementitious materials generally falls within the range of 0.5–1000 nm. Consequently, micro-CT, with a highest resolution of around 0.5 μm, is inadequate for directly characterizing the pore structure of cement.
However, after cement reacts with CO2, tiny pores in cement are connected due to the dissolution of cement materials, and the newly formed pores are large enough for micro-CT observation. Therefore, it is appropriate to use micro-CT to characterize the structural changes of cement after exposure to CO2.
Primary characterization method: micro-CT scanning
Raw materials and experimental schemes

## Slide 17
Noise reduction and filtering of images (optional)
(a) Distinguish of features spots in cement surface before and after the reaction for registration purpose
(b) Selection of slices before and after the reaction, and then the slices were registered and aligned
(c) Acquisition of grayscale difference
(d) 2D and 3D visualization of cement degradation
The workflow of CT image post-processing
Before
After
Before
After
(Miao et al., 2020; Gan et al., 2024)
Raw materials and experimental schemes

## Slide 18
This study uses high-quality, high-resolution FE-SEM combined with QEMSCAN analysis to demonstrate the structural evolution of pores and mineral composition in different reaction zones within cement after reacting with CO2.
Although CT imaging can visualize the general evolution of pore structure in cement, its resolution limitations prevent the characterization of individual nanoscale pores after CO2 reaction.
To fully capture the multiscale evolution of pore structure in wellbore cement following CO2 corrosion, the combined use of CT scanning and high-resolution techniques (e.g., field emission SEM) is essential.
FE-SEM and QEMSCAN
Raw materials and experimental schemes

## Slide 19
Results and discussion
03

## Slide 20
For BC, the carbonation region is smaller than that of RF, leading to a lower carbonation depth compared with RF
For BC, the dissolution region is larger than that of RF, leading to a higher alteration depth compared with RF
For SCBC, both the carbonation and dissolution regions are smaller than those of RF, leading to lower carbonation and alteration depths compared with RF The SCBC sample has the best alteration resistance
Micro-CT analysis
Hakuzweyezu et al., 2026a, 2026b
Wang et al., 2026
Carbonation depth
Alteration depth
It is necessary to distinguish carbonation depth from alteration depth
CT characterization results
Notes: I will introduce the content from the following four parts, the first one is background and objectives.

## Slide 21
RF
Significant alteration occurs on the external surface of both RF and BC samples
CT slices revealing CO2-induced chemical alteration (YZ direction)
For the SCBC sample, both the carbonation and the dissolution regions are smaller than those of the RF and BC samples
CT scanning has been proved to be a good tool to evaluate the level of CO2-induced degradation of different cement samples
Micro-CT analysis
Before reaction
After reaction
Gray value change
SCBC
BC
CT characterization results
Notes: I will introduce the content from the following four parts, the first one is background and objectives.

## Slide 22
The SCBC sample demonstrated superior resistance to CO2 corrosion with a carbonation inhibition efficiency of 30.97%, compared to the BC, which had an efficiency of only 6.49%.
Group | Carbonation depth/μm | Standard deviation | Inhibition efficiency/%
RF | 594.75 | 154.53 | —
CM | 332.84 | 35.92 | 44.04
BC | 556.13 | 38.46 | 6.49
CA | 807.55 | 116.00 | -35.78
GP | 438.82 | 29.52 | 26.17
SCBC | 410.56 | 30 | 30.9
Carbonation depth of the cement samples with different additives
MgO | 502.4 | 20 | 
15.5
Analysis of carbonation depth
Carbonation depth/µm
CT-derived carbonation depth results
Notes: I will introduce the content from the following four parts, the first one is background and objectives.

## Slide 23
The XRD spectrum did not exhibit discernible peaks indicative of the formation of new minerals following the addition of BC.
XRD analysis
XRD patterns of samples RF and BC
XRD characterization results
Notes: I will introduce the content from the following four parts, the first one is background and objectives.

## Slide 24
Scan area：1.5 x 1.5 mm
A large amount of SiO2 is observed in the dense carbonate layer (Layer 2), due to the dissolution of C-S-H.
In the Ca(OH)2 dissolution layer (Layer 3), SiO2 is scarce because very limited C-S-H gets dissolved (pH higher than that in Layer 2).
The main mineral blocking the internal nano-pores of the cement is gypsum due to dissolution of ettringite/monosulfate.
The pH gradient is the key factor to drive the reactions.
Scan area：1.4 x 1.2 mm
Gypsum (CaSO4·2H2O) was generated in the reaction layer 4.
High
Low
pH
High
Low
pH
(Wang et al., 2026)
FE-SEM and QEMSCAN results--RF
SEM and QEMSCAN mineralogical analysis of RF

## Slide 25
QEMSCAN mineral composition mapping results for the biochar-modified sample after reacting with CO2. a) SEM of the SCBC sample after reaction with CO2; b) Mineral maps of different zones; c) Mineral list.
SCBC sample shows a higher hydration rate than that of the control sample due to less presence of unhydrated cement grains
Based on the mineralogical distribution, it is evident that Zone 1 of the SCBC sample is less porous than that of the control sample.
Small biochar particles can “immerse into” the cement matrix, while large biochar particles are not compatible with cement matrix. Particle size of biochar needs to be carefully controlled
Biochar contains sulfur, promoting generation of gypsum (CaSO4·2H2O) in the reaction layer 4.
FE-SEM and QEMSCAN results--SCBC
Scan area：1.5 x 1.5 mm
Scan area：1.3 x 1.4 mm
SEM and QEMSCAN mineralogical analysis of SCBC
Notes: I will introduce the content from the following four parts, the first one is background and objectives.

## Slide 26
Mechanical strength analysis
RF sample’s compressive strength declined by 40.5% after 28 days of CO2 exposure.
BC sample’s compressive strength declined by 20.5% after 28 days of CO2 exposure.
The SCBC sample demonstrated superior resistance to CO2 alteration. After 14 days of CO2 exposure, the compressive strength of SCBC increased from 23.66 MPa to 29.97 MPa, reflecting a 26.7% improvement. The sample gained 34.4% in compressive strength after 28 days of CO2 exposure.
SCBC outperforms all other samples in mechanical strength repair. Conversely, the compressive strengths of all other samples decreased under the same reaction condition.
Compressive strength test
Notes: I will introduce the content from the following four parts, the first one is background and objectives.

## Slide 27
Discussion
SEM micrograph showing pores created in biochar during pyrolytic conversion of saw dust to biochar
Micropore filling of CO2
Van der wall interaction between CO2 and surface groups on biochar
H-bonding between surface functional groups in biochar and CO2
Lewis acid-base interaction between N-containing functional groups in biochar and CO2
Pores and functional groups in biochar treated by ScCO2
(Modified from Świechowski et al. 2022)
ScCO2
treatment
Notes: I will introduce the content from the following four parts, the first one is background and objectives.

## Slide 28
Schematic diagram illustrating the reinforcement mechanisms of supercritical CO2 modified biochar in cement matrix: (i) showing cement-only system (ii) showing biochar-modified cement system
Key reinforcement mechanisms include: (a) pre-loaded CO2 promoting pore-blocking carbonate growth within the cement, (b) CO2 pre-treatment increasing biochar’s surface area for localized pH buffering, and (c) strong water holding capacity aiding in internal curing within the cement matrix.
Reinforcement mechanisms of SCBC
Discussion
Notes: I will introduce the content from the following four parts, the first one is background and objectives.

## Slide 29
Conclusions
04

## Slide 30
Under GCS conditions, wellbore cement samples with no biochar additives experienced significant deterioration, whereas those containing BC and SCBC exhibited reduced damage.
Cement containing supercritical CO2-modified biochar (SCBC) is effective in resisting CO2 corrosion, with a carbonation inhibition efficiency of 30.97%, compared to the BC, which had an efficiency of only 6.49%.
After 14 d of CO2 exposure, the compressive strength of SCBC increased from 23.66 MPa to 29.97 MPa, reflecting a 26.66% improvement. Conversely, the compressive strength of RF decreased by 28.66%, and the compressive strength of BC declined by 24.69% under the same conditions. This result suggests that SCBC outperforms unmodified biochar in mechanical strength repair.
SCBC’s reinforcement mechanisms included: (a) pre-loaded CO2 promoting pore-blocking carbonate growth within the cement, (b) CO2 pre-treatment increasing biochar’s surface area for localized pH buffering, and (c) strong water holding capacity aiding in internal curing within the cement matrix.
Conclusions

## Slide 31
Thank You for Your Attention!
Contact: Liwei Zhang (lwzhang@whrsm.ac.cn)

## Slide 32
Typical composition of BC(biochar)
Typical composition of different materials (from XRF)
Biochar | Particle size (mesh) | Bulk Density (g/l) | Specific surface area (m2/g) | pH
Quantity | 200 | 400-450 | 900-1300 | 7-9
Oxide composition of SCBC determined by XRF
Oxide | Na2O | MgO | Al2O3 | SiO2 | P2O5 | SO3 | Cl | CaO | Fe2O3 | Carbon
Wt.% | 1.330 | 0.042 | 0.174 | 1.328 | 4.661 | 0.508 | 0.155 | 0.072 | 0.064 | 91.667
Oxide | Na2O | MgO | Al2O3 | SiO2 | P2O5 | SO3 | Cl | CaO | Fe2O3 | Carbon
Wt.% | 0.328 | 0.114 | 0.358 | 2.112 | 9.722 | 0.696 | 0.132 | 0.114 | 0.137 | 86.287
Oxide composition of BC determined by XRF
Supporting slide