## Slide 1
Observation of Gas and Water Distributions
in a Proton Exchange Membrane Water Electrolyzer
Using Operando X-ray CT
○ Satoru Kato , Tetsuichiro Hayakawa, Yuki Higuchi, Yusaku Nishimura, Toshikazu Satoh, Wataru Yoshimune
(TOYOTA Central R&D Labs., Inc.)
MS10, 303
InterPore 2026

## Slide 2
Porous materials enable complex transport in water electrolyzers.
Porosity
30～70%
Pore size
1～100µm
1. Introduction
CL: Catalyst Layer
PTL: Porous Transport Layer
e-
H+
H2O
H2O
O2
H2
e-
Channel
PEM: Proton Exchange membrane
CL
PTL
Porosity
30～70%
Pore size
1nm～1µm
Channel
Anode
Cathode
Schematic of water electrolyzer

## Slide 3
Anode reactions are inhibited by poor contact or water blockage.
Schematic of water electrolyzer
1. Introduction
CL
PTL
e-
H+
H2O
H2O
O2
H2
e-
Channel
CL
Channel
Anode
Cathode
PEM
PTL
Good balance
of transport
Poor PTL/CL contact
Dense PTL blocks water transport
Bubbles blocks water transport
Variations in local structure and transport phenomena

## Slide 4
2. Challenge & Approach
Challenge:
Clarify reaction distributions based on local structure and transport.
Approach:
Operando X-ray CT visualization of local structure and transport.
N2
H2O
N2,H2,H2O
O2,H2O
Anode
Cathode
Suggested variation of local structure and transport phenomena
Good balance
of transport
Less contact
of PTL and CL
Dense PTL
block water
Bubble
block water
X-ray Camera

## Slide 5
2. Experimental
Schematic of Operand X-ray CT measurement during water electrolysis.
N2
H2O
N2,H2,H2O
O2,H2O
Anode
Cathode
Conducted at BL33XU (Toyota BL) at SPring-8
・ X-ray Energy 27 keV
・ Scan time 2 sec
・ Voxel resolution 3 μm
Sample
・ An-PTL : Titanium paper
・ An-CL : IrOx + Nafion
・ Membrane : NR211
・ Ca-CL : Pt/C + Nafion
・ Ca-PTL : Carbon – paper
Procedure
1. Scan under dry condition
2. Scan under water supplying condition
3. Scan under water electrolysis operation
Toyota Beamline
Since 2009
X-ray Camera

## Slide 6
2. Experimental
Schematic of Operand X-ray CT measurement of during water electrolysis.
N2
H2O
N2,H2,H2O
O2,H2O
Anode
Cathode
CL
PTL
PEM
PTL
CL
A series of sliced X-ray CT images.
Segmented 3D image
3 mm
3 mm
2.3 mm
1.2 mm
2.4 mm
2.3 mm
460
μm
X-ray Camera

## Slide 7
3. Result & Discussion
Cathode
Anode
(1) 3D image of CL contacting PTL.
Heterogeneous CL/PTL contact is observed.
“Dense” implies blocked water transport
“Coarse” implies poor PTL/CL contact.
2.3 mm

## Slide 8
3. Result & Discussion
Cathode
Anode
(2) 3D image of An-PTL during water electrolysis.
Extracted as 60μm thickness domain which close to An-CL.
Heterogeneous water/oxygen distribution near Anode-CL.
Oxygen occupation imply bubble block.
2.3 mm

## Slide 9
3. Result & Discussion
Cathode
Anode
(3) 3D image of Ca-PTL during water electrolysis.
Extracted as 60μm thickness domain which close to Ca-CL.
In Ca-PTL domain closing to Ca-CL, water distribute heterogeneously.
“Water” implies activity at the oposite Cathode-CL.
or
“Water” implies low activity at the opposite Cathode-CL.
or
2.3 mm

## Slide 10
scan
3. Result & Discussion
ROI scanning yields local water saturation and contact ratios.
Local correlations determined by comparing identical XY positions.
Cathode
Anode
 |  | X |  |  |  |  | 
 |  | 0 | 15 | … | … | … | 650
Y | 0 |  |  |  |  |  | 
 | 15 |  |  |  |  |  | 
 | … |  |  |  |  |  | 
 | … |  |  |  |  |  | 
 | … |  |  |  |  |  | 
 | 650 |  |  |  |  |  | 
 |  | X |  |  |  |  | 
 |  | 0 | 15 | … | … | … | 650
Y | 0 |  |  |  |  |  | 
 | 15 |  |  |  |  |  | 
 | … |  |  |  |  |  | 
 | … |  |  |  |  |  | 
 | … |  |  |  |  |  | 
 | 650 |  |  |  |  |  | 
 |  | X |  |  |  |  | 
 |  | 0 | 15 | … | … | … | 650
Y | 0 |  |  |  |  |  | 
 | 15 |  |  |  |  |  | 
 | … |  |  |  |  |  | 
 | … |  |  |  |  |  | 
 | … |  |  |  |  |  | 
 | 650 |  |  |  |  |  | 
scan
scan
scan
scan
scan
scan
scan
scan
(1) PTL/CL contact
(2) water saturation
in An-PTL
(3) water saturation
in Ca-PTL
X
Y
vs
vs

## Slide 11
3. Result & Discussion
Most data points fall within a triangular domain.
(1) PTL/CL contact
(2) water saturation in An-PTL
(3) water saturation in Ca-PTL
Chart: 
Chart: 
Water saturation
in Ca-PTL
Water saturation
in Ca-PTL
PTL/CL contact percentage
Water saturation in An-PTL

## Slide 12
3. Result & Discussion
Chart: 
Chart: 
Water saturation
in Ca-PTL
Water saturation
in Ca-PTL
PTL/CL contact percentage
Water saturation in An-PTL
(1) PTL/CL contact
(2) water saturation in An-PTL
(3) water saturation in Ca-PTL

## Slide 13
3. Result & Discussion
Chart: 
Chart: 
Water saturation
in Ca-PTL
Water saturation
in Ca-PTL
PTL/CL contact percentage
Water saturation in An-PTL
(1) PTL/CL contact
(2) water saturation in An-PTL
(3) water saturation in Ca-PTL
Explainable ?

## Slide 14
3. Result & Discussion
Water saturation
in An-PTL (%)
PTL/CL contact percentage(%)
Water saturation
in Ca-PTL (%)
(Average in classes)
0-10
10-20
20-30
30-40
40-50
50-60
60-70
70-80
20-30
30-40
40-50
50-60
60-70
70-80
80-90
90-100
Optimal PTL/CL contact: 40–60%

## Slide 15
3. Result & Discussion
Water saturation
in An-PTL (%)
PTL/CL contact percentage(%)
Water saturation
in Ca-PTL (%)
(Average in classes)
0-10
10-20
20-30
30-40
40-50
50-60
60-70
70-80
20-30
30-40
40-50
50-60
60-70
70-80
80-90
90-100
Optimal PTL/CL contact: 40–60%

## Slide 16
3. Result & Discussion
Water saturation
in An-PTL (%)
PTL/CL contact percentage(%)
Water saturation
in Ca-PTL (%)
(Average in classes)
0-10
10-20
20-30
30-40
40-50
50-60
60-70
70-80
?
20-30
30-40
40-50
50-60
60-70
70-80
80-90
90-100
Most regions can be explained by PTL/CL contact and Anode saturation.

## Slide 17
5. Conclusion
Analyze reaction distribution in PEM water electrolyzer based on 4 type phenomena resulting in local structure and transport phenomena.
Approach:
Visualizing local structure and transport phenomena by Operand X-ray CT under operating condition shows.
Anode reaction distribution is mainly governed by contact and transport parameters.

## Slide 19
Chart: 
Chart: 
Chart: 
| 0-10 | 10-20 | 20-30 | 30-40 | 40-50 | 50-60 | 60-70 | 70-80
20-30
30-40 | 2.8522 | 3.7067
40-50 | 3.4545 | 3.8836 | 4.2671 | 4.3237 | 2.8312
50-60 | 3.8059 | 4.4491 | 4.4652 | 4.6253 | 5.8144 | 4.6076
60-70 | 3.7972 | 4.1485 | 4.6878 | 4.7917 | 5.3009
70-80 | 3.674 | 3.9392 | 4.3397 | 3.8953 | 2.1339
80-90
90-100
Chart: 
| 0-10 | 10-20 | 20-30 | 30-40 | 40-50 | 50-60 | 60-70 | 70-80
20-30
30-40 | 2.8522 | 3.7067
40-50 | 3.4545 | 3.8836 | 4.2671 | 4.3237 | 2.8312
50-60 | 3.8059 | 4.4491 | 4.4652 | 4.6253 | 5.8144 | 4.6076
60-70 | 3.7972 | 4.1485 | 4.6878 | 4.7917 | 5.3009
70-80 | 3.674 | 3.9392 | 4.3397 | 3.8953 | 2.1339
80-90
90-100
Chart: 
| 0-10 | 10-20 | 20-30 | 30-40 | 40-50 | 50-60 | 60-70 | 70-80
20-30
30-40 | 2.8522 | 3.7067
40-50 | 3.4545 | 3.8836 | 4.2671 | 4.3237 | 2.8312
50-60 | 3.8059 | 4.4491 | 4.4652 | 4.6253 | 5.8144 | 4.6076
60-70 | 3.7972 | 4.1485 | 4.6878 | 4.7917 | 5.3009
70-80 | 3.674 | 3.9392 | 4.3397 | 3.8953 | 2.1339
80-90
90-100

## Slide 20
X-ray CT can visualize water distribution and microstructure in electrode.
Catalyst Layer
PTL
e-
H+
H2O
H2O
O2
H2
e-
Channel
PEM
Catalyst Layer
PTL
Channel
Anode
Cathode
Schematic of water electrolyzer
Cross sectional image of water electrolyzer
obtained by X-ray CT
1. Introduction

## Slide 21
It is suggested that reaction occur at the catalyst layer witch contact with PTL
due to insufficient electroconductivity in catalyst layer.
Schematic of water electrolyzer
Heterogeneously water transport
H2O
1. Introduction
Catalyst Layer
PTL
e-
H+
H2O
H2O
O2
H2
e-
Channel
Catalyst Layer
Channel
Anode
Cathode
PEM
PTL

## Slide 22
It is suggested that reaction cannot occur under the dense PTL domain
due to the water transport blocking .
Schematic of water electrolyzer
H2O
1. Introduction
Heterogeneously water transport
Catalyst Layer
PTL
e-
H+
H2O
H2O
O2
H2
e-
Channel
Catalyst Layer
Channel
Anode
Cathode
PEM
PTL

## Slide 23
It is suggested that reaction cannot occur due to oxygen bubble coverage on the catalyst layer surface.
Schematic of water electrolyzer
1. Introduction
Heterogeneously water transport
Catalyst Layer
PTL
e-
H+
H2O
H2O
O2
H2
e-
Channel
Catalyst Layer
Channel
Anode
Cathode
PEM
PTL