## Slide 1: A stress-strain constitutive model for bentonite-based engineered barriers considering adsorption, capillarity and pore structure evolution
Session: 4.1 - MS12
22th May 2026 – 09:20 am
Nantes, France
PRESENTED BY
Alessandro PARZIALE Angelica TUTTOLOMONDO
Lyesse LALOUI

## Slide 2: OUTLINE
Introduction
Water retention framework
Mechanical framework
Model calibration
Model performance
Conclusions

## Slide 3: Multi-barrier concept for geological disposal
Metallic canister
(HLW)
Bentonite
blocks
Host rock
Bentonite buffer
Liner
Safety functions (system-level) |  |  | 
Isolation | Mechanical support | Radionuclides retention | Long-term stability
Safety functions (barrier-level) |  | 
Low hydraulic conductivity | Swelling pressure | Sorption capacity
Controlling factors (barrier-level) |  |  | 
Dry density | Degree of saturation | Temperature | Pore structure

## Slide 4: Pore structure evolution
PSD
Pore size diameter
After wetting (constant volume)
Dry state
1
2
PSD
Pore size diameter
After compaction
Before compaction
1
2
Waste
Waste
Wetting front
Mechanical load
Host rock
Host rock
microstructure
macrostructure
microstructure
macrostructure
after Lloret et al., 2003
after Seiphoori et al., 2014
Mechanical effect
Hydration effect
Lloret et al. (2003). Mechanical behaviour of heavily compacted bentonite under high suction changes. Geotechnique. 53. 27-40. 10.1680/geot.2003.53.1.27.
Parziale, A., Tuttolomondo, A., & Laloui, L. (2026). Advances in understanding and modelling compacted expansive clays: a constitutive approach. Canadian Geotechnical Journal. 63. 1-19. 10.1139/cgj-2025-0669.
Seiphoori, A., Ferrari, A., & Laloui, L. (2014). Water retention behaviour and microstructural evolution of MX-80 bentonite during wetting and drying cycles. Geotechnique. 64. 721-734. 10.1680/geot.14.P.017.
How to include this stress-path dependency of the pore structure into a stress-strain constitutive model?
Bentonite
Bentonite

## Slide 5: OUTLINE
Introduction
Water retention framework
Mechanical framework
Model calibration
Model performance
Conclusions

## Slide 6
A double structure water retention model
Yield functions:
Definition of degree of saturation (Qiao et al., 2021):
Flow rules:
Hardening rules:
AWRC parameters | CWRC parameters | Contribution factor
AWRC parameters | CWRC parameters | Contribution factor
Parziale, A., Tuttolomondo, A., & Laloui, L. (2026). Advances in understanding and modelling compacted expansive clays: a constitutive approach. Canadian Geotechnical Journal. 63. 1-19. 10.1139/cgj-2025-0669.
Qiao et al. (2021). A generalized water retention model with soil fabric evolution. Geomechanics for Energy and the Environment. 25. 100205. 10.1016/j.gete.2020.100205.

## Slide 7
Suction, s
wetting
Contribution factor
Degree of saturation
CWRC
AWRC
SWRC
1
2
1
2
Suction, s
1
2
1
2
PSD
Pore size diameter
After wetting (constant volume)
Dry state
1
2
PSD
Pore size diameter
After compaction
Before compaction
1
2
microstructure
macrostructure
microstructure
macrostructure
after Lloret et al., 2003
after Seiphoori et al., 2014
Void ratio, e
compaction
Contribution factor
Degree of saturation
CWRC
AWRC
SWRC
1
2
Suction, s
Mechanical effect
Hydration effect
Lloret et al. (2003). Mechanical behaviour of heavily compacted bentonite under high suction changes. Geotechnique. 53. 27-40. 10.1680/geot.2003.53.1.27.
Parziale, A., Tuttolomondo, A., & Laloui, L. (2026). Advances in understanding and modelling compacted expansive clays: a constitutive approach. Canadian Geotechnical Journal. 63. 1-19. 10.1139/cgj-2025-0669.
Seiphoori, A., Ferrari, A., & Laloui, L. (2014). Water retention behaviour and microstructural evolution of MX-80 bentonite during wetting and drying cycles. Geotechnique. 64. 721-734. 10.1680/geot.14.P.017.
Pore structure evolution under different stress-paths

## Slide 8: OUTLINE
Introduction
Water retention framework
Mechanical framework
Model calibration
Model performance
Conclusions

## Slide 9
Mechanical framework
Strain variable:
Non-linear elasticity:
Yield functions:
Hardening rule:
Effective stress framework:
Flow rules:
Elastic parameters | Isotropic plastic parameters | Deviatoric plastic parameters
Elastic parameters | Isotropic plastic parameters | Deviatoric plastic parameters
Parziale, A., Tuttolomondo, A., & Laloui, L. (2026). Advances in understanding and modelling compacted expansive clays: a constitutive approach. Canadian Geotechnical Journal. 63. 1-19. 10.1139/cgj-2025-0669.

## Slide 10: OUTLINE
Introduction
Water retention framework
Mechanical framework
Model calibration
Model performance
Conclusions

## Slide 11
ACMEG-Ex-S: Calibration
Water retention parameters |  |  |  |  |  |  |  |  |  |  |  | 
Capillary mechanism |  |  |  |  |  | Adsorptive mechanism |  |  |  |  | Contribution factor | 
 |  |  |  |  |  | 65 | 3.8 |  |  |  |  | 
Water retention parameters |  |  |  |  |  |  |  |  |  |  |  | 
Capillary mechanism |  |  |  |  |  | Adsorptive mechanism |  |  |  |  | Contribution factor | 
 |  |  |  |  |  | 65 | 3.8 |  |  |  |  | 
Parziale, A., Tuttolomondo, A., & Laloui, L. (2026). Advances in understanding and modelling compacted expansive clays: a constitutive approach. Canadian Geotechnical Journal. 63. 1-19. 10.1139/cgj-2025-0669.
Seiphoori, A., Ferrari, A., & Laloui, L. (2014). Water retention behaviour and microstructural evolution of MX-80 bentonite during wetting and drying cycles. Geotechnique. 64. 721-734. 10.1680/geot.14.P.017.

## Slide 12
ACMEG-Ex-S: Calibration
Isotropic compression test saturated conditions (Tang, 2005)
Triaxial compression test
saturated conditions (Kim et al., 2024)
Mechanical parameters |  |  |  |  |  |  |  |  |  | 
Elastic parameters |  |  | Isotropic plastic parameters |  |  |  |  | Deviatoric plastic parameters |  | 
 |  |  |  |  |  |  |  |  | 1 | 
Mechanical parameters |  |  |  |  |  |  |  |  |  | 
Elastic parameters |  |  | Isotropic plastic parameters |  |  |  |  | Deviatoric plastic parameters |  | 
 |  |  |  |  |  |  |  |  | 1 | 
Oedometric compression tests at different suction level (Lloret et al., 2003)
Kim et al. (2024). Salinity-dependent ultimate shear strength of compacted Wyoming-type bentonite investigated by triaxial tests. Applied Clay Science. 261. 107576. 10.1016/j.clay.2024.107576.
Lloret et al. (2003). Mechanical behaviour of heavily compacted bentonite under high suction changes. Geotechnique. 53. 27-40. 10.1680/geot.2003.53.1.27.
Parziale, A., Tuttolomondo, A., & Laloui, L. (2026). Advances in understanding and modelling compacted expansive clays: a constitutive approach. Canadian Geotechnical Journal. 63. 1-19. 10.1139/cgj-2025-0669.
Tang, A.M. (2005). Temperature effect on the behaviour of engineered clay barriers. PhD thesis. Ecole des Ponts ParisTech. pastel-00001594.

## Slide 13: OUTLINE
Introduction
Water retention framework
Mechanical framework
Model calibration
Model performance
Conclusions

## Slide 14
ACMEG-Ex-S: Mechanical compression tests
Isotropic compression tests
Oedometric compression tests
Parziale, A., Tuttolomondo, A., & Laloui, L. (2026). Advances in understanding and modelling compacted expansive clays: a constitutive approach. Canadian Geotechnical Journal. 63. 1-19. 10.1139/cgj-2025-0669.
Seiphoori, A. (2014). Thermo-hydro-mechanical characterisation and modelling of MX-80 granular bentonite. PhD thesis. EPFL, Lausanne.
Tang, A.M. (2005). Temperature effect on the behaviour of engineered clay barriers. PhD thesis. Ecole des Ponts ParisTech, Paris.

## Slide 15
ACMEG-Ex-S: Swelling pressure tests
Stress-paths
Literature data
Bucher, F., & Müller-Vonmoos, M. (1989). Bentonite as a containment barrier for the disposal of highly radioactive wastes. Applied Clay Science. 4. 157-177. 10.1016/0169-1317(89)90006-9.
Ferrari et al. (2022). Volume change response and fabric evolution of granular MX80 bentonite along different hydro-mechanical stress paths. Acta Geotech. 17. 3719-3730. 10.1007/s11440-022-01481-0.
Karnland et al. (2008). Sealing ability of Wyoming bentonite pellets foreseen as buffer material – Laboratory results. Physics and Chemistry of the Earth, Parts A/B/C. 33. S472-S475. 10.1016/j.pce.2008.10.024.
Parziale, A., Tuttolomondo, A., & Laloui, L. (2026). Advances in understanding and modelling compacted expansive clays: a constitutive approach. Canadian Geotechnical Journal. 63. 1-19. 10.1139/cgj-2025-0669.

## Slide 16
ACMEG-Ex-S: Free swelling tests
Ferrari et al. (2022). Volume change response and fabric evolution of granular MX80 bentonite along different hydro-mechanical stress paths. Acta Geotech. 17. 3719-3730. 10.1007/s11440-022-01481-0.
Parziale, A., Tuttolomondo, A., & Laloui, L. (2026). Advances in understanding and modelling compacted expansive clays: a constitutive approach. Canadian Geotechnical Journal. 63. 1-19. 10.1139/cgj-2025-0669.

## Slide 17: OUTLINE
Introduction
Water retention framework
Mechanical framework
Model calibration
Model performance
Conclusions

## Slide 18
Conclusions
Microstructural informations embedded in the water retention model
Stress-path dependency of the pore structure
Water retention mechanisms are independently modelled
Validated against hydro-mechanical stress-paths for bentonite
References:
Bucher, F., & Müller-Vonmoos, M. (1989). Applied Clay Science. 4. 157-177.
Ferrari et al. (2022). Acta Geotech. 17. 3719-3730.
Karnland et al. (2008). Physics and Chemistry of the Earth, Parts A/B/C. 33. S472-S475.
Kim et al. (2024). Applied Clay Science. 261.
Lloret et al. (2003). Geotechnique. 53. 27-40.
Parziale et al. (2026). Canadian Geotechnical Journal. 63. 1-19.
Qiao et al. (2021). Geomechanics for Energy and the Environment. 25. 100205.
Seiphoori, A. (2014). PhD thesis. EPFL, Lausanne.
Tang, A.M. (2005). PhD thesis. Ecole des Ponts ParisTech, Paris.
Contact: alessandro.parziale@epfl.ch
Pore structure evolution
Advanced mechanical formulation
Water retention mechanisms
(adsorption + capillarity)
HM stress-paths for bentonite
Mechanics
Hydraulics
Structure
Validation

## Slide 19: Thank you for your attention !
PRESENTED BY
Alessandro PARZIALE Angelica TUTTOLOMONDO
Lyesse LALOUI