## Slide 1: Humidity-driven crystallization and deliquescence of salt in nanopores
Olivier Vincent, Hugo Bellezza, Marine Poizat
CNRS & Univ. Lyon 1, Institute for Light & Matter (Lyon, France)

## Slide 2
Crystallization and Deliquescence
1
NaCl(aq) droplet
50%RH
Notes: Let’s start with a droplet …
We have two phases with a transition line situated at 75%RH for NaCl
Phase diagram

## Slide 3
Crystallization and Deliquescence
1
NaCl(aq) droplet
Relative Humidity
low
high
75%RH
80%RH
Notes: Let’s start with a droplet …
We have two phases with a transition line situated at 75%RH for NaCl
Phase diagram

## Slide 4
Motivations / Applications
2
Atmosphere aerosols
Water harvesting
Soil salination
Shokri et al., 2024
(+ CO2/H2 sequestration, heat/energy storage & conversion etc.)
Civil engineering, heritage conservation , geophysics
Flatt et al., 2014
Espinosa-Marsal & Scherer, 2010
Putnis, 2015
O’Sullivan et al. 2015
Al-Handawi et al. 2023

## Slide 5
Scientific question
3
Critical RH triggering phase change in pores?
Impact of
Salt concentration
Pore size (nm range)
Relative Humidity (RH)
low
high

## Slide 6
Methods
4
Water sorption isotherms
Vacuum system controlled in RH
Samples
Mean pore diameters 3 to 20 nm
Imbibed with NaCl solution
Porous silica and alumina
White light interferometry (WLI)
( water content)
Notes: Soak into salt solution and then put in RH controlled chamber.

## Slide 7
5
AAO
Pore diameter 12 nm
no salt
with salt
Water content (OPL)
crystallization
deliquescence
Relative Humidity
Crystallization and deliquescence define the shape of water sorption isotherms
Water sorption isotherms
Notes: Salt phase transitions define hysteresis, not water capillarity

## Slide 8
Impact of salt concentration
6
No effect of salt amount on the RH of crystallization & deliquescence
Pore size-dependent shift of phase transitions compared to bulk
Notes: Define Kelvin radius here

## Slide 9
Theory
7
Liquid / vapor equilibrium
solubility (mole ratio)
osmotic coefficient
(super)saturation
vapor
capillary
osmotic
(Kelvin)
Confined nucleation theory
Confined nucleation possible only if
r* < rp ≃ rK (steric criterion)

## Slide 10
Theory vs. Experiments
8
bulk equilibrium
steric nucleation

## Slide 11
Theory vs. Experiments
8
bulk equilibrium
steric nucleation
Notes: I know this is what some people would call reasonable agreement, but in reality it shows …

## Slide 12
Theory vs. Experiments
8
bulk equilibrium
steric nucleation
kinetic nucleation

## Slide 13
Theory vs. Experiments
8
bulk equilibrium
steric nucleation
kinetic nucleation

## Slide 14
Steric nucleation vs. Deliquescence
9
Sterically limited nucleation (r* = rp)
3-phase equilibrium
(Talreja-Muthreja et al. Langmuir 2022)
(this work)
Mathematically equivalent!
Notes: Describe the same situation (unstable equilibrium)

## Slide 15
Conclusion & Acknowledgements
10
Salts qualitatively change water uptake/release in nanopores
ANR JCJC (SINCS)
ANR–DFG (SolutInPore)
Hugo Bellezza
Marine Poizat
Capillary condensation
Meniscus evaporation
More info:
Bellezza, H., Poizat, M. & Vincent, O. Salt crystallization and deliquescence triggered by humidity cycles in nanopores. arXiv:2510.27309 (in revision)
Deliquescence (equilibrium)
Crystallization (metastable)
(!)
Notes: Shape and hysteresis of sorption isotherms is not defined anymore by … but by …
Equilibrium, even if metastable
Interesting to finely tune absorption and release of water in materials for various applications

## Slide 16
Supporting Slides

## Slide 17
Water sorption isotherms
s1
cryst.
deliq.
No salt
NaCl 1.6 M
NaCl 2.5 M
NaCl 3.7 M
Water content (relative)
Relative Humidity