## Slide 1: Water Dynamics in Porous Materials: What can we learn from Quasielastic Neutron Scattering?
Denis MORINEAU
CNRS – Institute of Physics of Rennes

## Slide 2: Neutron scattering / Space & time
Characteristics:
Spatial properties are probed via
the scattering vector
Temporal properties are probed via
the transfer of energy -
Structure & trajectories
Length scale ~ 1Å – 100 nm
Time scale ~ 0.1 ps – 100 ns
Incoming neutrons
Scattered neutrons
Sample
QENS ideally-suited for nanoconfined liquids
In the liquid state
D = 2.10−9 m2s−1 and t=1ns,
Principle:

## Slide 3: Neutron Scattering Facilities
European
  ILL Institut Laue Langevin (Grenoble, F) Reactor
  ESS European Spallation Source (Lund, S) Under construction, start 2028
National
  MLZ FRMII (Garching, G) Reactor expected to restart in 2027
  ISIS (Oxford, UK) Spallation Source
  SINQ (CH) Spallation Source
Around 50 research reactors in the world and 8 spallation sources
ILL in Grenoble is currently the most performant facility worldwide
Power 58 MW
40 instruments
Per year : ~1400 researchers from over 40 countries conduct ~ 1000 experiments

## Slide 4: Model Nanoporous hosts - Tuning surface interaction
c = 0.7-1.2 nm
S ≈ 500-1,000 m2/g
V ≈ 0.5-1 cm3/g
X-ray diffraction
100
110
200
210
001
002
Pure Silica
PMOs
001
Silicas (MCM-41) & Periodic Mesoporous Organosilicas (PMOs)
Different bridging units
Water sorption isotherm
Hydrophoby
D = 3-4 nm
M. Fröba et al. J. Phys. Chem. C 2018, 122, 12673−12680
Crystalline arrangement of aligned nanochannels

## Slide 5: Different instruments
IN5B
IN16B
SHARP
Time of flight spectrometer
Backscattering spectrometer
Fast dynamics (vibration, rotation)
t ~ 0.1 à 100 ps
S(, ℏ)
Quasielastic intensity
Slow dynamics
(translational diffusion)
t ~ 0.1 à 1 ns
DE

## Slide 6: Water dynamics in MCM-41 silica
Q dependence:
Temperature dependence:
A. Jani et al. J. Chem. Phys. 154, 094505 (2021)
Modelling
2 motions:
Local fast motion (t =1-3ps)
“intrabassin motion” (rotation, tumbling)
+
Translational diffusion
Spatially restricted Jump diffusion (non-Fickian)
S(, ℏ)
Water motions

## Slide 7: Impact of hydrophilicity of water dynamics
Compared to bulk water :
10 % reduction of diffusivity,
x2-x4 increase of residence time,
Modest effect of surface chemistry
Diffusivity
Residence time
A. Jani et al. J. Chem. Phys. 154, 094505 (2021)

## Slide 8: Ionically Charged Pore Surface
Divinyl-pyridine PMO
Divinyl-methylpyridinium PMO
A. Mozhdehei et al. J. Phys. Chem. C 129, 18311-18324 (2025)

## Slide 9: Ionically Charged Pore Surface
Neutral pore
Charged pore
Jump diffusion
model
~DTQ2 (Fick’s law)
t0
Jump diffusion
model
Mean jump length
Compared to bulk water :
x4 reduction of diffusivity
x10 increase of residence time
No charge effect on jump length (l=2-3 Å)
A. Mozhdehei et al. J. Phys. Chem. C 129, 18311-18324 (2025)
QENS broadening (HWHM)

## Slide 10: Charged vs neutral hydrophilic vs hydrophobic surfaces
Diffusivity
Residence time
Bulk
Hydrophobic
Hydrophilic neutral
Charged

## Slide 11: Variable pore filling : Range of Ionic Charge Interaction?
Spectra (Filled symbols)
IFWS (Open symbols)
Neutral
Charged
75% RH
33% RH
Diffusivities
Residence time
Neutral
Charged
33% RH
75% RH
%RH has small impact on dynamics
compared
to surface charge
HWHM diffusive motion
HWHM diffusive motion

## Slide 12: Acknowledgements - Thank you for your attention !
Benjamin Malfait, Aïcha Jani, Ronan Lefort, Armin Mozdehei, Nadim Kamar, Alain Moréac
Patrick Huber
Michael Fröba
NanoLiquids
N° 18-CE92-0011
SolutinPore
N° 23-CE29-0028
Markus Appel, Bernhard Frick, Jean-Marc Zanotti, Quentin Berrod, Jacques Ollivier
Institute of Physics of Rennes

## Slide 13: QENS modelling
EISFs:
2 motions:
Local fast motion (t =1-3ps)
“intrabassin motion” (rotation, tumbling)
+
Slow dispersive motion
spatially restricted jump translational diffusion
Confined water: A. Jani et al., J. Chem. Phys. 154, 094505 (2021) Bulk water: J. Teixeira et al., Phys. Rev. A 31(3), 1913 (1985)
J. Qvist et al., J. Chem. Phys. 134(14), 144508 (2011)
EISF Local fast motion
EISF slow motion
HWHM slow motion
HWHM slow motion (low-Q)

## Slide 14: MCM-41 silicas
MCM-41 (D = 3.6 nm, ~10s)
DSC
-50K
Melting point
G. H. Findenegg, et al. ChemPhysChem 9, 2651 (2008)
SANS
DTm

## Slide 15: Interfacial layer
Unfreezable surface layer e≈0.6nm
Dielectric Spectroscopy
B. Malfait et al. J. Phys. Chem. C 125, 16864 (2021)
Along with geometrical confinement
Surface plays a central role

## Slide 16: Impact of surface chemistry on H-bonds structure
Totally filled pores (75%RH)
Disrupted ‘bulk-like’ H-bonded structure
Interfacial contribution is overwhelmed by bulk-like order
B. Malfait et al. J. Phys. Chem. C 126, 3520 (2022)

## Slide 17: Impact of surface chemistry on H-bonds structure
Partially filled pores (33%RH)
H-bond structure evidences Water-Surface and Water-Vapor interfaces
Adsorbed
layer
Vapor
Organic
bridge
33% RH
2 types of interfacial
dangling OH
H-bonded
Raman intensity
B. Malfait et al. J. Phys. Chem. C 126, 3520 (2022)

## Slide 18: Impact of hydrophilicity of water dynamics
Jump diffusion
model
~DTQ2
t0
HWHM diffusive motion