## Slide 1: Periodic Mesoporous Organosilicas as Host Materials for Studying Surface Chemistry and Pore Size Effects on the Properties of Nanoconfined Water
P. Lenz, U. Sazama, S. König, S.-M. Meinert, M. Steiger and M. Fröba
Institute of Inorganic and Applied Chemistry University of Hamburg, Germany
Anorganisch-Chemisches Kolloquium, Universität Bayreuth, 17. Mai 2022

## Slide 2: Research
Carbons and polymers
2
1 µm
Confinement
Periodic mesoporous organosilicas (PMOs)
Metal-Organic Frameworks (MOFs)
Mesoporous silicas (M41S/SBAs)
Notes: Synthesis: phase separated alkali borosilicate glasses
Applications:
reference materials for texture analytic methods MPI, PALS, N2 Sorption,
inert support for enzyme immobilization
transparent support for photochemical applications

## Slide 3: Research ̶ Systems in nanoconfinement
Water/ice/vapor
3
Binary mixtures
salts/salt hydrates
alkanediamines
n= 2…7
alkanedioles & glycerol
n= 3…9
Aqueous solutions of
aqueous solutions
or
Poster # 43 Anna Westhues
Thu. 21.05.26, 10.05-11.35 a.m.
Poster # 46 Sonja Kemmerer
Wed. 20.05.26, 3.35-5.05 p.m.
Notes: Synthesis: phase separated alkali borosilicate glasses
Applications:
reference materials for texture analytic methods MPI, PALS, N2 Sorption,
inert support for enzyme immobilization
transparent support for photochemical applications

## Slide 4: Mesoporous silica (MCM-41 type)
Nitrogen physisorption (77 K)

## Slide 5: Water/ice in mesoporous silica
Melting point of confined water in MCM-41 silica
  smaller pore diameter  lower melting point
  no freezing in pores < 2.8 nm?
liquid
solid
?

## Slide 6: Water/ice in mesoporous silica
Melting point of confined water in MCM-41 silica
  smaller pore diameter  lower melting point
t
R
Different types of water:
free water in the middle of pores which can freeze to form Ih or Ic
non-freezable water (interfacial water)
  in general: 2-3 water layers (t-layer)
  low order
  width can be influenced by surface chemistry
  structure is different from that of both the bulk crystal and liquid “liquid-like” or “quasi-liquid”
ΔTm(R) change of the melting temperature
CGT Gibbs-Thomson-constant
R pore radius
t non-freezable layer

## Slide 7: Periodic mesoporous organosilicas – Wall structure
F. Hoffmann, M. Cornelius, J. Morell, M. Fröba, Angew. Chem. Int. Ed. 2006, 45, 3216-3251.
Periodic Mesoporous Organosilicas (PMOs) with crystal-like pore walls
  high thermal stability
  only observed for rigid organic bridges (all C sp2 hybridized)
  pore diameters in the range of 2 to 10 nm
  metal-free compounds
for terminal Si-groups:
Si = Si(OR)3
R = CH3, C2H5

## Slide 8: Organosilica precursors: examples
BTEVB
hydrophilic
hydrophobic
BTEBP
BTEVB-F
BTEVB-Cl
BTEVB-p2F
BTEVB-o2F
BTEVB-Py
BTEVB-N+I–
BTEVB-NH2
BTEBP-bPy

## Slide 9: Water in PMOs
Water vapor sorption
Differential scanning calorimetry (DSC)
2025
2025

## Slide 10: Water in PMOs
DSC-TGA coupled
2025
2026

## Slide 11: Fluorinated PMOs
XRD and nitrogen physisorption (77 K)
  hexagonal pore arrangement
  crystal-like pore walls
  narrow pore size distribution
  high surface area
4.0 nm
0.81 cm3g-1
866 m2g-1

## Slide 12: Fluorinated PMOs
P. Lenz, S.-M. Meinert, S. König, M. Steiger, and M. Fröba, J. Phys. Chem. C 2025, 129, 12536−12550.
Water vapor sorption (298 K)
  all PMOs with the same surface chemistry, but different pore diameters (2.6 -̶ 4.7 nm)
  isotherms are shifted to higher relative pressure
  effect of pore size (Kelvin equation)

## Slide 13: Repertoire of PMO precursors
Water vapor sorption (298 K)
  all PMOs with the same pore diameter (3.2 nm)
  isotherms are shifted to higher relative pressure (humidity)
  effect of surface polarity!

## Slide 14: Different PMOs
Water vapor sorption (298 K)
  PMOs with the same pore diameter of about 3.8 nm
  isotherms are normalized with respect to the BET surface area of each material to show the number of water molecules per surface unit
P. Lenz, S.-M. Meinert, S. König, M. Steiger, and M. Fröba, J. Phys. Chem. C 2025, 129, 12536−12550.

## Slide 15: Different PMOs
Hydrophilicity indices (HI)
  PMOs with the same pore diameter (3.8 nm)
  all hydrophilicity indices (HI) show the same trend for the different materials
P. Lenz, S.-M. Meinert, S. König, M. Steiger, and M. Fröba, J. Phys. Chem. C 2025, 129, 12536−12550.

## Slide 16: Different PMOs
t-layer thicknesses
  PMOs with different pore diameters (2.5 -̶ 5.5 nm)
  BTEB-PMO shorter organic bridging unit (7.6 vs. 11.8 Å)
  for more hydrophilic pore walls thinner t-layers
P. Lenz, S.-M. Meinert, S. König, M. Steiger, and M. Fröba, J. Phys. Chem. C 2025, 129, 12536−12550.
calculated from adsorption (ta) and desorption (td) isotherms

## Slide 17: Different PMOs
Melting point depression
for larger pores (rP > 1.9 nm), no significant influence of the surface chemistry on the melting point
for smaller pores (rP < 1.9 nm) stronger melting point depression in more hydrophobic materials
P. Lenz, U. Sazama, M. Steiger, and M. Fröba, J. Phys. Chem. C 2025, 129, 20373−20386.

## Slide 18: Different PMOs
Melting (•) and freezing points (Δ)
below the temperature of the intersection of the freezing and melting curve no more first-order phase transition
despite ist hydrophilic nature N-MBTEVP+I−-PMO exhibits the largest values for all critical pore radii
P. Lenz, U. Sazama, M. Steiger, and M. Fröba, J. Phys. Chem. C 2025, 129, 20373−20386.

## Slide 19: Summary
hydrophilicity
Tmelting
t-layer
surface effect has a greater impact on pores smaller than 3.8 nm
larger t-layer  melting occurs at lower temperature
t
R

## Slide 20
Philip Lenz
Sophia Schwake
Tabea Haug
Dr. Tamas Simon
Sarah Claas
Anna Westhues
Christian Köhn
Patrick Funnemann
Timm Kraus
Tim Wagner
Maurice Sifrin
Sonja Kemmerer
Sandra König
Uta Sazama
Dr. Frank Hoffmann
Jingxuan Zeng
Notes: Synthesis: phase separated alkali borosilicate glasses
Applications:
reference materials for texture analytic methods MPI, PALS, N2 Sorption,
inert support for enzyme immobilization
transparent support for photochemical applications

## Slide 21
Acknowledgements
collaborations
  Prof. P. Huber (TU Hamburg)
  Prof. M. Steiger (U Hamburg)
  Prof. D. Morineau (U Rennes)
  Dr. F. Lehmkühler (DESY, Hamburg)
  Prof. M. Thommes (FAU Erlangen-Nuremberg)
  Prof. D. Enke (U Leipzig)
  financial support
Cluster of excellence
Hamburg Centre for Ultrafast Imaging (CUI)