## Slide 1: Cavitation in nanopores Institut de Sciences des Matériaux de Mulhouse – B. Lebeau, H. Nouali, P. Ott ICMN Orléans – Joël Puibasset Institut Néel – P. Coutin, P. Spathis Laboratoire de Physique de l’ENS – K. Davitt, E. Rolley ANR project NanoCav

## Slide 2
Interpore 2026 - Nantes
Evaporation in ordered mesoporous silica
Sharp drop of Vads
+
Evaporation pressure P*  0.45 Psat
(N2 @ 77 K)
[Rasmussen 2010]
[Thommes 2004]
0 0.2 0.4 0.6 0.8 1
P/P0
signature of cavitation
[Thommes 2004]

## Slide 3
Interpore 2026 - Nantes
Evaporation in ordered mesoporous silica
Evaporation pressure P*/P0 lies in the range 0.42 – 0.46
depends on pore size (cavitation more difficult in confined liquid)
 How to identify cavitation unambiguously ?
 Impact of confinement ?
P* dependance on pore radius, temperature…
[Rasmussen 2010]

## Slide 4
Interpore 2026 - Nantes
Capacitive measurements
High accuracy capacitance bridge – resolution 10-5 pF
Relation capacitance – adsorbed mass:
see you at poster session Thursday 10:05
= 20 mm
Espacement = 0.1 mm
SBA-16  = 8 nm
Sample mass = 10 mg
N2 @ 77.45 K

## Slide 5
Continuous measurements at controlled pressure rate
SBA-16  = 7.6 nm
N2 @ 70.07 K
assuming DC is proportional to the amount of adorbed fluid,
normalization gives the fraction  of filled pores as a function of P
 precise determination of cavitation threshold
as a function of

half
filled
Empty pores
Filled pores
P*
Interpore 2026 - Nantes

## Slide 6
Continuous measurement at controlled pressure rate
SBA-16  = 7.6 nm
N2 @ 70.07 K
assuming DC is proportional to the amount of adorbed fluid,
normalization gives the fraction  of filled pores as a function of P
 precise determination of cavitation threshold
as a function of

 depends of the pore size distribution (= 1 for homogeneous nucleation or heterogeneous with monodiperses pores)
half
filled
Empty pores
Filled pores
Interpore 2026 - Nantes

## Slide 7
Results – shape of A(P)
@ 94.81 K
Homogeneous nucleation : curves A ln collapse on a single master curve
Critical nucleation radius 1.0 nm @ 70 K pore radius RP = 3.8 nm
1.8 nm @ 95 K
Interpore 2026 - Nantes
SBA-16  = 7.6 nm
@ 70.06 K

## Slide 8
Experimental results – phase diagram
Interpore 2026 - Nantes
cavitation
condensation
3 SBA-16 samples
with dif. pore diameter
the larger the pores
the easier the cavitation
Pcav
Pcond

## Slide 9
Experimental results – coefficients a and b
The smaller the pore radius RP
the larger T (hence critical radius R*)
the larger the departure from homogeneous cavitation
homogeneous cav.
homogeneous cav.
Interpore 2026 - Nantes
R*= 1.8 nm
R*= 1 nm

## Slide 10
Large cavities (inter-grains ?) cavitation
Interpore 2026 - Nantes
N2 @ 70 K
additionnal evaporation step at
observed only if pressure is ramped up to Psat
T-dependence of  cavitation event
position of  cavitation in large cavities
possibly voids between SBA grains ?
Cavities ( bulk liquid) provide a reference for cavitation features

## Slide 11
Thermodynamic approach – the energy barrier EB
Grand potential for bubble formation in the metastable liquid [ Sharp interface - Bonnet & Wolf 2019 ]
gain in chemical
potential: known
correction due to
substrate-fluid
interaction potential
cost of the interface
Surface tension a corrected for bubble curvature
Measured for N2 homogeneous cavitation in large pores
Substrate-fluid potential - derivation from dispertion forces ( Saam & Cole, Neimark and co-workers …)
- empirical exponential dependance (Celtini, Pellenq, Morishige…)
1 or 2 adjustable parameters / adjusted on the critical point for confined fluid (point where hysteresis disappears)
Interpore 2026 - Nantes

## Slide 12
Thermodynamic approach – substrate-fluid potential
Substrate-fluid potential - derivation from dispertion forces ( Saam & Cole, Neimark and co-workers …)
[Saam&Cole]
 1 adjustable parameter: pore radius 6.7 nm (NLDFT-type potential: 7.0 nm)
Bubble
filled
empty
Interpore 2026 - Nantes

## Slide 13
Thermodynamic approach – substrate-fluid potential
Substrate-fluid potential - derivation from dispertion forces ( Saam & Cole, Neimark and co-workers …)
- empirical exponential dependance (Celtini, Pellenq, Morishige…)
1 or 2 adjustable parameters / adjusted on the critical point for confined fluid
[Saam&Cole]
 pore radius 6.7 nm (NLDFT potential 7.0 nm)
Bubble
bubble
nucl.
pore filling
Phase diagram (similar with NLDFT potentials)
E*
E*
filled
empty
Interpore 2026 - Nantes

## Slide 14
Thermodynamic approach – substrate-fluid potential
Substrate-fluid potential - derivation from dispertion forces ( Saam & Cole, Neimark and co-workers …)
- empirical exponential dependance (Celtini, Pellenq, Morishige…)
Assuming Rp = 6.7 nm
Interpore 2026 - Nantes

## Slide 15
Thermodynamic approach - results
The NLDFT potential does the best job, but predicted a still smaller than measured for small pores
 underestimates confinement
Interpore 2026 - Nantes

## Slide 16
Thermodynamic approach – nucleation rate
Untill now, no assumption on the nucleation rate
at nucleation threshold :
Measurements + model(s)  ( VP , t , EB ) 
Interpore 2026 - Nantes

## Slide 17
Thermodynamic approach – nucleation rate
Untill now, no assumption on the nucleation rate
at nucleation threshold :
Measurements + model(s)  ( VP , t , EB ) 
CNT [Bl. & Katz 1975]
Hyp.  nucleation site density = liquid number density
 escape rate controlled by viscous dynamics of the
critical bubble.
CNT overestimates 103 x at high T
significant ? (equiv. to DEB  7-8 kT)
if yes - Effect of confinement on bubble dynamics
- Number of nucleation sites ?
=
Interpore 2026 - Nantes

## Slide 18
Conclusion  New capacitive continuous method for measuring isotherms
 Allows to evidence confinement impact on cavitation  Reasonnable agreement with simple thermodynamic approach
 indication that the kinetic prefactor J0 is impacted by confinement What’s next ?  Go for molecular dynamics?
 Effect of the distributions of pore diameter (parameter b)
THANKS FOR YOUR ATTENTION !