## Slide 1
Coupled thermal-hydraulic-mechanical-chemical processes in nanoporous media
Chair Professor, China University of Petroleum (East China), China
Emeritus Distinguished Professor, University of Texas at Arlington, USA
Presentation at
InterPore2026 Minisymposia 13 ID#521
May 21, 2026
(Max) Qinhong Hu, Y.F. Xiao, T. Zhang, J.C. Wen, J.Q. Liang, Q.M. Wang, and S.Y. Yang

## Slide 2: Presentation Outline
1. Rational and significance
2. Multi-approach and multi-scale methodologies
3. Summary and perspectives

## Slide 3
Conventional oil and gas production (1859‒present)
Air and surface water contamination (1950s‒1980s)
Environmentalism movement (since 1960s)
Soil contamination (1960s‒present)
Geothermal energy mining/exploitation (1974‒present)
Tight sand and coalbed methane (1976‒present)
Nuclear energy and geological repository of high-level nuclear waste (1978‒present)
Groundwater remediation and Superfund (1980‒present)
Carbon sequestration or carbon capture and storage (CCS) or carbon capture, utilization and storage (CCUS) (1996‒present)
Petroleum production in shale gas and oil reservoirs (1981; 2000; 2008‒present)
Gas (methane) hydrate extraction (2005‒present)
Critical minerals sustainability (2011‒present)
Underground gas (H2, He, air) storage (2019‒present)
1970
1962
1977
Commonly involves tight (clay) materials & fractured media
Historical Evolution of Major Research Thrusts in the Energy and Resources Geosciences
Hu, 2015-2026

## Slide 4: Scientific and Societal Issues (1979-2012)
1979
1998
2000
Sep. 2012 in Philadelphia
2010

## Slide 5
Nanopores (BEG, Loucks
et al., 2009)
“Shale Revolution” (1981; 2000; 2008-2018）
~15,850 horizontal wells and ~5,250 vertical wells
A net importer of energy since 1953
Crude oil production (MMB/d): 1970-9.6; 2019-12.2; 2023-12.9
2025: 13.6 MMB/d; tight oil 70% (9.0 MMB/d; 450 m tonnes/y)
The United States became a net energy exporter in November 2019
Univ. Texas Arlington
2008.7
George Mitchell (1919–2013; “Father of Fracking”)
Export | Canada(52%) | Mexico (11%) | Saudi (5%) | Iraq (4%) | Brazil (3%)
Import | Mexico (11%) | China (10%) | Dutch (9%) | Canada(8%) | Japan (6%)

## Slide 6
Tailing and rebound
Shale Petroleum Development: Production Decline
Steep initial decline (both gas and oil: -2/3 after 1 yr)
Low recovery (shale gas: <40%; tight oil: <10%)
Theoretical power-law exponent between 0.5 to 1 reported by Monteiro et al. (PNAS, 2012)
Fracture-matrix interaction (fractures: -1; matrix: -1/2 or -1/4)

## Slide 7
Energy Geosciences for Carbon Neutrality (2017-Present)
Coupled THMCB processes
Seven major research areas
Lessons learned from 40+ yrs of subsurface studies
(USDOE, 2000)
Multi-scale investigations
Interdisciplinary
Mechanistic studies
Process-level understanding
Innovative approaches (experimental, theoretical, numerical)
Sandstone
Carbonate
Mudstone
Salt rock
Coal
Sandstone
Carbonate
Mudstone
Salt rock
Coal
Basalt
Granite
Granite
Salt rock
Mudstone
Claystone
OM-rich mudstone
Deep and OM-rich mudstone
CCUS
EGS
Critical Minerals
Green Hydrogen
Nuclear Waste
Shale Petroleum
Energy geology
Gas Hydrate

## Slide 8: Presentation Outline
1. Rational and significance
2. Multi-approach and multi-scale methodologies
3. Summary and perspectives

## Slide 9
Rock milling in 1998
Field observation (preferential flow in a fracture network) of dye distribution in unsaturated fractured tuff at Yucca Mountain
tm = 4µαφdm2 /k
My Postdoctoral Research on Rock (1997‒2000): Fracture-Matrix Interaction
My work on fracture-matrix interaction starts with this rock
Hu et al., JCH, 2001; VZJ, 2002
2019
Tailing

## Slide 10
Pore Structure: Geometry and Topology
“Surface Zone”
~400 µm (atmospheric temp-pressure)
mm？(reservoir temperature-pressure)
Dead ends
Backbone
Through
Edge-accessible
“Isolated”
Connected
Total pore space
Accessible porosity/Total porosity (fa / ft )
“Surface Zone”: ~70%
For deep & organic matter-rich shale
Sample surface
“Bulk Zone”: ~0.1%
Total (absolute)ft
Accessible (open; saturation) fa
Effective (dynamic; percolating) fe
ft
fi
Hu, 2010-2025
“Bulk Zone”
“Isolated” ratio

## Slide 11
Fracability
Permeability
Diffusivity
Accessibility
Nano-Petrophysics and Fracture-Matrix Interaction
Wettability
Movability
nm
µm
10× µm
Capillarity
Tortuosity
2.54 cm
km
~1 m
mm
Pilot hole with logging and core samples
10× m
Multi-Approach and Multi-Scale Methodologies
Microscopic pore structure characteristics control macroscopic fluid flow and petroleum movement
30 cm
10 cm

## Slide 12
Chemicalmovement
Fluid flow
Pore structure
μm CT
Vacuum saturation & high- pressure intrusion (different sample sizes)
Gas & liquid pycnometry (sizes)
Bulk density (sizes)
MIP (sizes)
Gas physisorption
NMR & NMRc
(U)SANS & SAXS
FE-SEM & FIB-SEM
nm CT
Impregnation and mapping of Wood’s metal, 14C-PMMA, and sodium tetrachloroaurate (sizes)
GRI matrix k (sizes)
Wettability-fluids imbibition
Batch sorption (sizes)
Column transport (sizes)
Imbibition (HPHT)
Diffusion (HPHT; sizes)
Core flooding (HPHT)
dm-block tri-axial fracturing & post-mortem THMC processes (HPHT)
Basic data
TOC
Mineralogy
XRF mapping
Cation exchange capacity
Anion exchange capacity
Surface area
Thin section
Grain size distribution
Liquid-air & liquid-liquid contact angle (HPHT)
Wettability-fluids & -tracers recipe
Liquid imbibition (sizes)
Gas (O2, H2, CH4, and CO2) diffusion (HP)
Gas sorption-advection (HPHT)
NMR (HPHT)
Hu, 2010-2026
HPHT: high pressure-high temperature
Multi-Approach and Multi-Scale Nano-Petrophysical Studies
Research philosophy
Upgrading commercial instrument: 30%
Custom-designing and improvement: 30%
Sharing among international collaborators: 30%
Utilizing large-scale international facilities: 10%

## Slide 13
API brine (8 wt.% NaCl+2 wt.% CaCl2) [water-wet]
  ReO4- (0.553 nm), anionic Sb2--complex (0.89 nm)
Cs+ (0.234), Cationic Ru2+-complex (1.0 nm)
2DT [n-decane (D): toluene (T)] [oil-wet]
Organic-I (1-iododecane)
Organic-Re [trichlorooxobis(triphenylphosphine)rhenium(V)]
Wettability-Based Fluids and Tracers
1.393 nm × 0.287 nm × 0.178 nm
1.273 nm × 0.919 nm × 0.785 nm
0.23 nm
0.85 nm
Hu et al., 2004; 2010; 2017; 2019; 2024
Re
Diffusion
A
B
Notes: 图例

## Slide 14
Re background: 1.29±1.24 mg/kg
5–71 μm
1–5 μm
0–1 μm
Barnett 7109’
Fluid: API brine
Imbibition time: 94 hrs
Edge-Accessible Effective Porosity & Steric Entanglement
background levels
I (mg/kg; sampling point)
bkdg: 0.50±0.52 (9); side: 15.3±4.03 (49)
interior: 7.10±3.01 (180) for 44.6±17.0%
Re (mg/kg; sampling point)
bkdg: 1.55±1.46 (9); side: 675±398 (49)
interior: 3.77±5.45 (180) for 0.33±0.58%
Niobrara: 17-1A H
Fluid: n-decane
Vacuum saturation + high pressure intrusion
Pore-throat size distribution

## Slide 15
CNPC International Cooperative Project (2024-2026): “Fundamental studies on fluid-solid coupling and mechanic failure of weak shale laminae based on small angle scattering experiments”
Jiacheng Wen
Jingqi Liang
Nano-indentation
dm sample fracturing
Tao Zhang
Guoqing Bao
Lamina characteristics
Wen Liu
Pore structure
Lamina mechanics
Research Institute of Production and Exploration Development (RIPED) PetroChina, Beijing
Ongoing Project

## Slide 16
Results of nano-indentation and SAXS
An integrated design of “lamina identification – multi-mechanical parameter testing – macroscopic comparison”: a foundation for establishing the relationship between lamina mechanics and pore structure response
Correlation of Pore Structure with Micromechanics
Lucaogou Formation, Tuha Area, Well Ma L101H, 6-21/57
Saxs Sample
No. | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8
E | 42.47 | 39.62 | 41.81 | 46.30 | 46.91 | 41.65 | 45.64 | 49.93
H | 2.25 | 2.08 | 2.08 | 2.30 | 2.45 | 1.85 | 2.27 | 2.46
Kc | 1.95 | 1.81 | 1.86 | 1.90 | 1.85 | 1.85 | 1.86 | 1.98
No. | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16
E | 51.24 | 40.63 | 53.04 | 49.67 | 51.77 | 44.60 | 51.55 | 52.34
H | 2.41 | 2.04 | 2.93 | 2.89 | 3.02 | 2.54 | 2.97 | 3.10
Kc | 1.99 | 1.86 | 2.08 | 2.04 | 2.05 | 1.93 | 2.07 | 2.08
E: Young’s Modulus (GPa）H: Hardness (GPa） Kc: Fracture Toughness (MPa·m1/2)
1
2
3
4
5
7
9
6
8
10
13
15
12
11
14
16
Integrated experimental scheme of SAXS and nano-indentation
Notes: 左图展示了在中国东莞中子散裂源进行小角X射线散射的大科学实验装置，右图是具体的实验方案，红色圈是小角X射线的测试区域，黄色方框是纳米压痕测试区域，保证他们的中心位置是重叠的。

## Slide 17
Mineral- and Lamina-Scale Based Prediction of Young’s Modulus
Based on micromechanical parameters, a multiscale upscaling framework for modulus prediction is established using the fractal dimension/Self-Consistent Homogenization Method, linking mineral composition, lamina structure, and elastic modulus; meanwhile, validation is achieved through macroscopic uniaxial mechanical experiments.
Predicted Macroscopic Young’s Modulus
Downhole Core Sample
Nanoindentation
Uniaxial Compression
300 mN
5 mN
Mineral Scale
Lamina Scale
Design of multiscale upscaling scheme for laminated shale
Schematic diagram of the Self-Consistent Homogenization Method
SC Equivalent Homogeneous Medium
Iteration
Self-Consistent Condition
Phase 1
Phase 2
Phase 3
(Hill, 1965)
53%
6.6%
6.3%
91%
Notes: 这一页展示的是基于矿物尺度和纹层尺度的微观模量尺度升级的实验方案：以纳米压痕获得的微观力学参数为输入，分别从矿物尺度和纹层尺度出发预测宏观杨氏模量，并通过宏观单轴压缩实验进行对比验证。

## Slide 18
Influence of Bedding Angle on Shale Failure Modes
Experimental methods: uniaxial compression, acoustic emission (AE), digital image correlation (DIC), and SEM
CT+SEM: morphology of internal crack propagation and microscopic characterization of fracture surfaces
AE: The changes in AE signals during the crack propagation of the sample
DIC: surface damage morphology during the destruction process
AE+DIC: analysis of fracture distribution from temporal and spatial perspectives
Stage Ⅰ
Stage Ⅱ
Stage Ⅲ
Stage Ⅳ

## Slide 19
different experimental conditions (bedding, in-situ stress, fracturing fluid viscosity)
Migration behavior of fracturing fluid within shale matrix
µm-CT
Laser ablation-ICP-MS tracer mapping
Fracture growth under different bedding densities
Hydraulic fracturing equipment
Propagation of hydraulic fracturing
single fracture morphology
Spatial tracer distribution
Multi-Scale Characterization of Hydraulic Fracture Evolution and Fluid Migration in Shale
10-cm black fracturing + µm-CT + LA-ICP-MS
Fracture propagation
Fluid migration

## Slide 20
Development of in situ high-pressure neutron scattering system that independently controls overburden stress and fluid pressure while resolving 1 nm-1.5 μm pore structure during deformation
At 33.9 MPa over-burden stress, sample deformation 13.7% by LVDT vs. neutron-measured pore volume change 2.1% (apparent porosity increase from 8.38% to 9.50%)
Apparent-porosity increase predominately (86%) from 60-800 nm pore-diameter interval
Decoupling of Shale Bulk Volume and Pore Volume Using in situ VSANS

## Slide 21: Presentation Outline
1. Rational and significance
2. Multi-approach and multi-scale methodologies
3. Summary and perspectives

## Slide 22
http://www.hydraulicfracturing.com/Process/Pages/information.aspx
Soils
Aquifers
Geological repositories
Shale petroleum development
CCUS
UHS
Soil contamination
Geothermal energy mining/exploitation
Nuclear energy and geological repository of high-level nuclear waste
Groundwater remediation and Superfund
Carbon capture, utilization and storage
Petroleum production in shale gas and oil reservoirs
Underground gas (H2, He, air) storage
“Deeper” Studies for Deep Understanding

## Slide 23
130 °C
90 MPa
5000 m
7000 m
1000 m
3000 m
30 °C
18 MPa
80 °C
58 MPa
East
West
Deep-UltraDeep
PSD%
Chart: 
1-10 nm | 0.656
0.01-0.1 µm | 10.471
0.1-1 µm | 33.254
1-10 µm | 41.272
10-100 µm | 11.7961
100-1000 µm | 2.5505
Mega
242 °C
170 MPa
175 °C
130 MPa
11000 m
10 nm
1 μm
1 m
1 km
1 Å
Atomic
Micro
Meso
Macro
Lab-scale（1 nm-30 cm）
DFT
MD
LBM
FEM/FEM (MODFLOW; Hydrus; PHREEQC ; TOUGH; Eclipse)
Nano-petrophysical parameters:
ᵠe , r, k, kr , Pc , As , De , τ , R…
Temporal heterogeneity
Advection
Diffusion
Sorption
Reaction
Degradation
Spatial heterogeneity
Deep Subsurface Geoscience and Engineering

## Slide 24
Summary and Perspectives
huqinhong@upc.edu.cn
  Multi-approach and multi-scale methodologies are developed for pore structure, fluid flow and chemical transport studies in the context of low-permeability media and fracture-matrix interaction
  Pore structure characteristics, especially low pore connectivity and associated “dual effective porosity zones”, is observed for low-permeability shale
  It is urgent to study the nano-petrophysics and coupled THMCB processes under reservoir in-situ temperature-pressure conditions
  Mechanistic understanding, custom-designed apparatus, and the application of large-scale scientific facilities are essential for exploration or storage of various energy-related fluids for carbon neutrality