## Slide 1: Exploring Helium Metastability Using Artificial Porous Systems
ANR CAVCONF & NANOCAV
Interpore 2026 21/05/2026
Institut Néel, Université Grenoble Alpes:
Paul COUTIN, Laurent Cagnon, Benoit Chabaud, Thierry Crozes, Jean-Francois Motte, Marine Schott, Panayotis Spathis, Pierre-Etienne Wolf
LPENS, Ecole Normale Supérieure, Paris
Etienne Rolley, Kristina Davitt

## Slide 2: Cavitation in liquidHe
Liquid under tension
Open Questions on Bubble Nucleation
  Role of surface tension in the energy barrier
  Dynamical effects during bubble propagation
  Finite-size effects
Superfluid Phase
  Possible role of vortices as cavitation nucleation centers
Cavitation
Boiling
Notes: 1er = cout énergétique de l’interface liquide-gaz : surfacique
2ème = stabilisation volumique
ACTIVATION THERMIQUE
L’équipe a montré que, pour des fluides classique, la théorie décrit efficacement la cavitation dans les milieux poreux

## Slide 3: How to reach a metastable state ?
Cavitation is a stochastic process; therefore, experiments must be repeated multiple times to obtain reliable data
Ultrasonic methods
  Require sequential repetition of experiments
Ink-bottle pore geometry
  independent pores
  Allowing massive parallelization of measurements
Caupin & Balibar, ENS Paris:
Dynamic Sensing
Doebele PRL 2020 & Bossert PNAS 2022:
Ink-Bottle Pores

## Slide 4: Porous Alumina Samples
200 nm
Sample: 1 inch aluminium wafer
Top view
Side view
200 nm
Before ALD
after 160cycles of ALD
ALD deposition is required to obtain the ink-bottle shape
ALD deposition
ALD
Notes: Membrane détaché
EMPREINTE dans l’alu
ALD FLASH

## Slide 5: Porous Alumina Samples
Before ALD
after 160cycles of ALD
ALD deposition is required to obtain the ink-bottle shape
ALD deposition
ALD
Sample: 1 inch aluminium wafer
Top view
Side view
200 nm
Notes: Membrane détaché
EMPREINTE dans l’alu
ALD FLASH

## Slide 6: Setup for Isotherm Measurements
Sample
Gaz injection (300K)
Pump
P
P
Cryostat
Cell
needle valve
Capacitive bridge
Continuous Injection

## Slide 7: Native Porous Membranes
Independent Pores
Corrugated conical pores

## Slide 8: Same Porous Membrane After ALD Deposition
Same condensation branch,
evaporation shifts to lower pressure:
Ink bottle geometry
1 ALD cycle =>

## Slide 9: Reaching cavitation
Sorption isotherms at different temperatures ()
Evaporation proceeds through cavitation

## Slide 10: Reaching cavitation
Sorption isotherms at different temperatures ()
Evaporation proceeds through cavitation
Extraction of the cavitation threshold

## Slide 11: Reaching cavitation
Sorption isotherms at different temperatures ()
Evaporation proceeds through cavitation
Extraction of the cavitation threshold
The same isotherm is measured at different pressure sweep rates ()

## Slide 12: Cavitation Analysis Through Controlled Pressure Rates
ASSUMING the capacitance is proportional to the mass of adsorbed fluid:
Normalize the data to obtain the fraction of filled pores as a function of P
Subtract the condensation branch
Convert the gaseous pressure to liquid pressure with
Rate
The same isotherm is measured at different pressure sweep rates ()

## Slide 13: Cavitation Analysis Through Controlled Pressure Rates
Empty pores
Filled pores
Rate
The same isotherm is measured at different pressure sweep rates ()
ASSUMING the capacitance is proportional to the mass of adsorbed fluid:
Normalize the data to obtain the fraction of filled pores as a function of P
Subtract the condensation branch
Convert the gaseous pressure to liquid pressure with

## Slide 14: Cavitation Analysis Through Controlled Pressure Rates
Empty pores
Filled pores
Rate
The same isotherm is measured at different pressure sweep rates ()
By varying the pressure sweep , we determine for each isotherm the experimental barrier energy :
where:
: prefactor assumed constant over the full sweep-rate range
: fixed by the geometry of the porous sample
: controlled through the pressure sweep rate during cavitation

## Slide 15: Cavitation Analysis Through Controlled Pressure Rates
Empty pores
Filled pores
Half filled
Rate
The same isotherm is measured at different pressure sweep rates ()
By varying the pressure sweep , we determine for each isotherm the experimental barrier energy :
where:
: prefactor assumed constant over the full sweep-rate range
: fixed by the geometry of the porous sample
: controlled through the pressure sweep rate during cavitation

## Slide 16: Cavitation Analysis Through Controlled Pressure Rates
Empty pores
Filled pores
Half filled
Rate
The same isotherm is measured at different pressure sweep rates ()
By varying the pressure sweep , we determine for each isotherm the experimental barrier energy :
where:
: prefactor assumed constant over the full sweep-rate range
: fixed by the geometry of the porous sample
: controlled through the pressure sweep rate during cavitation

## Slide 17: Cavitation Analysis Through Controlled Pressure Rates
Empty pores
Filled pores
Half filled
Rate
The same isotherm is measured at different pressure sweep rates ()
By varying the pressure sweep , we determine for each isotherm the experimental barrier energy :
where:
: prefactor assumed constant over the full sweep-rate range
: fixed by the geometry of the porous sample
: controlled through the pressure sweep rate during cavitation
For all rates, the pore distribution is fitted by:
With

## Slide 18: Estimating the experimental Barrier Energy and Local Slope

## Slide 19: Estimating the experimental Barrier Energy and Local Slope

## Slide 20: Comparison with theory
below
CNT (+ bulk) not valid below 4K

## Slide 21: Comparison with theory
CNT (+ bulk) not valid below 4K
We have a better fit with the DFT
Same
different

## Slide 22: Conclusions and Perspectives
Conclusions
  CNT with bulk surface tension does not describe the low-temperature regime
  Experimental measurements agree with DFT predictions
  No observable signature of vortex-assisted nucleation
Perspectives
  Study of cavitation closer to the critical point
  Enhanced investigation of confinement effects
  New porous system under investigation

## Slide 24: Reaching Cavitation: Using Ink-Bottle Shaped Pores
R1
R2
R1
R2

## Slide 25: Reaching Cavitation: Using Ink-Bottle Shaped Pores
R1
R2
R1
R2

## Slide 26: Reaching Cavitation: Using Ink-Bottle Shaped Pores
Minimum Radius to Observe Cavitation :
We use an ALD deposition to close the constrictions and obtain this radius value