## Slide 1
Experimental observation of the dependence of a
liquid adsorbate’s elastic modulus on the pore size
K. Schappert and R. Pelster
Saarland University, Department of Physics, Germany
MS13 - Fluids in Nanoporous Media
Abstract ID : 366

## Slide 2
Increase of the adsorbate’s bulk modulus at small pore radii
C.D. Dobrzanski, B. Gurevich, G. Gor, Appl. Phys. Rev. 2017, 4, 011303
Here: Experimental test
nanoporous glass monoliths with interconnected pores
Particle Solutions, LLC (Florida, USA)
origin: solvation pressure of the confined liquid (G. Gor, Langmuir 2014,30, 13564-13569)
liquid adsorbate: argon at 86 K
ultrasonic measurements
(effective longitudinal modulus⟶ )
theoretical prediction (MC simulations/DFT calculations)
Motivation:
for

## Slide 3
→ Pore Size Distributions
 | porosity | mean pore radius
sample A | 0.611 | 12.8 nm
sample B | 0.349 | 4.4 nm
sample C | 0.411 | 1.8 nm
sample A | 0.611 | 12.8 nm
sample B | 0.349 | 4.4 nm
sample C | 0.411 | 1.8 nm
Nanoporous glass monoliths
with interconnected pores
Particle Solutions, LLC (Florida, USA)
Sorption Isotherms (argon, )

## Slide 4
Measured effective longitudinal modulus - empty samples
Ultrasonic measurement
(transit time of pulses)

## Slide 5
Effective longitudinal modulus: empty pores (measured)
and filled pores (expected behavior for constant )
filled pores:
(expected)
Taylor expansion
some effective media formula predict such a relation
(e.g., Voigt & Gassmann)
(*)
high contrast limit
⟶ behavior similar to micro- structure with empty pores

## Slide 6
Effective longitudinal modulus:
empty & filled pores (both measured)
(*)
but

## Slide 7
Measured change of the effective modulus upon filling with liquid argon
The smaller the pores,
the higher the modulus
of the adsorbate
(*) ⟶
⟹
next step: normalization

## Slide 8
Normalized longitudinal modulus of the adsorbate (liquid argon) vs.
enhancement
by a factor of
the order of 2
constant slope

## Slide 9
Liquid: bulk modulus longitudinal modulus
⟹ experimental confirmation of a theoretical prediction
C.D. Dobrzanski, B. Gurevich, G. Gor, Appl. Phys. Rev. 2017, 4, 011303
Summary
The smaller the pore size, the higher the modulus of the adsorbed liquid:
Strong increase despite weak
interaction with pore surface
Klaus Schappert and Rolf Pelster
Experimental Evidence for the Pore Size Dependence of Elastic Properties in a Liquid Adsorbate Confined to Nanopores
The Journal of Physical Chemistry Letters 2026 17 (6), 1640-1646
DOI: 10.1021/acs.jpclett.5c03903
for