## Slide 1: Sébastien SAUNIER, Paul BARAL, Renaud FERRIER
22 MAY 2026
Jnanesh GOPALE GOWDA
Microstructure/permeability relation of porous ceramics through active learning-assisted experimental campaign

## Slide 2: Introduction
Process
Properties
Microstructure
Research work approach
Microstructure/permeability relation of porous ceramics through active learning-assisted experimental campaign
Regression
Active Learning
Conclusion
Permeability test
Porous sample
Introduction
Powder Metallurgy
Porous ceramics samples of varying porosity and pore morphology
Pore Morphology
Mechanical Integrity & Permeability
Study the infusion process in the porous media.
Current models struggle to predict fluid behavior in saturated & unsaturated porous media accurately.
H. Teixidó et al .vol. 9, p. 809226, Feb. 2022.
Notes: Ceramics because of ease of study and repeatable testing.

## Slide 3: Introduction
Process
Properties
Microstructure
Research work approach
Microstructure/permeability relation of porous ceramics through active learning-assisted experimental campaign
Regression
Active Learning
Conclusion
Permeability test
Porous sample
Introduction
Powder Metallurgy
Porous ceramics samples of varying porosity and pore morphology
Pore Morphology
Study the infusion process in the porous ceramics.
Current models struggle to predict fluid behavior in saturated & unsaturated porous media accurately.
Mechanical Integrity & Permeability
Notes: Ceramics because of ease of study and repeatable testing.

## Slide 4: Summary
Porous sample manufacturing
Permeability test
Active learning–assisted porous ceramic manufacturing
Regression on permeability measurements.
Conclusion

## Slide 5: Porous sample manufacturing
Atomized alumina BA15W (Al₂O₃)
from Baikowski Chimie
Polymethyl methacrylate (PMMA)
Powder Metallurgy Process
Introduction
Regression
Active Learning
Conclusion
Permeability test
Porous sample
J.G. Gowda et al. Active learning-assisted experimental design for porous ceramic manufacturing (2026).
Sample preparation process. a- Granulometry/ Sphere diameter distribution of alumina powder and PMMA spheres used in this study, b- De-binding and c- Sintering temperature cycles.
Porous alumina samples

## Slide 6: Permeability testing
Flow velocity calculation
Testing flow pressure and mass flow from the flowmeter
Permeability K of the 60 vol.% PMMA sample
Introduction
Regression
Active Learning
Conclusion
Porous sample
Permeability test
Darcy equation -
J.G. Gowda et al. Active learning-assisted experimental design for porous ceramic manufacturing (2026).

## Slide 7: Active learning classification model
Manufacturing Parameters
Varying Parameters
PMMA of 2 different grain size ratio
Volumetric ratio of Alumina and PMMA mixture
Constant Parameters
Uniaxial and Isostatic compaction load.
Debinding and Sintering temperature.
Introduction
Regression
Conclusion
Permeability test
Porous sample
Active Learning
J.G. Gowda et al. Active learning-assisted experimental design for porous ceramic manufacturing (2026).
Porogen 1 vol.%
(PMMA of 25-100µm)
0
100
100
Non-fractured & Permeable
Porogen 2 vol.%
(PMMA of 100-200µm)
Fractured
Non- permeable
Porogen 1 vol.%
(PMMA of 25-100µm)
Porogen 2 vol.%
(PMMA of 100-200µm)
60% - 100-200
30% - 100-200
30% - 25-100
60% - 25-100
30% - 25-100 & 30%- 100-200
Notes: Part of research Project with a student (Liam Latour)

## Slide 8: Active learning classification model
Manufacturing Parameters
Varying Parameters
PMMA of 2 different grain size ratio
Volumetric ratio of Alumina and PMMA mixture
Constant Parameters
Uniaxial and Isostatic compaction load.
Debinding and Sintering temperature.
Introduction
Regression
Conclusion
Permeability test
Porous sample
Active Learning
J.G. Gowda et al. Active learning-assisted experimental design for porous ceramic manufacturing (2026).
Fractured
Non- permeable
Non-fractured & Permeable
Porogen 1 vol.%
(PMMA of 25-100µm)
Porogen 2 vol.%
(PMMA of 100-200µm)
Porogen 2 vol.%
(PMMA of 100-200µm)
Porogen 2 vol.%
(PMMA of 100-200µm)
Porogen 1 vol.%
(PMMA of 25-100µm)
Porogen 2 vol.%
(PMMA of 100-200µm)
60% - 100-200
30% - 100-200
30% - 25-100
60% - 25-100
30% - 25-100 & 30%- 100-200
Notes: Part of research Project with a student (Liam Latour)

## Slide 9: Active learning classification model
Manufacturing Parameters
Varying Parameters
PMMA of 2 different grain size ratio
Volumetric ratio of Alumina and PMMA mixture
Constant Parameters
Uniaxial and Isostatic compaction load.
Debinding and Sintering temperature.
Introduction
Regression
Conclusion
Permeability test
Porous sample
Active Learning
J.G. Gowda et al. Active learning-assisted experimental design for porous ceramic manufacturing (2026).
Porogen 1 vol.%
(PMMA of 25-100µm)
Porogen 2 vol.%
(PMMA of 100-200µm)
Fractured
Non- permeable
Non-fractured & Permeable
Porogen 1 vol.%
(PMMA of 25-100µm)
Porogen 2 vol.%
(PMMA of 100-200µm)
60% - 100-200
30% - 100-200
30% - 25-100
60% - 25-100
30% - 25-100 & 30%- 100-200
Notes: Part of research Project with a student (Liam Latour)

## Slide 10: Active learning classification model
Introduction
Regression
Conclusion
Permeability test
Porous sample
Active Learning
Gaussian Processes (GP) are a nonparametric supervised learning method used to solve regression and probabilistic classification problems
Gaussian Process
Carl E. Rasmussen and Christopher K.I. Williams, MIT Press 2006
Gaussian process classifier
Gaussian process regressor
Notes: Part of research Project with a student (Liam Latour)

## Slide 11: Active learning classification model
Initial samples manufactured for model data collection
Initial Classification of the Database
Fractured
Permeable Boundary
Fracture
Boundary
Introduction
Regression
Conclusion
Permeability test
Porous sample
Active Learning
Porous ceramic samples
& + Non-fractured or permeable
& + Fractured or non-permeable
J.G. Gowda et al. Active learning-assisted experimental design for porous ceramic manufacturing (2026).
16 different samples.
2 fractured or non-permeable samples were identified for each.
Fracture limit – external cracks
Permeability limit - greater than m²
0 Not
acceptable
- 1.0 Acceptable
Notes: Proof of concept for 3D , 90% uncertainty

## Slide 12: Active learning classification model
Introduction
Regression
Conclusion
Permeability test
Porous sample
Active Learning
J.G. Gowda et al. Active learning-assisted experimental design for porous ceramic manufacturing (2026).
Iteration 0
& + Non-fractured or permeable
& + Fractured or non-permeable
Not acceptable
Acceptable

## Slide 13: Active learning classification model
Introduction
Regression
Conclusion
Permeability test
Porous sample
Active Learning
J.G. Gowda et al. Active learning-assisted experimental design for porous ceramic manufacturing (2026).
& + Non-fractured or permeable
& + Fractured or non-permeable
Not acceptable
Acceptable
Iteration 1

## Slide 14: Active learning classification model
Introduction
Regression
Conclusion
Permeability test
Porous sample
Active Learning
J.G. Gowda et al. Active learning-assisted experimental design for porous ceramic manufacturing (2026).
Iteration 2
& + Non-fractured or permeable
& + Fractured or non-permeable
Not acceptable
Acceptable

## Slide 15: Active learning classification model
Classification limit
Classification validation
0 Not
acceptable
- 1.0 Acceptable
Introduction
Regression
Conclusion
Permeability test
Porous sample
Active Learning
valid parametric space
J.G. Gowda et al. Active learning-assisted experimental design for porous ceramic manufacturing (2026).

## Slide 16: Gaussian process regression on permeability
Comparison between data point and the model for selected diagonal
Regression model permeability map on valid parametric space
Introduction
Active Learning
Conclusion
Permeability test
Porous sample
Regression
J.G. Gowda et al. Active learning-assisted experimental design for porous ceramic manufacturing (2026).

## Slide 17: Gaussian process regression on permeability
Experimental and GPR predicted permeability comparison
Validation of regression model
Introduction
Active Learning
Conclusion
Permeability test
Porous sample
Regression
J.G. Gowda et al. Active learning-assisted experimental design for porous ceramic manufacturing (2026).
Notes: Gaussian extrapolation

## Slide 18: Gaussian Process Regression on permeability measurements
Conclusion
  Experimental
Permeability test bench provides reliable with an accuracy of ± 4%.
GPR model successfully captures the non-monotonous influence of porogen parameters.
  Active learning and Regression
Developed proof of concept Batch AL with GPC can be generalized to similar other manufacturing processes.
GPR predicts permeability based on porogen parameters.
Developed codes are made available with the article.
Introduction
Active Learning
Permeability test
Porous sample
Regression
Conclusion
Notes: Gaussian extrapolation

## Slide 19: Perspective
Process
Properties
Microstructure
Research work approach
Powder Metallurgy
Porous ceramics samples of varying porosity and pore morphology
Mechanical Integrity & Permeability
Pore Morphology
Pore size distribution of the sample
Morphological parameters
Porosity
Pore size distribution
Crack size and length
Tortuosity
Rezaee et al, Relationships between permeability, porosity, and pore throat size in carbonate rocks using regression analysis and neural networks. 3(4), 370-376 (2006).
Porogen 1 vol.%
(PMMA of 25-100µm)
Porogen 2 vol.%
(PMMA of 100-200µm)
60% - 100-200
30% - 100-200
30% - 25-100
60% - 25-100
30% - 25-100 & 30%- 100-200
Notes: To add size

## Slide 20: Thank you for your attention
Jnanesh GOPALE GOWDA
jnanesh.gopalegowda@emse.fr

## Slide 21: Active learning classification model
Fracture Boundary
Permeable Boundary
Iteration 0
Iteration 2
Flowchart of Active learning algorithm for fracture and permeability
Introduction
Regression
Permeability test
Porous sample
Active Learning
AL points (white stars)
& + Non fractured
& + Fractured
AL points (white stars)
& + Non fractured
& + Fractured
Fractured
Non
Fractured
Non Permeable
Permeable
Conclusion
Iteration 0
Iteration 2
AL points (white stars)
& + Non fractured
& + Fractured
AL points (white stars)
& + Non fractured
& + Fractured
Notes: Batch manufacturing

## Slide 22: Active learning classification model
valid parametric space
Classification limit
Classification validation
0 Not
acceptable
- 1.0 Acceptable
Introduction
Regression
Conclusion
Permeability test
Porous sample
Active Learning

## Slide 23: Gaussian Process Regression on permeability measurements
Introduction
Active Learning
Conclusion
Permeability test
Porous sample
Regression
100-200
25-100
100-200
25-100
Comparison between data point and the model for selected diagonal
100-200
30 vol.%
60 vol.%