## Slide 1
Yue SHI1,2, Chi YAO1 , Wanqing SHEN2 , Chuangbing ZHOU1 , Jianfu SHAO2
May 21, 2026
Beyond phenomenology: a micromechanics-based model for rock-like materials within the framework of irreversible thermodynamics and multistep homogenization
1. Engineering Research Center of Water Basin Carbon Neutrality, Nanchang University, China
2. Laboratoire de Mécanique, Multiphysique, Multiéchelle, Université de Lille, France
(MS16) Complex fluid and Fluid-Solid-Thermal coupled process in porous media: Modeling and Experiment
18th ANNUAL MEETING

## Slide 2
Engineering and scientific background
Mechanical behavior of rock-like materials
Brittle-ductile transition - Liu. 2017
Brittle-ductile transition
Hydromechanical coupling - Huang. 2022
Long-term strength decrease
Deformation increase
Jinping I Hydropower Station - Marble
Andra Laboratory - COx claystone
Anisotropy - Zhang. 2019
How to model rock-like materials ?
Explicit Physics.
Simple Form.
High Efficiency.
Notes: three bench seven step excavation method

## Slide 3
Micro-macro model
Based on the homogenization approach (Dilute, Mori-Tanaka and Ponte-Castaneda-Willis)
Considering microstructural information, such as microcrack, pore and mineral inclusion
Considering the damage from microcrack frictional sliding and mineral-matrix debonding [Zhu et al. 2015, Farhat et al. 2020]
Existed model for rock-like materials
Phenomenological model
Most models depends on the definition of macroscopic free energy, yield surface, plastic potential, etc
Extend to anisotropy [Chen et al. 2010], time-dependent behavior [Pietruszczak et al. 2004] and THM coupling [Aldakheel. 2017]...
Limited applicability to other materials or beyond data used for calibration
Numerical model
DEM, FFT, PFM, PD, EFEM are visualized technologies and usually require expensive calculation consumption.
Engineering and scientific background
Notes: enriched finite element method
Fast Fourier Transform
discrete element method
Thermo-hydro-mechanical

## Slide 4
Micromechanics-based model
Representative elementary volume
Abutment slope
Unit：m
Microscale
Mesoscale
Macroscale
Nanoscale
Matrix
Microcrack
Equivalent homogeneous material
Homogenization
10-3
10-6
10-9
Pore
Mineral
1st
Homogenization
2nd
Tunnel face
Factors are considered for stress and damage state
Circumstance
Microstructure
Load-unload condition

## Slide 5
Homogenization scheme
What local behaviors should be modeled ?
Plastic deformation of matrix
Microcrack propagation
Frictional sliding along microcracks
Debonding along mineral-matrix interfaces
…
Micromechanics-based model

## Slide 6
Ellipsoidal inclusion
Penny-shaped microcracks =,
Damage density
Volume fraction
Effective elastic stiffness
Spherical pores
Volume fraction
Effective elastic stiffness
Homogeneous stiffness =
Model formulation - Microstructure
Micromechanics-based model
a
d
φp

## Slide 7
Irreversible Thermodynamics
Global stress-strain relation
Local stress-strain relation
Damage driven force
Criterion for local behaviors
Microcracks propagation
Porous matrix deformation
Frictional sliding along microcrack surface
Debonding along mineral-matrix interfaces
Model formulation – Global and Local behaviors
Micromechanics-based model

## Slide 8
Wide range of confining pressure
Granite

## Slide 9
In multiple directions
Sandstone

## Slide 10
Time-dependent behaviors
Sandstone and Granite

## Slide 11
Hydro-mechanical coupling
Sandstone
50 MPa
30 MPa
10 MPa

## Slide 12
Conclusions
Prospects
Matrix plasticity and microcrack inelasticity are physically coupled in thermodynamics framework
Time effect on matrix and microcrack phase is separately considered
The proposed model is well implemented into a standard finite element software
More detailed microstructure information to be considered
Mineral inclusion, distribution, direction(anisotropy), etc.
Complicated thermo-hydro-mechanical coupling condition to be considered
Application in practical engineering

## Slide 13
Thank you for your attentions!
Yue SHI
Nanchang University, China
Email: yue.shi@ncu.edu.cn
Questions & Answers
Wechat
Whova

## Slide 14
duse@cumt.edu.cn
https://onlinelibrary.wiley.com/journal/27701328
Scope
Exploration and extraction of geo-resources
Energy extraction and storage
Underground infrastructures
Geo-environments and waste geological disposal
Research and testing space in deep underground
Plan，design and construction technology for under space and engineering and more!
Editor-in-Chief：Prof. Heping Xie，China
Executive Editor-in-Chief：Prof. Chunfai Leung, Singapore
Editorial Board
Quality assured with a robust peer review process
Deep Underground Science and Engineering
JCR Q1 OPEN ACCESS NO ARTICLE PUBLICATION CHARGES
@DUSE_Office
The journal has been indexed in Scopus, Web of Science (ESCI/EI), DOAJ, and Ei；
CiteScore 2024 of 5.0 and CiteScoreTracker 2025 of 7.2；
It holds a Q1 ranking in the Journal Citation Reports (IF=5.0)；
The articles have been downloaded by scholars from 189 countries or regions, with a total download count exceeding 220000 times.
Progress （Sept. 2022-Nov. 2025)
Submission URL
https://wiley.atyponrex.com/journal/DUG2