## Slide 1: Fluid–solid–thermal coupling in fibrous porous media: distinct roles of porosity, fiber orientation and relative humidity in cellulose fiber stacks
Karen MOURDA
Supervisor: Philippe COUSSOT
19 May 2026
Interpore 2026

## Slide 2: The New Frontier in Sustainable Building: Bio-based Construction Materials
2
Introduction: Bio-based materials, derived from renewable sources, offer sustainability, renewability, and a significant reduction in environmental impacts compared to traditional construction materials.
Trends: Growing trends in the construction industry towards green building and the increasing adoption of sustainable practices.

## Slide 3: From Microstructure to Insulation: Probing the Thermal Behavior of Bio-Based Materials
Physical Origin ?
These materials have Low thermal conductivity
Temperature
Porosity
Structure
Moisture Content
depending on:
🎯
3

## Slide 4
4
Literature data: strong dispersion despite similar materials
For similar density ranges, reported conductivities span a wide interval.
[1] F. Ye, H. Wei, Y. Xiao, U. Berardi, G. Quaranta, C. Demartino, Bio-based insulation materials in sustainable constructions: A review of environmental, thermal and acoustic insulation, durability, and mechanical performances, Renew. Sustain. Energy Rev. 223 (2025) 115872. https://doi.org/10.1016/j.rser.2025.115872
[2] A. Bakkour, S.-E. Ouldboukhitine, P. Biwole, S. Amziane, A review of multi-scale hygrothermal characteristics of plant-based building materials, Constr. Build. Mater. 412 (2024) 134850. https://doi.org/10.1016/j.conbuildmat.2023.134850.
[1]
[2]

## Slide 5: Overview of the Study
5
Part 1_ Measurement Challenges
Part 2_ Porosity & Structure
Part 3_ Moisture Effect
steady-state regime
minimal lateral heat losses
reproducible measurements
Bound Water in the Solid structure

## Slide 6: Controlled Compression & Humidity: Tailoring Cellulose Fiber Orientation for Thermal Studies
Samples Preparation
Cellulose: Structurally similar to real bio-based insulating materials
Controlled
Porosity
Fiber Orientation
Relative Humidity
Axial Compression
Perpendicular Compression
6
(Arbocel® BC 200, from Kremer Pigmente)

## Slide 7: Measuring Thermal Conductivity in Bio-Based Materials is Challenging …
Measurements done with the HFM
following Standard Calibration process for samples with different thicknesses
7

## Slide 8: Towards a Reliable Measurement Protocol
8
varies with T in standard protocol → due to edge losses in thick samples
With 1 cm thick samples and raw flux averaging, almost independent of temperature
In this range (10–45°C), T has minimal physical effect on for cellulose
✅ A reference protocol for the rest of the study:
    Thickness: 1 cm
    Raw flux analysis (no calibration factor)
    ΔT = 5°C, mean T = 17.5°C, 22.5°C, 27.5°C
K. Mourda, Y. Zou, V. T. Nguyen, P. Coussot, "Enhancing the Accuracy of Thermal Conductivity Measurements with Insulating Construction Materials: Addressing Edge Effects and Methodological Improvements", Journal of Building Engineering (2025)
To Raw data: Direct Measurement of average heat fluxes Without Imposed Calibration Factor

## Slide 9: Bio-Based Materials: Complex and Anisotropic Structures
9

## Slide 10
10
Bio-Based Materials: Complex and Anisotropic Structures

## Slide 11: Thermal conductivity vs. Porosity in Dried Samples: Impact of Orientation_with theoretical Models
Structures parallel to heat flow
Structures perpendicular to heat flow
Heat flux
Heat flux
11

## Slide 12: Thermal conductivity vs. Porosity in Dried Samples: Impact of Orientation_with Effective Models
Heat flux
12
Our model_Transverse Direction
Our model_Axial Direction

## Slide 13
13
Bio-Based Materials: Complex and Anisotropic Structures

## Slide 14
Thermal conductivity vs. Apparent density: Analogy of our model with Litterature data
14

## Slide 15
Evolution of Thermal Conductivity with Relative Humidity at Different Porosities
15
Heat flux
30%

## Slide 16
Moisture Effect Depends on Porosity
Saturate samples (RH ≈ 100 %): start from maximum moisture content
100 % RH → 80 % → 60 % → 40 % → 30 % → Oven 60 °C → 0 % RH
16
Thermal conductivity cannot be predicted without considering both structure and moisture together
Drying
Bound Water
Drying

## Slide 17: Key Conclusions – Thermal Conductivity in Bio-based materials
✅ Robust protocol → 1 cm sample thickness, raw flux method
→ Extrapolable; aspect ratio ≤ 1/7 to be maintained
No significant variation with temperature (10–45°C)
📉 Thermal conductivity decreases with porosity
🔀 Fiber orientation matters: Stronger impact in perpendicular direction
💧 Moisture increases conductivity via bound water adsorption
Structure and moisture are intrinsically coupled
17

## Slide 18: Thank you !
karen.mourda@univ-eiffel.fr

## Slide 19: Fibers Morphology
Cellulose
ribbon-like morphology
300 µm in length, 10 µm in width,
and 1 µm in thickness
Dry cellulose solid phase:
Hemp
predominantly cylindrical morphology,
diameters from 20 to 40 µm
lengths of several millimeters
Human Hair: a quasi-cylindrical morphology (diameter 50 - 100 µm ).
SEM observations reveal faceted surfaces associated with the cuticle structure and non-circular cross-sections
Density of the keratine:

## Slide 20: Measurement Setup: Heat Flow Meter Method
Objective: Study and understand the Thermal conductivity of cellulose network
1. Calibration with Standard Material
2. Test with desired sample
Range of Temperature: 10°C to 45°C
Samples compressed of Cellulose of Porosity 0.5
final Thickness: 5 mm to 35 mm
intrinsic to material, should be independent of
🔍
25 mm
75 mm
Transducers
Top plate
Bottom
+
20

## Slide 21: Enhancing the Accuracy of Thermal Conductivity Measurement: Methodological Improvement (1/3)
Measurements done with the Standard Calibration process for samples with different thicknesses
21

## Slide 22: Enhancing the Accuracy of Thermal Conductivity Measurement: Methodological Improvement (2/3)
To Raw data: Direct Measurement of average heat fluxes Without Imposed Calibration Factor
Direct Measurement Without Imposed Calibration, Validating with air and standard sample NIST 1450E
22

## Slide 23: Establishing a Reliable Measurement Protocol
varies with T in standard protocol → due to edge losses in thick samples
With 1 cm thick samples and raw flux averaging, almost independent of temperature
In this range (10–45°C), T has minimal physical effect on for cellulose
✅ A reference protocol for the rest of the study:
    Thickness: 1 cm
    Raw flux analysis (no calibration factor)
    ΔT = 5°C, mean T = 17.5°C, 22.5°C, 27.5°C
K. Mourda, Y. Zou, V. T. Nguyen, P. Coussot, "Enhancing the Accuracy of Thermal Conductivity Measurements with Insulating Construction Materials: Addressing Edge Effects and Methodological Improvements", Journal of Building Engineering (2025)
Modeling Heat Transfer in the Sample
23

## Slide 24
Hypothesis: Fibers aligned perpendicularly to the compression axis =>
In practice, compression starts from the state associated with
« Extended to »
AXIAL
TRANSVERSE
Thermal conductivity vs. Porosity in Dried Samples: Impact of Orientation_with theoretical Models
24