## Slide 1
InterPore 2026 - Nantes, France - 22 May 2026
F. Neupert*, N. Eißmann, S. Loos, T. Büttner, I. Lindemann, T. Weißgärber, E. Andreou, C. Savaniu, J. Irvine, M. Al Aiti, G. M. Lange, P. Falat, G. Cuniberti
Coated Metallic Foams as Versatile Porous Substrate: From Hydrogen-Electrolysis Electrodes to Photocatalytic Water Treatment
&

## Slide 2: Coated Metallic Foams as Versatile Porous Substrate
Outline
1
4
General Information
Project Example: KoMMet
2
3
Coating methods
Project Example: EXSOTHyC
5
Conclusion, Q&A

## Slide 3: Coated Metallic Foams as Versatile Porous Substrate
1 General Information
Metallic foams
Materials
Ni, Co, Fe, Cu, Ag and their alloys
Properties
Pore size: 450 – 3000 µm
Porosity: > 90 %
Thickness: 1.5 – 5 mm
Areal density: 400 – 1500 g m-2
Advantages
High permeability  efficient fluid transport
Large accessible surface area
Good thermal and electrical conductivity
Mechanically stable 3D structure
Material provided in cooperation with Alantum Europe
© Alantum

## Slide 4: Coated Metallic Foams as Versatile Porous Substrate
1 General Information
Functionalizing and Tailoring
Functionalizing
Catalytic layers
Electrochemical active materials
Photoactive materials
 Adjustment of properties
Tailoring
Rolling – adjusting thickness and porosity
Graded structures – spatial variation of properties
Welding / joining – integration into larger structures
 Upscaling
Project AEL4GW
_
XXL-Cathodes for Alkaline Water Electrolysis
Notes: Challenges: Achieving uniform, conformal coatings on complex 3D strut networks
Ensuring strong adhesion and stability of the functional layer
Controlling coating thickness
Preserving pore accessibility and permeability

## Slide 5: Coated Metallic Foams as Versatile Porous Substrate
2 Coating methods
Dry coating process
10 µm
10 µm
Doctor blade technology
Scattering technology
The 3D structures were generated using ChatGPT (OpenAI).

## Slide 6: Coated Metallic Foams as Versatile Porous Substrate
10 µm
300 µm
10 µm
Wet Powder spraying
10 µm
Dispense robots/ screen printing
2 Coating methods
Wet coating process
The 3D structures were generated using ChatGPT (OpenAI).

## Slide 7: Coated Metallic Foams as Versatile Porous Substrate
3 Project Example: EXSOTHyC
EXSOTHyC: Exsolution-based Nanoparticles for lowest cost green hydrogen via electrolysis
Developing advanced materials, processes, and designs for alkaline electrolysers
Xu, X., et al. “Perovskite oxides as potential electrocatalysts for water splitting.” Nano Energy, Volume 29, 2016, Pages 122–139.
+

## Slide 8: Coated Metallic Foams as Versatile Porous Substrate
3 Project Example: EXSOTHyC
EXSOTHyC: Exsolution-based Nanoparticles for lowest cost green hydrogen via electrolysis
The basic metallic foam structure was generated using ChatGPT (OpenAI).
Spraying
+
Powder
+
Heat treatment
Binder mixture
Coated and heat-treated foam
Pure Ni foam
La0.42Ca0.48Ti0.89Co0.11O3

## Slide 9: Coated Metallic Foams as Versatile Porous Substrate
4 Project Example: KoMMet
KoMMet: Metallic foams for low-energy photocatalytic-based wastewater treatment
Energy-efficient wastewater purification using sunlight-driven photocatalysis and upconversion nanoparticles to remove pharmaceutical residues by converting NIR into UV/VIS light on porous UV-resistant foam substrate
KoMMet
+
https://www.edinst.com/resource/what-is-upconversion/

## Slide 10: Coated Metallic Foams as Versatile Porous Substrate
INC625 foam coated with UCMKs
INC625 Foam
UCMKs
+
Ionomer + Solvent
4 Project Example: KoMMet
KoMMet: Metallic foams for low-energy photocatalytic-based wastewater treatment
The basic metallic foam structure was generated using ChatGPT (OpenAI).
β-NaYF4

## Slide 11: Coated Metallic Foams as Versatile Porous Substrate
5 Conclusion
✓
✓
Open-cell metallic foams provide a highly permeable and mechanically stable 3D porous backbone
Tailoring approaches such as rolling, grading and joining support scalability and device integration
✓
✓
Functional coatings enable application-specific properties e.g. for electrochemical and photocatalytic systems
Different coating strategies allow tailored integration of active materials into complex porous structures

## Slide 12
Thanks for your attention!
Any questions?
Contact:
Felix Neupert
felix.neupert@ifam-dd.fraunhofer.de
+49 351 2537-349
Fraunhofer Institute for Manufacturing Technology and Advanced Materials IFAM
Dresden Branch
Winterbergstrasse 28, 01277 Dresden, Germany
www.ifam-dd.fraunhofer.de