## Slide 1: Rethinking Electrode Choice: Matching Porous Microstructures to Electrolyte Properties in Redox Flow Batteries
Sonia Khalghollah, Andreina Camano Alcedo, Arielle Chung, Tova Gilbert, and Maxime van der Heijden
Assistant Professor
Department of Chemical Engineering, University of Waterloo
InterPore2026, Session MS17, 21st of May

## Slide 2
250 μm
250 μm
250 μm
Urgent need for renewable technologies and energy storage at a large scale
We need tailored electrode microstructures for redox flow batteries
Forner-Cuenca, A. et al., J. Electrochem. Soc., 166(10) A2230-A2241 (2019)
Van der Heijden, M. et al., Encyclopedia of Energy Storage, Elsevier, 480-499 (2022)
Current generation not optimized, affecting three major losses:
Activation losses
Ohmic losses
Mass transport losses
↓ Pressure drop
↑ Electrochemical performance
2
Key properties:
- Surface area
- Permeability
- Mass transport
- Conductivity
Porous electrodes
Introduction
Experimental testing
Electrode manufacturing
Electrode optimization

## Slide 3
Increased fitness:
↑ Electrochemical power
↓ Pumping power
Genes
Generation
Selection
Crossover
Mutation
Selection
Generation
Genetic optimization of electrode structures
Bimodal pore size distribution enhances the performance
100 μm
Flow direction
0 10 20 30 40
Pore diameter [μm]
1000 generations
Thickness
Membrane
Current collector
3
Termination
Fitness
Ppump
Generation
Pel
Introduction
Experimental testing
Electrode manufacturing
Electrode optimization

## Slide 4
100 μm
X-ray tomography
Watershed segmentation
Towards realistic battery operation
Enhancing the performance of conventional electrode designs
0 10 20 30 40
Pore diameter [μm]
z
y
x
100 μm
Generation 1
1000 generations
Generation 1000
Flow direction
Cubic electrode
Conventional electrode
Vanadium electrolyte:
4
v = 1.5 cm s-1
Void
Solid
Introduction
Experimental testing
Electrode manufacturing
Electrode optimization

## Slide 5
The effect of the electrolyte chemistry
Trade-off between active surface area and through-plane conductivity
5
100 μm
100 μm
Generation 1000
Flow direction
Cubic electrode
Conventional
Vanadium electrolyte
TEMPO electrolyte
v = 1.5 cm s-1
Introduction
Experimental testing
Electrode manufacturing
Electrode optimization

## Slide 6
250 μm
250 μm
500 μm
Which electrode performs best for each chemistries?
Electrodes tested: Cell configurations tested:
Paper Cloth Felt Single-electrolyte Full cell
Chemistries tested: Single-electrolyte Full cell
All-Vanadium: VO2+/VO2+ V2+/V3+ - VO2+/VO2+
All-Iron: Fe2+/Fe3+ Fe0/Fe2+ - Fe2+/Fe3+
Aqueous-organic: [Fe(CN)6]3-/[Fe(CN)6]4- AQDS - [Fe(CN)6]3-/[Fe(CN)6]4-
Redox flow battery electrodes
Interplay between electrode microstructure and redox chemistry
6
Khalghollah, S. & Camano Alcedo, A. et al., in preparation
Introduction
Experimental testing
Electrode manufacturing
Electrode optimization

## Slide 7
Redox flow battery electrodes – All-iron
Interplay between electrode microstructure and redox chemistry
7
Chart: Current density [mA cm-2]
| 2.1796405968939054E-4 | 1.8145362598939851E-2 | 3.6019224105249562E-2 | 5.3831992761415454E-2 | 7.1604800040306893E-2 | 8.9315563618381513E-2 | 0.10693502282267001 | 0.12445759785235792 | 0.14196668584225181 | 0.15936422152187688 | 0.17664616411148337 | 0.19375603235653621
Felt - 20 mL min | 0.00028399 | 0.013705 | 0.02723 | 0.040886 | 0.054573 | 0.068425 | 0.082442 | 0.096689 | 0.11097 | 0.12547 | 0.1402 | 0.15524
Felt - 2.5 mL min | 0.00032587 | 0.022837 | 0.045899 | 0.06962 | 0.094493 | 0.12117 | 0.14992 | 0.18127 | 0.21472 | 0.25077 | 0.28851 | 0.32773 | 0.36837
Freudenberg - 20 mL min | 0.00032148 | 0.013353 | 0.026217 | 0.03909 | 0.051942 | 0.064716 | 0.077648 | 0.090498 | 0.10345
Freudenberg - 2.5 mL min | 0.0004372 | 0.02595 | 0.053016 | 0.083962 | 0.12063 | 0.16189 | 0.20515 | 0.24893 | 0.29341
Cloth - 20 mL min | 0.00029033 | 0.013411 | 0.026442 | 0.039437 | 0.052251 | 0.064878 | 0.077524 | 0.090134 | 0.10277 | 0.11526 | 0.13004 | 0.15288
Cloth - 2.5 mL min | 0.00041568 | 0.025682 | 0.051419 | 0.078146 | 0.10656 | 0.13774 | 0.17176 | 0.20881 | 0.24819 | 0.2903 | 0.33385 | 0.37704
Ideal performance
Winner for Fe2+-Fe3+:
Single-electrolyte cell with 1 Fe2+/Fe3+ tank:
Full cell with Fe0/Fe2+ - Fe2+/Fe3+
(cloth on Fe2+/Fe3+ side)
Chart: Current density [mA cm-2]
| -9.815821960784314 | -29.792372843137255 | -49.822790196078429 | -69.831133333333327 | -89.845839215686283 | -109.84333431372551 | -129.86215686274511 | -149.8828480392157
Felt - 20 mL min | 1.2387 | 1.187 | 1.1432 | 1.1115 | 1.0728 | 1.0288 | 0.93759 | 0.78429
Felt - 2.5 mL min | 1.1969 | 1.1753 | 1.1544 | 1.1327 | 1.1073 | 1.0749 | 1.0276 | 0.96311
Freudenberg - 20 mL min | 1.1996 | 0.96941 | 0.84402 | 0.76963
Freudenberg - 2.5 mL min | 1.1508 | 1.0648 | 0.93479 | 0.88707 | 0.82803
Cloth - 20 mL min | 1.1934 | 0.93766 | 0.76748 | 0.54958
Cloth - 2.5 mL min | 1.1578 | 1.0762 | 0.96708 | 0.89778 | 0.84238 | 0.76385 | 0.65278
250 μm
500 μm
Winner for Fe0-Fe2+:
Fast kinetics: combination of p and km
Plating reaction: combination of p and ECSA
Introduction
Experimental testing
Electrode manufacturing
Electrode optimization

## Slide 8
Redox flow battery electrodes – All-iron
Interplay between electrode microstructure and redox chemistry
8
Khalghollah, S. & Camano Alcedo, A. et al., in preparation
Introduction
Experimental testing
Electrode manufacturing
Electrode optimization
Chemistry | Best electrode
VO2+/VO2+ | Felt
V2+/V3+ | Felt
Fe2+/Fe3+ | Cloth
Fe0/Fe2+ | Felt
[Fe(CN)6]3-/[Fe(CN)6]4- | Paper
AQDS | Felt
Which electrode performs best for each chemistries?
Showing the need to select the best
electrode for each application
Next steps:
Cycling performance:
Full-vanadium with the felt electrode on both sides.

## Slide 9
Advanced designs - TPMS
Primitive
Gyroid
IWP
Diamond
1 mm
Cubic
lattice
Oxidation + Carbonization
Flow cell testing
TEMPO electrolyte
Additive manufacturing of TPMS structures
Advanced electrode structures are expected to enhance the mass transport
9
Van der Heijden, M. et al., Adv. Mater. Technol., 8 (18), 2300611 (2023)
Van der Heijden, M. et al., SSRN pre-print (2026)
Advantages:
V Enhanced mass transfer
V Flexibility in design and material
V Pre- and post-processing methods
Disadvantages to date:
X Lower electrochemical surface area
X Lower performance
Gyroid
1 mm
Felt
500 μm
1 cm
Introduction
Experimental testing
Electrode manufacturing
Electrode optimization

## Slide 10
10
Porous electrode synthesis
MXene-coated 3D print performance
Solution mixture
3D printing process
3D printed electrode
MXene-coated electrode
Carbonized electrode
Hierarchically organized porous materials
For redox flow batteries
Application
Introduction
Experimental testing
Electrode manufacturing
Electrode optimization

## Slide 11
Acknowledgements
Projects collaborators
11
Projects collaborators:
Projects funding:
Group acknowledgements:
Andreina Camano Alcedo
Sonia Khalghollah
Tova Gilbert
Arielle Chung
Muhammad Zain Qamar
m35vande@uwaterloo.ca
https://vdheijdenlab.com/