## Slide 1: Mass transport characterization in nanoporous polymer electrolyte membranes used in electrochemical systems.
HTJS - May. 14th 2025
1. Univ. Bordeaux, CNRS, Bordeaux INP, I2M, UMR 5295, F-33400, Talence, France
2. Arts et Metiers Institute of Technology, CNRS, Bordeaux INP, I2M, UMR 5295, F-33400 Talence, France
3. Arts et Metiers Institute of Technology, CNAM, LIFSE, F-75013 Paris, France
Alejandro MATEOS1,2,3, Abel NETTER1,2,3, Tommaso CARPOSU3, Michael DELIGANT3, Stéphane CHEVALIER1,2
Collaboration Prof. Dr. ChungHyuk Lee.

## Slide 2
Mass transport in PEM
Mechanisms that drive proton conductivity of PEM:
PEM Water Electrolyzer

## Slide 3
Mass transport in PEM
Pristine
Contaminated (M2+ cation)
Nano pores
J L Pineda-Delgado et al 2019 Nanotechnology 30 105707

## Slide 4
How Cation Contaminants Moves in Nafion?
Understanding how cations move in fuel cells is an important first step for developing mitigation strategies.
The reaction at cathode can consume H+ by 2H+ + 2e-→H2, so Ce can go to that position of H+ and migrate with potential-driven
The cation can diffuse by concentration gradients
Slide from
Chung Lee, TMU

## Slide 5
Technological and scientific locks
 Microfluidic electrolyzer combined with IR imaging can answer these needs
How to access to the PEM chemistry in operando?
How to measure the PEM transport properties in operando?
Current methods are mainly limited to
Electrochemical measurements (such as EIS)
X-ray or neutron imaging which cannot be used for screening or aging experiments

## Slide 6
Our approach: operando IR imaging
Objectives:
Develop the chip
Characterize using IR
Mesure the water gradients
Benefits:
  Chemical information
  Safe beam energy levels
  Operando transmission characterization
  Design flexibility
Constraints:
  Water attenuation
  Materials
  Transparency
  Electrochemical performance

## Slide 7
Microfluidic electrolyzer
How do we image the PEM water content?

## Slide 8
Microfluidic electrolyzer
Take home message:
We can optically access to the PEM water content and cation concentration
Water + Sulfuric acid
(0.5 M)
Water + Sulfuric acid
(0.1, 0.5 or 1 M)
PEM is Aquivion E80 (Syensqo)

## Slide 9
Experimental Setup: Thermospectroscopy
9
: Thermal emission
: Light from the black body source
DL (-)
Take home message:
Live monitoring of the IR light transmission through the PEM

## Slide 10
Cation diffusion

## Slide 11
Data analysis

## Slide 12
Data analysis

## Slide 13
Data analysis
Diffusion fitting
Undergoing work
(collab TMU – prof. Chung Lee)

## Slide 14
Conclusion
We designed a PEM microfluidic electrolyzer
We imaged the water gradients in operando in the nanoporous PEM
We observed a strong impact of cations concentration on PEM water gradient
Next: identification of diffusion and ion mobility through nanopores

## Slide 15
Acknowledgements
Contact:
Ass. Prof. Stéphane Chevalier
Institute of Mechanical Engineering of Bordeaux
France
stephane.chevalier@ensam.eu
References from my group:
Krause, Kevin, et al. “Heat and Mass Transfer Visualisation of an Exothermic Acid-Base Microfluidic Reactor Using Infrared Thermospectroscopy.” Quantitative InfraRed Thermography Journal, vol. 00, no. 00, Taylor & Francis, Sept. 2024, pp. 1–18, doi:10.1080/17686733.2024.2402141.
Krause, Kevin, et al. “Water Gradient Manipulation through the Polymer Electrolyte Membrane of an Operating Microfluidic Water Electrolyzer.” Journal of Power Sources, vol. 623, Dec. 2024, p. 235297, doi:10.1016/j.jpowsour.2024.235297.
Link to my WebPage

## Slide 16
Slope in thin media
Slope = -0.5

## Slide 17
Working Principles of IR PHTI