## Slide 1
Presenter: Ashkan Irannezhad, PhD Supervisor: Prof. Aimy Bazylak
May 2026
Prof. Aimy
Bazylak
Vasant Batta
Dr. Tess Seip
Dr. Alexandre Tugirumubano
Dr. Aida Farsi
Dr. Harsharaj Parmar
Dr. Qianpu
Wang

## Slide 2: Electrochemical CO2 Conversion for Carbon Emission Reduction
CO2 Electrolyzer
Carbon capture, utilization, and storage (CCUS) is widely recognized as essential for achieving net-zero climate targets by 2050.
Among CCUS strategies, those powered by renewable energy to convert captured CO2 into value-added chemicals using CO2 electrolyzers are particularly attractive, offering a carbon-negative alternative to the conventional fuels and chemicals on which society depends.
Ashkan Irannezhad, PhD (Ashkan.Irannezhad@utoronto.ca)
O’Brien, Colin P., et al. "CO2 electrolyzers." Chemical Reviews (2024)

## Slide 3: How CO2 Electrolyzers Operate
Anode
Cathode
Catalyst coated GDL
Flow Fields
Membrane
Catalyst coated GDL
Flow Fields
KOH (l)
CO2
e-
e-
O2 (g)
CO
CO2
H2O
Ashkan Irannezhad, PhD (Ashkan.Irannezhad@utoronto.ca)
K+
CO2 electrolyzers operate through coupled mass transport, charge transfer, and electrochemical reaction mechanisms to convert CO2 into value-added products such as CO.
Catalyst
H2O
K+
CO2
OH-

## Slide 4: How CO2 Electrolyzers Operate
e-
e-
Anode
Cathode
Catalyst coated GDL
Flow Fields
Membrane
Catalyst coated GDL
Flow Fields
KOH (l)
CO2
O2 (g)
CO
Ashkan Irannezhad, PhD (Ashkan.Irannezhad@utoronto.ca)
CO2 electrolyzers operate through coupled mass transport, charge transfer, and electrochemical reaction mechanisms to convert CO2 into value-added products such as CO.
H2O
K+
CO2
OH-

## Slide 5: How CO2 Electrolyzers Operate
e-
e-
Anode
Cathode
Catalyst coated GDL
Flow Fields
Membrane
Catalyst coated GDL
Flow Fields
KOH (l)
CO2
O2 (g)
CO
Ashkan Irannezhad, PhD (Ashkan.Irannezhad@utoronto.ca)
CO2 electrolyzers operate through coupled mass transport, charge transfer, and electrochemical reaction mechanisms to convert CO2 into value-added products such as CO.
H2O
K+
CO2
OH-

## Slide 6: How CO2 Electrolyzers Operate
e-
e-
Anode
Cathode
Catalyst coated GDL
Flow Fields
Membrane
Catalyst coated GDL
Flow Fields
KOH (l)
CO2
O2 (g)
CO
Ashkan Irannezhad, PhD (Ashkan.Irannezhad@utoronto.ca)
CO2 electrolyzers operate through coupled mass transport, charge transfer, and electrochemical reaction mechanisms to convert CO2 into value-added products such as CO.
H2O
K+
CO2
OH-

## Slide 7: How CO2 Electrolyzers Operate
e-
e-
Anode
Cathode
Catalyst coated GDL
Flow Fields
Membrane
Catalyst coated GDL
Flow Fields
KOH (l)
CO2
O2 (g)
CO
Ashkan Irannezhad, PhD (Ashkan.Irannezhad@utoronto.ca)
CO2 electrolyzers operate through coupled mass transport, charge transfer, and electrochemical reaction mechanisms to convert CO2 into value-added products such as CO.
H2O
K+
CO2
OH-

## Slide 8: How CO2 Electrolyzers Operate
e-
e-
Anode
Cathode
Catalyst coated GDL
Flow Fields
Membrane
Catalyst coated GDL
Flow Fields
KOH (l)
CO2
O2 (g)
CO
Ashkan Irannezhad, PhD (Ashkan.Irannezhad@utoronto.ca)
CO2 electrolyzers operate through coupled mass transport, charge transfer, and electrochemical reaction mechanisms to convert CO2 into value-added products such as CO.
H2O
K+
CO2
OH-

## Slide 9: How CO2 Electrolyzers Operate
e-
e-
Anode
Cathode
Catalyst coated GDL
Flow Fields
Membrane
Catalyst coated GDL
Flow Fields
KOH (l)
CO2
O2 (g)
CO
Ashkan Irannezhad, PhD (Ashkan.Irannezhad@utoronto.ca)
CO2 electrolyzers operate through coupled mass transport, charge transfer, and electrochemical reaction mechanisms to convert CO2 into value-added products such as CO.
Hydrophilic KHCO3 salt
H2O
K+
CO2
OH-

## Slide 10: How CO2 Electrolyzers Operate
e-
e-
Flooding
Anode
Cathode
Catalyst coated GDL
Flow Fields
Membrane
Catalyst coated GDL
Flow Fields
KOH (l)
CO2
O2 (g)
CO
Ashkan Irannezhad, PhD (Ashkan.Irannezhad@utoronto.ca)
CO2 electrolyzers operate through coupled mass transport, charge transfer, and electrochemical reaction mechanisms to convert CO2 into value-added products such as CO.
H2O
K+
CO2
OH-
Hydrophilic KHCO3 salt

## Slide 11: Scaling and Heating Effects Drive CO2 Electrolyzers to Higher Temperatures
Ashkan Irannezhad, PhD (Ashkan.Irannezhad@utoronto.ca)
As CO2 electrolyzers scale toward industrial operation, understanding heat management and the viable operating temperatures in larger systems is important.
Owing to the energy inefficiency of electrolyzers, heat generation within CO2 electrolyzer stacks will favour operating temperatures of 40 to 70, far from the ambient temperatures used so far.
How temperature affects the multiphase transport in CO2 electrolyzer’s porous electrode?
Burdyny et al., "Scaling and heating will drive low-temperature CO2 electrolysers to operate at higher temperatures." Nature Energy (2025)

## Slide 12: Operando X-ray Radiography Enables Direct Visualization of Multiphase Transport
Ashkan Irannezhad, PhD (Ashkan.Irannezhad@utoronto.ca)
We conducted synchrotron-based operando X-ray radiography at the Canadian Light Source (CLS) to visualize multiphase transport inside the gas diffusion electrode of CO2 electrolyzers at different operating temperatures.
X-ray absorption values indicate locations where the quantity of anolyte has increased with respect to the reference image (before operation).

## Slide 13: How Temperature Affects Anolyte Saturation in the Cathode GDE During CO2 Electrolysis
Ashkan Irannezhad, PhD (Ashkan.Irannezhad@utoronto.ca)
We visualize electrolyte saturation within a silver-based cathodic gas diffusion electrode (GDE) in CO2 electrolyzers operated at 200 mA.cm-2 over 2 h at 3 different temperatures: 25, 40, and 60.
This behavior is likely attributed to higher KHCO3 solubility at elevated temperatures, which suppresses carbonate/bicarbonate salt formation.
The results reveal an inverse relationship between electrolyte saturation in the GDE and operating temperature, with the lowest electrolyte saturation observed at 60.
40
60
25

## Slide 14: Spatial Distribution of Salt Precipitation in the Cathode GDE
Ashkan Irannezhad, PhD (Ashkan.Irannezhad@utoronto.ca)
At all temperatures, the salt precipitates were primarily located adjacent to and on top of the silver catalyst, indicating preferential salt precipitation on the silver catalyst rather than the PTFE or carbon black particles at all temperatures.
SEM/EDX maps of ex-situ degraded cathode GDEs at 25, 40, and 60 confirms the lack of salt formation at the highest temperature.
40
60
25

## Slide 15: Reduced salt precipitation at elevated temperatures lowers flooding but does not necessarily improve CO2 electrolysis performance
Ashkan Irannezhad, PhD (Ashkan.Irannezhad@utoronto.ca)
High-temperature operation introduces a transport trade-off; while it suppresses flooding and salt precipitation, it may also shift the cathode toward CO2-limited performance. Future work should identify the optimal operating temperature and GDE designs that balance electrolyte management with sufficient local CO2 availability.
At elevated temperatures, reduced CO2 solubility limits dissolved CO2 availability near the catalyst surface.
Lower local CO2 concentration restricts CO production, resulting in lower Faradaic efficiency toward CO (FECO).
Flooding mitigation alone is insufficient to achieve optimal high-temperature CO2 electrolyzer performance.
40
60
25

## Slide 16: Summary
Ashkan.Irannezhad@utoronto.ca
Synchrotron-based operando X-ray radiography enabled direct visualization of electrolyte transport inside the cathodic gas diffusion electrode (GDE) at different operating temperatures (25, 40, and 60).
Elevated temperatures reduced electrolyte saturation inside the GDE.
Lower flooding at higher temperatures did not necessarily translate to higher CO selectivity.
Reduced CO2 solubility at elevated temperatures likely limited local CO2 availability near the catalyst surface.
Results highlight the strong coupling between heat management, multiphase transport, and electrochemical performance in CO2 electrolyzers.
Ashkan Irannezhad, PhD
Thank You
May 2026
Supervisor: Prof. Aimy Bazylak