## Slide 1
Morphological and non Beerian radiative characterization of a fibrous medium
Presented by : Mahé Souveton
Supervision : Franck Enguehard
Vital Le Dez

## Slide 2
Summary
Introduction to the subject
  Context
  Radiative characterization
  Morphological results
Development of a non Beerian model
  Definitions
  Practical application
  Monte Carlo algorithm
  Results and discussions
Conclusion and perspectives

## Slide 3
Introduction to the subject

## Slide 4
Introduction to the subject
Context
Industrial context:
  Thermal insulation at high temperatures often relies on highly porous materials.
  The radiative transfer must be characterized at all scales.
Representative medium:
  Theoretical study of a virtual cold fibrous medium composed of overlapping cylinders (acting as an absorbing and scattering phase).
  Morphological simplification: infinite cylinders, same shape and properties, randomly orientated medium statistically homogeneous and isotropic.
  Either specular or diffuse conditions imposed between void and fibers. No interface events on entrance and exit of the calculation box.
Radiative characterization:
  Directional-hemispherical transmittance and reflectance values.
  Homogenization procedure: determining an equivalent continuous medium.
and values as a function of the angle of the incident radiation
SEM of a zirconia felt
A computer-generated virtual fibrous medium
Specular

## Slide 5
Introduction to the subject
Radiative characterization
Direct Simulation Monte Carlo (DSMC):
  A Monte Carlo algorithm follows each ray through reflection and refraction events until its absorption or its exit of the calculation box.
Standard homogenization procedure:
  Scalar coefficients have to be determined (, , , , , …):
    - By inversion (requires to specify a phase function).
    - By direct identification (RDFI [1]).
Non Beerian approach:
  The statistics in our fibrous medium does not follow Beer-Lambert law !
  A non Beerian model, integrated inside a Monte Carlo algorithm, could be constructed with the true statistics of absorption and scattering.
, , ,
Monte Carlo in the fibrous medium (top) and in the continuous medium (bottom)
[1] Tancrez, M., & Taine, J. (2004). Direct identification of absorption and scattering coefficients and phase function of a porous medium by a Monte Carlo technique. International Journal of Heat and Mass Transfer, 47(2), 373-383
Homogenization

## Slide 6
Introduction to the subject
Morphological results [2]
Study of random chords
  -random, -random, -random chords, etc…
  Provides an algorithm to construct an homogeneous and isotropic fibrous medium.
Analytical derivation for a stack of cylinders
  Porosity as a function of the number of fibers .
  REV (from the standard deviation of porosity )
  Autocorrelation function.
Final result
  CDF of -random chord lengths in the fibrous phase :
[2] Souveton M. et al. (2026). Morphological properties of random arrays of infinitely long overlapping cylinders for
modeling statistically homogeneous and isotropic fibrous media. Physical Review E, 113, 024111.
Chords in an isolated cylinder (, and )
as a function of the porosity for circular observation subsurfaces of various radius
analytical vs measurements

## Slide 7
Development of a non Beerian model

## Slide 8
Development of a non Beerian model
Definitions and hypothesis [3]
Generalized radiative functions:
  Extinction CDF:
  Absorption and scattering PCF: and
  Conditional probability of scattering:
  Probability to be in the void phase:
    Where means « after the scattering event » and , or is the phase in which the ray is travelling.
First trajectories are -chords, the next are -chords.
Scattering phase function:
  Following Snell-Descartes’s law (specular)
  Following Lambert’s law (diffuse) with
DSMC with a Monte Carlo raytracing algorithm in the fibrous medium
[3] Several works on a non Beerian approach by Dauvoix, Seyer, Enguehard, Taine, etc…

## Slide 9
Development of a non Beerian model
Practical application
Example:
  and:
    - Diffuse reflection:
    - Specular reflection: and
Scattering phase function:
  Analytical expression derived for the specular case.
  Expression obtained by a curve fitting for the diffuse case.
Monte Carlo
Analytical
Scattering phase function indicatrix in the fibrous medium with specular conditions
Extinction CDF ()

## Slide 10
Development of a non Beerian model
Monte Carlo algorithm for the model
For each ray impinging the calculation box:
  A random distance before extinction is drawn according to .
  A uniform number on [0, 1] is drawn and compared to .
    - If absorbed, a new ray is fired.
    - If scattered, a new direction is chosen in accordance with the scattering phase function.
  The algorithm continues until the ray is out of the calculation box (or absorbed).

## Slide 11
Development of a non Beerian model
Results and discussions
Specular interface:
Diffuse interface:

## Slide 12
Development of a non Beerian model
Results and discussions
Highlighting the role of the variable
  In the void phase:
  At the optically thin limit:
  Otherwise:
  The asymptotic behavior of the conditional scattering probability:

## Slide 13
Conclusion and Perspectives
Several morphological properties of statistically homogeneous and isotropic cylinder stacks have been determined analytically.
The generalized non Beerian radiative properties of the equivalent homogeneous medium have also been determined analytically, especially:
  Extinction CDF
  Scattering and absorption CPF
  Specular scattering phase function
They have been used in a non Beerian radiative transfer model, and we are currently in the process of analyzing the results.
We need to compare the previous results with a Beerian approach.

## Slide 14
Appendix

## Slide 15
Morphological study
Definitions
Classic chords distributions:
  -random chords
  -random chords
  -random chords
Let us focus on -random chords
Probability density function (PDF) and cumulative distribution function (CDF) of -random chord lengths in an isolated cylinder [2]:
    (results are scaled with respect to the diameter of the fibers)
Probability that an -random chord length in an isolated cylinder is less than
[2] Tomadakis, M. M., & Sotirchos, S. V. (1993). Random paths in random arrays of cylinders. Radiation research, 135(3), 302-311.
Chords in an isolated cylinder (, and )

## Slide 16
Morphological study
-random chords in a random stack of cylinders
We study now a random stack of overlapping infinite cylinders. The medium is statistically homogeneous and isotropic. Let us denote the porosity (void volume fraction) . What is ?
In the void phase, the behaviour is known:
  : Beerian phase [2]
In the fiber phase:
  [2]
  In the Laplace domain [3]: with the autocorrelation function of the void phase
Knowing will allow the numerical evaluation of
Visual representation of chords emitted in volume in the void phase (dark blue) and in the fiber phase (light blue)
[3] Roberts, A. P., & Torquato, S. (1999). Chord-distribution functions of three-dimensional random media: approximate first-passage times of Gaussian processes. Physical Review E, 59(5), 4953.

## Slide 17
Morphological study
Statistics of overlapping fibers
Let and be two random points, their distance, and , two random variables counting the number of cylinders covering and .
The covering theory says:
  [4]
  Therefore : and
  Overlapping ratio :
With more calculations, we can deduce:
Visual representation of two random points within the medium
[4] Sampson, W. W. (2008). Modelling stochastic fibrous materials with mathematica®. Springer Science & Business Media.

## Slide 18
Morphological study
Autocorrelation function and :
The autocorrelation function of the void phase is easily obtained:
Therefore we conclude:
Numerical inversion of the Laplace expression:
  For a very fast inversion with precision up to 2 digits: Wilcox’s algorithm.
  A slower approach with precision up to 8 digits: De Hoog’s algorithm.
Asymptotic expansion:
Probability that an -random chord length is less than in the fiber phase for different porosities

## Slide 19
Morphological study
Representative Elementary Volume for porosity:
In a representative box, the effective porosity of a subarea or a subvolume is not , but fluctuates.
Let us note the standard deviation of the effective porosity when is moved around.
Analytical expressions [5]:
Asymptotic behaviors for large :
Standard deviation of the effective porosity in an observation domain as a function of its dimension and the mean porosity
[5] Torquato, S. (2002). Random heterogeneous materials: microstructure and macroscopic properties (Vol. 16). New York: Springer.