## Slide 1: RANDOM-WALK SIMULATION METHODS FOR THE MODELING OF BALLISTIC/DIFFUSIVE HEAT AND MASS TRANSFER IN EVOLVING POROUS MEDIA
20260520_Vignoles_Interpore_ Nantes
Gérard Vignoles
Laboratoire des Composites Thermostructuraux
3 allée de la Boétie – Pessac – France

## Slide 2: CONTENTS
Context
Problems
Methods
Some results
Outlook
May 20, 2026
Vignoles - Interpore 2026, Nantes
2

## Slide 3: CONTEXT
May 20, 2026
Vignoles - Interpore 2026, Nantes
3

## Slide 4: LABORATOIRE DES COMPOSITES THERMOSTRUCTURAUX LABORATORY FOR THERMOSTRUCTURAL COMPOSITES
38 years of joint research & innovation
May 20, 2026
Vignoles - Interpore 2026, Nantes
4

## Slide 5: WHAT ARE THERMOSTRUCTURAL COMPOSITES ?
Ceramic-Matrix Composites(CMC)
Reinforced by ceramic fibers
Interphase between fibers and matrix
Non-brittle, even though having brittle components !
And, of course : stiff & refractory
May 20, 2026
Vignoles - Interpore 2026, Nantes
5

## Slide 6: APPLICATIONS
Current
Space propulsion: nozzle throat, divergent
Brakes for aviation and racing cars
Thermal protection systems
Ionic propulsion
Industry
Future
Aircraft propulsion
Nuclear (fission, fusion)
Other energies
May 20, 2026
Vignoles - Interpore 2026, Nantes
6

## Slide 7: Application spectrum of CMCs
Adv. civil eng.
Service temperature (°C)
Duration
3000
2000
1000
0
Minute
Hour
Day
Month
Year
Century
Decade
Civil aircraft propulsion
Nuclear, Industrial
Ion thrusters
Brakes
Space technology
Military aircraft propulsion
May 20, 2026
Vignoles - Interpore 2026, Nantes
7

## Slide 8: PROBLEMS
May 20, 2026
Vignoles - Interpore 2026, Nantes
8

## Slide 9: ABLATIVE CF/C MATERIALS
Compact (almost non-porous) materials
  3D C/C
  Needle-punched « 2.5D » C/C
Felts (eg. Mersen’s Calcarb ®)
  Pyrolyzed C/resin
  Needle-punched « 2.5D » C/C
  3D C/C
Porous ablators
  Pyrolyzed C/resin
  Felts (eg. Mersen’s Calcarb ®)
May 20, 2026
Vignoles - Interpore 2026, Nantes
9

## Slide 10: ABLATION
modifies fluxes and ablation rate
Surface becomes rough
linked to effective rate
Porous ablators acquire an affected depth
May 20, 2026
Vignoles - Interpore 2026, Nantes
10

## Slide 11: HIGH-TEMPERATURE HEAT TRANSFER
Applications
  Thermal gradients in CVI
  Thermal protection systems for atmospheric reentry
  Heat management in nuclear & CSP power plants
Materials
  Ceramic foams
  Fibrous media
  Ceramic-matrix composites
large contribution of radiation even at moderate temperatures
Very porous, large pores
May 20, 2026
Vignoles - Interpore 2026, Nantes
11

## Slide 12: PURPOSE OF THE MODELING APPROACH
Ablation
Account for diffusion/reaction competition
Describe morphological evolution of the material
Obtain information on evolution kinetics & evolving effective properties
Work on 3D images  as close as possible to the « actual material »
Heat transfer
Account for radiation/conduction competition
Obtain morphology/effective properties relationships
Interest of Random-walks methods
Large computational domains :
Memory requirements
May 20, 2026
Vignoles - Interpore 2026, Nantes
12

## Slide 13: METHODS
May 20, 2026
Vignoles - Interpore 2026, Nantes
13

## Slide 14: PHENOMENA – « small scale »
Mass transfer
Solid/gas are clearly distinguished
Gas may be rarefied => address kinetic theory of gases
Ordinary diffusion : Brownian motion
Deposition/ablation are interfacial phenomena
Growth/recession: Moving fronts
Heat transfer
Radiative cavities are distinguished
Radiative transfer : analogous to rarefied gas transfer
Conductive transfer : analogous to ordinary gas diffusion
Exchange conditions between void and solid : analogous to « handling sticking events »
May 20, 2026
Vignoles - Interpore 2026, Nantes
14

## Slide 15: PHENOMENA – « large scale »
Mass transfer
Continuous field of solid mass fraction
Gas described by its effective anisotropic diffusion coefficient
Ordinary diffusion : Brownian motion
Deposition/ablation are volumic and surfacic phenomena
Growth/recession: evolving porosity and moving fronts
Heat transfer
Continuous field of anisotropic conductivity
Radiative transfer : only as a conductivity modifier
Conductive transfer : analogous to ordinary gas diffusion
Exchange conditions between void and solid : analogous to « handling sticking events »
May 20, 2026
Vignoles - Interpore 2026, Nantes
15

## Slide 16: EQUATIONS AND METHODS at two scales
Mass transfer
Boltzmann kinetic equation: « Kinetic » (or Pearson) random walk
Diffusion equation for solid : « Brownian » random walk
Reaction: notion of « sticking probability »
Heat transfer
Kinetic equation for radiation : « Kinetic » random walk (or simple ray-tracing)
Diffusion/conduction equation for solid : « Brownian » random walk
Rad./Cond. exchange: « transition probability »
May 20, 2026
Vignoles - Interpore 2026, Nantes
16

## Slide 17: Fiber-scale infiltration modeling
1
2
3
4
1
Random position and direction
Voxel borders
Binary collision
Wall collision
End of time process
1
Start of time process
Random position
Random direction
Isotropic distribution
2
Binary collision
Time until next collision
Random direction
Isotropic distribution
3
Wall collision without reaction
Random direction
Knudsen’s cosine law
4
Wall collision with reaction
+
1
Random walk w/ reaction and surface growth
G. L. VIGNOLES, W. ROS, C. MULAT, O. COINDREAU, C. GERMAIN, Comput. Mater. Sci. 50, 1157-1168 (2011)
Notes: 17

## Slide 18
Diffusive step : random
direction w/ anisotropic
Gaussian distribution
following D
Advective step following
div.D (heterogeneity)
Diffusion tensor D
computed in each voxel from
greyscale value (density)
and local fiber orientation
Large-scale Infiltration Modelling
Itô-Taylor random walks
« Russian roulette » for deposition reaction
G. L. VIGNOLES, W. ROS, I. SZELENGOWICZ, C. GERMAIN, Comput.l Mater. Sci. 50, 1871-1878. (2011)

## Slide 19: RESULTS - PART 1
Ablation of a fibrous preform
May 20, 2026
Vignoles - Interpore 2026, Nantes
19

## Slide 20: Ablation simulations: porous felts
Rebuilt flow conditions
Measured recession rate
Affected depth observation & measurement
G. L. VIGNOLES et al., Carbon (2018), vol. 134, pp. 376–390.
Nitrogen plasma ablation testing on carbon preforms
New analytical and numerical models
Effective rate constants
Intrinsic rate constants
May 20, 2026
Vignoles - Interpore 2026, Nantes
20

## Slide 21: DETAILED NUMERICAL MODEL FOR ABLATION
What does it solve ?
Diffusion-reaction equation (1 species ; ablation + recombination)
+ surface recession equation (solid)
Single boundary condition : fixed conc. at a given distance above surface
Parameters: D, knit, krec (diffusion & reaction constants)
Output
Effective ablation depth
Effective reaction rate = impinging mole flux /surface concentration
Random walk « engine »
Brownian walkers  continuum diffusion
Simplified Marching Cube
G. L. VIGNOLES et al., Carbon (2018), vol. 134, pp. 376–390.
May 20, 2026
Vignoles - Interpore 2026, Nantes
21

## Slide 22: NUMERICAL SIMULATION OF ABLATION
G. L. VIGNOLES et al., Carbon (2018), vol. 134, pp. 376–390.
May 20, 2026
Vignoles - Interpore 2026, Nantes
22

## Slide 23: NUMERICAL SIMULATION OF ABLATION
1 pix = 2 µm
G. L. VIGNOLES et al., Carbon (2018), vol. 134, pp. 376–390.
May 20, 2026
Vignoles - Interpore 2026, Nantes
23

## Slide 24: ABLATION : DIMENSIONLESS RESULTS
where
A simple analytical model predicts a slope of 2
G. L. VIGNOLES et al., Carbon (2018), vol. 134, pp. 376–390.
May 20, 2026
Vignoles - Interpore 2026, Nantes
24

## Slide 25: ABLATION : DIMENSIONLESS RESULTS
This exponent is ½ in the analytical model
G. L. VIGNOLES et al., Carbon (2018), vol. 134, pp. 376–390.
May 20, 2026
Vignoles - Interpore 2026, Nantes
25

## Slide 26: MODEL EXPLOITATION: NITRIDATION IN PLASMA
Diffusion coefficient is corrected by the Knudsen effect
and tortuosity coefficient :
Rate constants are scaled wrt ¼ molecular velocity
dp =
Effective nitridation rate is corrected by the blowing effect
G. L. VIGNOLES et al., Carbon (2018), vol. 134, pp. 376–390.
May 20, 2026
Vignoles - Interpore 2026, Nantes
26

## Slide 27: IDENTIFIED NITRIDATION PROBABILITY
G. L. VIGNOLES et al., Carbon (2018), vol. 134, pp. 376–390.
May 20, 2026
Vignoles - Interpore 2026, Nantes
27

## Slide 28: ABLATION – SUMMARY & OUTLOOK
Interest of the numerical model
Results are similar to predictions of a simple analytical model
The differences are due to the complex porous structure
A complete strategy to interpret ablation tests
Effective reaction constants can be recovered from CFD analysis + image analysis
The method can be used the other way to obtain the influence of structural parameters on ablation rate
 It becomes a design tool
Next step: application to oxidation of Cf/C composites
G. L. VIGNOLES et al., Carbon (2018), vol. 134, pp. 376–390.
May 20, 2026
Vignoles - Interpore 2026, Nantes
28

## Slide 29: RESULTS - PART 2
Heat transfer by conduction and radiation
May 20, 2026
Vignoles - Interpore 2026, Nantes
29

## Slide 30: HYBRID RANDOM WALK
Solid phase: Brownian motion, simulates diffusion linked to heat conduction
Fluid phase: ray-tracing or kinetic RW
Interface: « flux matching » condition
G. L. VIGNOLES, Int. J. of Heat & Mass Transfer 93, 707–719 (2016)
May 20, 2026
Vignoles - Interpore 2026, Nantes
30

## Slide 31
Open-cell SiSiC foams (courtesy SUPSI)
Nu’ = 4sT3/ks.(P/Sv)
kcond/ksolid
1
May 20, 2026
Vignoles - Interpore 2026, Nantes
31

## Slide 32: RADIATIVE ETC EXCESS VS. RADIATION/CONDUCTION RATIO
High-T
Emissivity-independent regime
Low-T
Emissivity-dependent regime
k+∞ + eDk+
k+∞
Nu*
Critical ratio
k+∞ = (keff – kcond)/Nu’ksolid
May 20, 2026
Vignoles - Interpore 2026, Nantes
32

## Slide 33: EQUIVALENT CIRCUIT
D
D
Pure conduction fully in //
with radiation : OPEN-CELL medium
When radiation fully dominates (Nu’ > Nu*), the emissivity-dependent part does not contribute any more
c
o
n
d
N
u
'
k
∞
+
k
+
N
u
*
k
+
e
N
u
'
k
G. L. VIGNOLES & A. ORTONA, Int. J. Therm. Sci. (2016), vol. 109, pp. 270–278
May 20, 2026
Vignoles - Interpore 2026, Nantes
33

## Slide 34: FIBROUS PREFORM
May 20, 2026
Vignoles - Interpore 2026, Nantes
34

## Slide 35: FIBROUS PREFORM
May 20, 2026
Vignoles - Interpore 2026, Nantes
35

## Slide 36: FIBROUS PREFORM
May 20, 2026
Vignoles - Interpore 2026, Nantes
36

## Slide 37: FIBROUS PREFORM
Large decrease
of anisotropy
when going from
low T (conduction)
to high T
(radiation)
Isotropic, again !
Much more
than foams (~0.4) !!
May 20, 2026
Vignoles - Interpore 2026, Nantes
37

## Slide 38: COMPARISON WITH EXP. DATA
Chart: Temperature (K)
| 300 | 400 | 500 | 600 | 700 | 800 | 900 | 1000 | 1100 | 1200 | 1300 | 1400 | 1500 | 1600 | 1700 | 1800 | 1900 | 2000 | 2100 | 2200
Computed - Slowest | 0.12978 | 0.13163 | 0.13343 | 0.13611 | 0.13986 | 0.14485 | 0.15125 | 0.15925 | 0.16902 | 0.18073 | 0.19457 | 0.21071 | 0.22933 | 0.2506 | 0.27471 | 0.30182 | 0.33212 | 0.36578 | 0.40298 | 0.44389
Computed - Mid | 0.23928 | 0.24155 | 0.24375 | 0.24703 | 0.25161 | 0.2577 | 0.26552 | 0.27529 | 0.28722 | 0.30153 | 0.31844 | 0.33815 | 0.3609 | 0.38688 | 0.41633 | 0.44945 | 0.48646 | 0.52758 | 0.57302 | 0.623
Computed - Fastest | 0.46306 | 0.4659 | 0.46866 | 0.47277 | 0.47851 | 0.48615 | 0.49596 | 0.50821 | 0.52317 | 0.54111 | 0.56231 | 0.58703 | 0.61555 | 0.64814 | 0.68506 | 0.72659 | 0.773 | 0.82456 | 0.88154 | 0.94422
Data published by Mersen on
Calcarb CBCF 15-2000
May 20, 2026
Vignoles - Interpore 2026, Nantes
38

## Slide 39: SEMI-TRANSPARENT MEDIA
Evolution with Kn is as predicted by a simple law:
Chart: 
| 1E-4 | 1E-3 | 0.01 | 0.03 | 0.1 | 0.3 | 1 | 10 | 100 | 1000
Data (ε = 0.1) | 8.6092e-06 | 6.3827e-05 | 0.00052461 | 0.0013638 | 0.0043755 | 0.011165 | 0.024143 | 0.042208 | 0.047905 | 0.047905
Analytical approximation | 3.6631e-06 | 8.0712e-06 | 5.2108e-05 | 0.00048816 | 0.0014299 | 0.0044562 | 0.011307 | 0.024495 | 0.044534 | 0.048502 | 0.048938
Transparent medium limit | 0.048938 | 0.048938 | 0.048938 | 0.048938
Pure conduction limit | 3.1733e-06 | 3.1733e-06 | 3.1733e-06 | 3.1733e-06
« Brownian » walk in the solid, « kinetic » walk in the voids
May 20, 2026
Vignoles - Interpore 2026, Nantes
39

## Slide 40: HYBRID RANDOM WALKS: SUMMARY
Numerical tool
Fast convergence to effective behavior (although detailed field is not converged)
Effective conducto-radiative conductivity described with few dimensionless parameters
Nonlinearity successfully introduced (see talk by Penazzi et al.)
Perspectives
Study semi-transparent media, e.g. ox/ox CMCs
Development of other numerical methods (« moments » methods)
May 20, 2026
Vignoles - Interpore 2026, Nantes
40

## Slide 41: CONCLUSION
Summary
Outlook
May 20, 2026
Vignoles - Interpore 2026, Nantes
41

## Slide 42: MAIN RESULTS
Monte-Carlo Random Walks are well adapted to image-based modeling :
Effective gas diffusivity in rarefied regime
Ablation simulations (also, infiltration)
Effective conducto-radiative heat conductivity
Applications relevant to space technology problems :
Ablation
Thermal protection systems modeling
… but also Chemical Vapor Infiltration
May 20, 2026
Vignoles - Interpore 2026, Nantes
42

## Slide 43: PROS & CONS OF MC/RW METHODS
Low memory requirements
Easily parallelizable
Easy handling of non-standard boundary conditions
Fast « pre-convergence » to effective properties
PROS
CONS
Actual convergence rate is only N-1/2
Some physical problems are more difficult to « translate » into MC/RW
May 20, 2026
Vignoles - Interpore 2026, Nantes
43

## Slide 44: OUTLOOK
It has been proved that a Brownian walk can be replaced by a more efficient « kinetic-like » walk*
Modified solver for ablation
 Modified solver for CVI
 Modified solver for conducto-radiative media
Possibility to address convective flow
Specific algorithm to solve Stokes’ equation and get the velocity field
Then, convection is easy to include in the algorithm
Rewrite solvers in unstructured meshes
Still more projects on Chemical Vapor Infiltration
Incorporation of thermal gradients
* Poëtte, G., De La Vauvre, A., Vignoles, G., Int. J. Heat Mass Transf. 239 (2025) 126603
May 20, 2026
Vignoles - Interpore 2026, Nantes
44

## Slide 45: ACKNOWLEDGEMENTS
Masters interns
  I. Szelengowicz
  X. Lamboley
  A. De la Vauvre
  T. Jeanneau
Funding
May 20, 2026
Vignoles - Interpore 2026, Nantes
45
Collaboration
  A. Turchi, VKI, Brussels
  R. Bianchi, U. La Sapienza Roma
  G. Poëtte, CEA/DAM/CESTA

## Slide 46: THANK YOU! QUESTIONS ?
Gérard L. VIGNOLES vinhola@lcts.u-bordeaux.fr https://lcts.cnrs.fr