## Slide 1
Micro-CT-Based Permeability Characterization of Virgin and Pyrolyzed Wood
21/05/2026
Presented by:
Supervisors / co-authors:
InterPore2026 - MS18
High-temperature heat and mass transfer within porous materials for energy and space
Univ. Bordeaux · I2M
Azita Ahmadi Senichault, Abdelaziz Omari, Cécile Gaborieau, Flora Lahouze, Shaolin Liu, Olivier Caty, Andrew King and Jean Lachaud
Abderrahman M'jikou

## Slide 2
Introduction
InterPore2026 - MS18

## Slide 3
InterPore2026 - MS18
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
Why permeability matters during pyrolysis
Pyrolysis
Thermochemical degradation of organic materials under heat in oxygen-free conditions.
Main products
Gases: (CO2/CO/H2/CH4/....)
Solid: char
Liquids: bio-oil / tar
Main objective
Quantify how pyrolysis modifies the anisotropic permeability tensor of wood from real micro-CT pore geometries.
Main effects
Outgassing / blowing pressure build-up
Microstructure change: porosity and permeability evolve
Deformation: shrinkage, cracking
[1] Scandelli, H. "Multi-Scale Modeling of Wood Shrinkage During Pyrolysis," Arts et Métiers Institute of Technology. Unpublished.
[1]

## Slide 4
From micro-CT to permeability
InterPore2026 - MS18

## Slide 5
InterPore2026 - MS18
Image-based permeability workflow
Approach
Apply the same image-based workflow to virgin and pyrolyzed microstructures to isolate the effect of pyrolysis on permeability.
Micro-CT
imaging
In-situ
pyrolysis
Deep-learning
segmentation
Adaptive
meshing
CFD
simulation
Output
Full anisotropic permeability tensor for virgin and pyrolyzed maritime pine earlywood.
0.30 µm voxel size
synchrotron micro-CT
N₂ atmosphere,
up to 525 °C
Three-plane U-Net +
majority vote
Adaptive voxel–hex
mesh
Creeping-flow
simulations in L, R, T

## Slide 6
InterPore2026 - MS18
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
In-situ pyrolysis and synchrotron micro-CT imaging
Controlled in-situ pyrolysis [2]
Input for simulations
Micro-CT volumes before / after pyrolysis
Reconstructed 3D volumes provide the real pore geometries used for segmentation, meshing, and pore-scale flow simulations.
Material:
Pinus pinaster earlywood
Heating:
IR lamps
Peak temperature:
525 °C
Atmosphere:
N2 purge
Beamline:
SOLEIL PSICHÉ
Dataset virgin:
2928 × 3144 × 2048
Dataset pyrolyzed:
2332 × 2160 × 2048
Voxel size:
0.30 µm
Longitudinal plane (L)
Radial plane (R)
Tangential plane (T)
Virgin wood
Pyrolyzed wood
Longitudinal plane (L)
Radial plane (R)
Tangential plane (T)
[2] F. Lahouze, Development of a pyromechanical model applied to biomass pyrolysis, PhD thesis in mechanics, University of Bordeaux, Bordeaux, France, defended on October 24, 2025 (2025)

## Slide 7
InterPore2026 - MS18
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
Deep-learning based segmentation of the pore space
Segmentation challenge
Segmentation output
Three-plane U-Net strategy
Majority-vote fusion provides an orientation-robust 3D pore/solid geometry for permeability simulations.
Low contrast:
solid/pore gray levels overlap
Anisotropic structure:
features depend on slice orientation
Thresholding insufficient:
artifacts and wall-
intensity gradients
2. Predict the full 3D volume with each model
3. Fuse predictions by majority vote
1. Train one 2D U-Net per anatomical plane (L, T, R)
Majority-vote ensemble segmentation

## Slide 8
InterPore2026 - MS18
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
Segmentation results and microstructural changes
Segmentation consistency
Final 3D pore/solid geometry
Virgin wood
Pyrolyzed wood
Final segmentation preserves pore/wall continuity across anatomical views.
Matched virgin and pyrolyzed geometries used for pore-scale simulations.
Segmentation consistency:
Final masks are coherent across L, T, and R views.
Matched 3D geometries:
Virgin and pyrolyzed volumes represent comparable earlywood regions.
Microstructural changes:
Pyrolysis induces compaction, wall roughening, and modified connectivity.

## Slide 9
InterPore2026 - MS18
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
Pore-scale meshing and flow simulations
Adaptive voxel-hex meshing
Permeability evaluation
Creeping-flow CFD setup
Directional permeabilities are extracted from the volume-averaged velocity and pressure gradient.
Flow
directions
L, R, T
Boundary condition
no-slip walls + inlet/outlet padding
Solver
OpenFOAM
simpleFoam
Pore-interior coarsening
large cells away from walls
Purpose
preserve geometry at lower cost
Near-wall resolution
0.30 µm at the solid-fluid interface
Output:

## Slide 10
InterPore2026 - MS18
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
Numerical reliability: mesh, padding and REV
Mesh convergence
Final settings for permeability simulations
Padding-size convergence
Adaptive voxel-hex mesh + 24 µm padding + 390 µm REV cube
Coarsening factor
Near-wall refinement
Adaptive mesh parameters selected from sensitivity analysis
Permeability-based REV
Selected padding
24 µm inlet / outlet
Permeability variation
≤ 5%
Selected REV
390 µm cube
Accuracy-cost compromise for all final cases.
Boundary effects become negligible after the plateau.
Directional permeabilities stabilize with increasing cube size.

## Slide 11
Results & discussion
InterPore2026 - MS18

## Slide 12
InterPore2026 - MS18
Pyrolysis strongly modifies the permeability tensor
Matched earlywood REVs: same anatomical region, same cube size (390 µm), before and after pyrolysis.
Anisotropy is strongly reduced
Pyrolysis redistributes transport pathways instead of uniformly increasing permeability.
Directional permeability
Directional changes
-47%
-24%
×5.86
Longitudinal
Radial
Tangential
Decrease
Decrease
Increase



: 361  250
: 7060  636
: 19.6  2.55

## Slide 13
InterPore2026 - MS18
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
Why does permeability change after pyrolysis?
Microstructure evolves non-uniformly
Interpretation
Flow paths reorganize by direction
Pyrolysis redistributes pore constrictions and transverse connectivity rather than uniformly increasing permeability.
R: limited transverse links reduce
T: improved connectivity explains × 5.86
L: aligned paths remain, but constrictions reduce
Porosity
76.9%  78.3%
Median
Porosity increases slightly, but pore openings shift toward smaller values
Virgin wood
Pyrolyzed wood
Local pore-opening thickness distribution

## Slide 14
Conclusions
InterPore2026 - MS18

## Slide 15
InterPore2026 - MS18
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
Conclusions
1. Image-based workflow
Implication
2. Anisotropic changes
Pyrolysis-induced permeability evolution must be treated as anisotropic and microstructure-dependent, not as a uniform scalar increase.
Permeability tensor extraction from real 3D geometries
Micro-CT  segmentation 
meshing  CFD
3. Mechanism
Porosity alone does not explain the transport evolution.
-47%
-24%
×5.86
Longitudinal
Radial
Tangential
Decrease
Decrease
Increase
Output:
Constrictions
smaller local openings limit flow
Connectivity
transverse pathways are redistributed

## Slide 16
Thank you for your attention
InterPore2026 - MS18

## Slide 17
Backup slides
InterPore2026 - MS18

## Slide 18
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
Microscale vs macroscale description
Pore-scale (micro) description
Resolve the complex pore geometry and solid/gas interface.
Solve full conservation laws in each phase (mass, momentum, energy, species).
Too expensive for realistic geometries.
Macro-scale (engineering) description
Use averaged fields (porosity, pressure, temperature, velocity).
Requires closure laws (e.g., permeability, interfacial transfer, momentum model).
Compute at the scale of the sample / reactor.
Homogenize
InterPore2026 - MS18

## Slide 19
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
From micro to macro: Volume Averaging
[1]
[1]: Scandelli, H. "Multi-Scale Modeling of Wood Shrinkage During Pyrolysis," Arts et Métiers Institute of Technology. Unpublished.
Idea
Average microscopic conservation equations over a Representative Elementary Volume (REV).
Obtain macroscopic equations with additional terms (dispersion, interfacial source terms, closure parameters).
Requires a scale-separation assumption:
lβ: characteristic length of phase β
lσ: characteristic length of phase σ
r: REV size (radius/length)
InterPore2026 - MS18

## Slide 20
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
Current macroscopic momentum model: Darcy's law
Darcy's law
Typical validity assumptions
Creeping flow (Re << 1), negligible inertia
Rigid porous skeleton, fixed interface
Continuum no-slip valid (Kn << 1)
No mass injection at the solid/gas interface
Steady state
Incompressible flow
In many pyrolysis models, gas momentum conservation in the porous medium is modeled with:
Pyrolysis-specific physics
Mass exchange at the solid/gas interface: non-zero normal gas velocity (blowing).
Non-rigid porous medium: evolving pores and moving interfaces.
Possible Re >1 locally: inertia corrections may matter.
Compressible and unsteady flow under strong heating and gas release.
Potential slip-flow effects in small pores (rarefaction effects)
InterPore2026 - MS18

## Slide 21
Pore-scale problem
Volume averaging
Darcy's law
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
Numerical procedure for evaluating permeability tensor
Pore scale
InterPore2026 - MS18

## Slide 22
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
Creeping-flow verification and pore-thickness statistics
For and the Reynolds number is equal to
Virgin wood
Pyrolyzed wood
InterPore2026 - MS18

## Slide 23
Coarsening factor
Near-wall refinement threshold
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
Mesh convergence Tables
InterPore2026 - MS18

## Slide 24
Comparison with literature
Directional Knudsen number
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
Comparison with the literature and directional Knudsen number
InterPore2026 - MS18

## Slide 25
Wood orthotropic directions
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
Wood Main-orthotropic directions
InterPore2026 - MS18
[3]
[3] Royuela, José Luis & Majano-Majano, Almudena & Lara-Bocanegra, Antonio José & Xavier, José & De Moura, Marcelo. (2022). Evaluation of R -curves and cohesive law in mode I of European beech. Theoretical and Applied Fracture Mechanics. 118. 103220. 10.1016/j.tafmec.2021.103220.

## Slide 26
U-Net training settings
Work package 4 : Volume-averaged mathematical models
Work package 4 : Volume-averaged mathematical models
U-Net model training parameters
InterPore2026 - MS18