## Slide 1: Multi-Physical Transport in Porous Media for Energy Applications
Prof. Sophia Haussener
Laboratory of Renewable Energy Science and Engineering Ecole Polytechnique Fédérale de Lausanne

## Slide 2: Porous Media in Energy Application
Photoelectrochemical Hydrogen Generation
Electrochemical CO2 Reduction
Solar Thermochemical Syngas Generation
Thermal Energy Storage

## Slide 3: Photoelectrochemical Fuel Generation
Initial idea and functional decoupling:
Challenges: Complex transient multi-physics and multi-scale problem
Component integration for practical devices
Implementation via porous photoelectrodes
photoabsorber
2H+ + 2e- → H2
H2O + 2h+ → 2H+ + 1/2O2
electrolyte
photocatalyst
photoabsorber II
h+
e-
H+
catalyst
protecting layer
separator
First demonstration:
Fujishima et al., Nature, 238, 1972.

## Slide 4: “Standard” Methodology
~1 cm
Physical sample
3D imaging (e.g tomography)
Image processing and structure digitalization
12 μm
8.5 μm
14.5 μm
Morphological characterization
Pore-scale simulations
Notes: The workflow starts with a physical sample, here some bismuth oxide deposited on a GDL for CO2 reduction. After the appropriate sample preparation the exact 3D structure is acquired trough a tomography technique and an image processing procedure allows to obtain a digitalized 3D structure. The structure then undergoes in depth morphological characterization; subsequently it can be meshed and used in pore-scale simulations.

## Slide 5: Photoelectrochemical Fuel Generation
Initial idea and functional decoupling:
Challenges: Complex transient multi-physics and multi-scale problem
Component integration for practical devices
Implementation via porous photoelectrodes
photoabsorber
2H+ + 2e- → H2
H2O + 2h+ → 2H+ + 1/2O2
electrolyte
photocatalyst
photoabsorber II
h+
e-
H+
catalyst
protecting layer
separator
First demonstration:
Fujishima et al., Nature, 238, 1972.
Challenge: structural details require nm resolution

## Slide 6: FIB-SEM Nanotomography
Zeiss NVision 40: e-beam: ZEISS Gemini, 1-30kV, 1nm@30kV, 2.5nm@1 kV, (1.7 kV, 1 nA)
Ion-beam: 1-30kV, 4nm@30kV, (30 kV, 300 pA)
EDS X-MAX (SDD) 80mm2 detector
Cantoni et al. (2014)
Our sample

## Slide 7: LaTiO2N
31.48 μm
Suter, Cantoni, Gaudy, Pokrant, Haussener, Sustainable Energy & Fuels, doi: 10.1039/C8SE00215K, 2018
LaTiO2N (photoanode, 2.1 eV bandgap)
Silvan Suter
Notes: 7.5 um thick, electrophoretic deposition of LTON particles on FTO, followed by a dip coating step resulting in particle necking with TiO2
Photoanode, 2.1 eV, n-type

## Slide 8: Quantification of the Film
Correlation functions (Monte Carlo), morphology operations
Solid volume fraction Specific surface
without nano-pores
-40%
-60%
with nano-pores that are
connected to void
Numerical: 3.2 m2/g; Experimental (BET): 14.2 m2/g
(Landmann et al., ChemSusChem, 2015)
Suter, Cantoni, Gaudy, Pokrant, Haussener, Sustainable Energy & Fuels, doi: 10.1039/C8SE00215K, 2018
Nanopores
Inner porosity = 10 %
34.1 % of pore that pore space is connected to the electrolyte
Notes: Density: LTON=6.18·10-12 g/µm3
Pokrant et al. [12] correlated specific crystallographic planes with LTON particle faces

## Slide 9: Transport Characterization
Microscopic:
Finite volume simulation
Macroscopic:
Empirical correlation
ci
Charge generation rates:
Species concentration / current density:
1 order of magnitude
variation in current density
Suter, Cantoni, Gaudy, Pokrant, Haussener, Sustainable Energy & Fuels, doi: 10.1039/C8SE00215K, 2018
Mass transport significantly affects local reaction environment and can lead to large heterogeneities

## Slide 10: Porous Media in Energy Application
Photoelectrochemical Hydrogen Generation
Electrochemical CO2 Reduction
Solar Thermochemical Syngas Generation
Thermal Energy Storage

## Slide 11: Electrochemical CO2 Reduction
Processes that typically operate at more moderate conditions
Utilization of CO2 can help to close the carbon cycle
SunCat@Stanford

## Slide 12: Device Designs
From low to high current-density operation – towards more practical systems:
Bui et al., Chemical Reviews, 2022
Norwegian Hydrogen
Notes: Solubility: 4mg/l
Left: more relevant for fundamental studies, although condition might be irrelevant (low current density)

## Slide 13: Electrochemical CO2 Reduction
Multi-physics, multi-phase, multi-component, multi-scale, multi-dimensional
Stephens et al., Journal of Physics: Energy, 10.1088/2515-7655/ac7823, 2022

## Slide 14: Pore-Scale Modeling of GDE Design
Reaction environment in more realistic CO2 electroreduction design configuration
CO2
CO, H2
OH-
e-
Electrolyte
Anode (OER)
Cathode
“Gas Diffusion Electrode”
Porous Catalyst
CO, H2
CO2
Evan Johnson
Johnson et al., EES Catalysis, 10.1039/D3EY00122A, 2023

## Slide 15: Model Details
Liquid-Gas interface:
Molar fluxes conserved (Jliq = Jgas)
Gas solubility: Henry’s constant (Ci,liq = Hi ·pgas)
Where (Sechenov relation)
  Higher local electrolyte concentration  lower solubility
“Generalized Modified Poisson-Nernst-Planck” (PNP + steric effects term) (K+, HCO3-, CO32-, H+, OH-, CO2, CO, H₂)
Multicomponent diffusion + porous fluid flow
(CO2, CO, H₂)
Catalyst Surface: Mass-weighted Tafel relation
at catalyst surface
Notes: Mixture averaged diffusion model

## Slide 16: Model Configurations - Results
@-1.1V vs. RHE

## Slide 17: Results on Catalyst Particle Scale
Applied potential (V vs. RHE)
“Triple-Phase Region”: active for CO2 reduction within ~1 μm of liquid-gas interface
“Particle” iCO (current density based on particle surface)
Johnson et al., EES Catalysis, 10.1039/D3EY00122A, 2023
Notes: Current density vs. Particle area (not geometric area)
At higher applied potential: more OH-, les solubility and more parasitic reactions

## Slide 18
3.6 μm
800 nm
3 μm
2 μm
2 μm
Examples of Catalyst Layers for CO2RR
DTU-Cu: Cu sputtered on GDL
Ubern-Bi2O3: Bi2O3 particles airbrush deposited on GDL
Ubern-Ag: Ag nanowires airbrush deposited on GDL
TUDelft-Cu: Cu sputtered on GDL
TUBerlin-PyrMOF: Pyrolyzed Ni-based MOF deposited on GDL
Meso-structural properties: Porosity, specific surface, size distributions, etc.
Effective transport properties: Effective diffusivity, permeability, effective ionic and
electronic conductivities, etc.
Lorenzutti et al., JECS, 10.1149/1945-7111/acff1c, 2023

## Slide 19: Effects of CL Mesostructure in Homogenized Model
Different Catalyst Layer Morphology
Venu Agarwal
Agarwal et al., Chem Com, 10.1038/s42004-024-01122-5, 2024

## Slide 20: Pore-Resolved Information
Lorenzutti et al., in preparation, 2026
Francesca Lorenzutti
Multi-physical simulations on pore level possible and reveal flooding-condition dependent heterogeneity

## Slide 21: Porous Media in Energy Application
Photoelectrochemical Hydrogen Generation
Electrochemical CO2 Reduction
Solar Thermochemical Syngas Generation
Thermal Energy Storage

## Slide 22: Solar Thermochemistry
World-record reactor from ETH Zürich
Tailor morphology for enhanced performance?
window
insulation
compound
parabolic
concentrator
H2O/CO2
N2
O2+N2
H2+CO
Microporous
monolith
Felt
Foam
Solar-to-fuel
efficiency:
0.4%
0.2%
1.7%

## Slide 23: Multi-Physics Model
1D model, with focus on multi-scale porous structure
Homogeneous media
Xiaoyu Dai
Dai et al., Journal of Solar Energy Engineering, 2022
Use tomography-based direct pore-level simulations of transport in porous structure to obtain effective transport properites

## Slide 24: Structural Drivers for Porous Media?
Morphological descriptors
Direct pore-level simulation (DPLS)
Continuum-level simulation
Fuel production
Effective transport properties
Machine Learning
Fuel production
Fuel production
Machine Learning
Morphological descriptors
reduced input information size
decreased computation steps
(DPLS)
Dai, PhD thesis, EPFL, 2022

## Slide 25: Machine Learning in Solar Thermochemistry
Random porous structure generation
Morphological characterization
Correlation functions
Pore size distribution
Geodesic tortuosity
Direct pore-level simulation
Conduction
Convection
Radiation
Continuum-level simulation
Multi-layer perceptron regression
Fuel production
Random noise + Gaussian filter
The random structure is isotropic
200 x 200 x 200 voxels
10 x 10 x 10 mm3
Dai, PhD thesis, EPFL, 2022

## Slide 26: Structural Drivers
Mean absolute percentage error (MAPE):
Integral O2 production under identical operation condition:
  Sun concentration ratio = 750 [-]
  O2 partial pressure = 10-5 [-]
  Reduction duration t = 600 [s]
Porosity and surface area not the morphological descriptors for performance
Dai, PhD thesis, EPFL, 2022

## Slide 27
Uniform porosity distribution
Non-uniform porosity distributions
P-1 radiation model:
Energy conservation:
Non-local thermal equilibrium
Solid:
Species conservation:
Mass conservation:
Momentum conservation:
Fluid:
Dai et al., in revision, 2021
Towards Non-Uniform Porous Media

## Slide 28: Effect Porous Media Inhomogeneity
7 times increase in fuel production is observed in f2.
Dai et al., Journal of Solar Energy Engineering, 2022

## Slide 29: Porous Media in Energy Application
Photoelectrochemical Hydrogen Generation
Electrochemical CO2 Reduction
Solar Thermochemical Syngas Generation
Thermal Energy Storage

## Slide 30: Thermal Energy Storage
Heat demand is large:
  Global final energy demand How to store:
Karyappa et al. Energy Mater., 10.20517/energymater.2024.149, 2025

## Slide 31: Typical Storage Design – Latent Heat
Charging
Discharging
Latent
Sensible
Sensible
Temperature
Stored Thermal Energy
Phase Change Material (PCM)
Heat Transfer Fluid (HTF)
Insulation
Encapsulation
Al87.4Si12.6
Al68.5Cu26.5Si5
Air
Stainless steel
Want fast (dis)charging, low pressure loss, high energy capacity, high power density, long discharge time at constant temperature
Notes: One type is latent
Heat battery – stores heat as latent heat during solid-liquid phase change – melting is charging and solidification is discharging
Popular method is encapsulating the PCM – pass hot or cold HTF over it to charge or discharge
In this thesis – Al alloys as PCM …

## Slide 32: Using AI to Support Design - Method
Output scalars:
  Melt time
  Normalized melt time
  Pressure drop
Volume fields:
  Temperature
  Pressure
  Velocity
Surface fields:
  Heat flux
  Shear stress
1163
Random structures
Ordered structures
68
Mallya et al., Journal Heat & Mass Transfer, 10.1115/1.4056663, 2023
Notes: Artificially generate random and ordered structures – unit cells - replicated on the 4 sides
Image with randomly created pixels - Skeletal structure of the arrangement
Convert to image stacks – random gaussian filters – spheres of required strut diameter
Make solid STLs – remove disconnected regions
Mesh - 3D CFD + phase change simulations
Output scalars
Larger structures take longer time to melt – normalize it using 1-porosity
Delta P – larger pressure drops require more expensive pumps

## Slide 33: “Best” Structure
Characterization:
Train set: 90%
Test set: 10%
Mallya et al., Journal Heat & Mass Transfer, 10.1115/1.4056663, 2023
Notes: Plot the two output scalars against each other
Example structures
Pareto front – ordered performing better
One reason – generation method used does not create highly porous random structures with large surface area

## Slide 34: Geodesic Convolutional Neural Network (GCNN)
Mallya et al., Journal Heat & Mass Transfer, 10.1115/1.4056663, 2023
Notes: GCNN – geodesic because we use geometries
Convolutional neural network on the volume mesh
on the surface mesh
Mean pooling – ANN to predict the scalars
Disentangling property – improves prediction by adding thing to predict that are correlated to the scalars

## Slide 35: GCNN Can Act as CFD Emulator
With this emulator, optimized pore-scale engineering will now be possible
Mallya et al., Journal Heat & Mass Transfer, 10.1115/1.4056663, 2023
Notes: We have ground truth and prediction and error between them
Temperature volume field and heat flux surface field
Same for pressure and velocity and shear stress
An additional benefit is that the GCNN acts as a replacement for the 3D CFD simulator – but much faster

## Slide 36: Acknowledgements
sophia.haussener@epfl.ch
http://lrese.epfl.ch
EPFL: LRESE team
Marco Cantoni
University of Salzburg: Simone Pokrant
TU Delft: Tom Burdyny
NeuralConcept: Pierre Baque, Pascal Fua,
Francois Fleuret
Open PhD and Postoc positions:
Apply now!

## Slide 37: Pore-Level Characterization
Morphology geometrical descriptors:
Dai, PhD thesis, EPFL, 2022

## Slide 38: Effects of CL Mesostructure in Homogenized Model
Different CLs
Non-uniform CLs
Venu Agarwal
Agarwal et al., Chem Com, 10.1038/s42004-024-01122-5, 2024

## Slide 39: Anisotropic Operating Conditions and Porous Media
Optimized (anisotropic) porous media properties deduced numerically:
Parallel:
Perpendicular:
+10%
x2.56
Dai, PhD thesis, EPFL, 2022

## Slide 40: Heat Transfer Limitations
Forced convection to PCM:
  Approach 2: Ceramic fins for increased performance
PCM
Foam
dp = 2.5 mm / 10 PPI foam
without foams
denc = 20-100 mm
Lenc = 200-1000 mm
dp = 1.25, 2.5, 5 mm
Rezaei, Barbato, Ortona, Haussener, Applied Energy, 10.1016/j.apenergy.2019.114330

## Slide 41: Optimization and validation
 | Case 1 |  |  | Case 2 | 
 | [-] | [MJ/m3] |  | [-] | [MJ/m3]
Prediction | 0.890 | 672.1 |  | 0.900 | 280.2
Simulation | 0.903 | 706.0 |  | 0.842 | 268.1
Error (%) | 1.5 | 5.0 |  | 6.4 | 4.3
 | Case 1 |  |  | Case 2 | 
Prediction | 0.890 | 672.1 |  | 0.900 | 280.2
Simulation | 0.903 | 706.0 |  | 0.842 | 268.1
Error (%) | 1.5 | 5.0 |  | 6.4 | 4.3
Notes: We created two metamodels based on the output results and we considered two optimization cases.
Pareto frontier shows the highest performance we can obtain.

## Slide 42: Heat Transfer Limitations
Best structure of porous media?
From the numerical model to the real foam by indirect additive manufacturing
Transport characterization (heat and mass transport):
AM of a polymer
Replica
Silicon infiltration
Pyrolysis
Rezaei, Ortona, Haussener, J. of Heat Transfer, 10.1115/1.4045732

## Slide 43: Transport Limitations in GDE
What is driving down the iCO to form the bell-shaped curve?
Both solubility and parasitic reactions enabled
Neither parasitic reactions or reduction in solubility enabled (optimal)
Turn on parasitic reactions
Turn on solubility reduction (reactions off)
Mostly solubility. Parasitic reactions have lesser effect.
Red line gives optimum, if no OH- builds up at all. Catalyst layer must have ample diffusion pathways to relieve OH- accumulation.
Johnson et al., EES Catalysis, 10.1039/D3EY00122A, 2023

## Slide 44: Calculation procedure
Heat transfer:
Steady state method
Experimental-Numerical
5 points at 75 < Re < 250
Pressure drop:
Experimental
10 points at 40 < Re < 1000
Darcy-Forchheimer equation:
Experiment with chosen mass flow rate and measuring the temperature data
Equivalent numerical model using the initial/calculated value for hv
Compare the outlet temperature in the simulation with experiment
Converged?
yes
New simulation with a new hv
no
hv

## Slide 45: Heat Transfer Limitations
Best structure of porous media?
Heat and mass transport characterization:
Rezaei, Ortona, Haussener, J. of Heat Transfer, 10.1115/1.4045732
Mechanical properties:

## Slide 46: Method – Experiments in extreme conditions
Alumina foam samples, 92.1±0.07% porosity, 316±2.8 kg/m3, 40x40x20mm, typical pore size 0.1 mm
Water-cooled sample holder, high-flux solar simulator, environmental chamber
Notes: Up to 20 MW/m2

## Slide 47: Temperature measurements
Shielded thermocouples
Infra-Red camera FLIR A655sc
  Uncooled microbolometer
  Longwave infrared (LWIR) range (8-14 μm)
  Resolution of 640x480 with 17 μm pixels, frame rate up to 50Hz
  Emissivity of material 0.95
Y(mm)
X(mm)
Mora-Monteros et al., in preparation
Notes: 600K temperature drop over 1.5 cm!
1 MW/m2

## Slide 48: PATO: Material response code based on OpenFOAM
Usually used for carbon-phenolic materials (pyrolysing) adapted to Al2O3 (no pyrolysis)
3D simulations, 1st-order implicit finite-volume schemes in time and space
BCs:
  Mapped T on surface
  Re-radiation and convection on backface and sides
  Fixed cold temperature on edges in contact with sample holder
Typical: 260s computational time on 4 cores (3.6 GHz),
20x50x20 mesh (100 MB RAM)
Edges at 290K
Energy Equation
Mass conservation equation
T
vgas
PATO
Internal energy + advection
Diffusion
Conduction + viscous effects
Mass content + convection
Momentum conservation
Equation of state, ideal gas law
Lachaud et al., IJHMT, 2017

## Slide 49: Effective conductivity
ρs = 316 kg/m3 (de Cavis foams specifications certificate), hback = 1.0 W/m2K (estimated), hsides = 25.0 W/m2K (estimated)
Cp and k of bulk aluminum from literature
Živcová et al., JECS, 2009
Touloukian, Thermophysical Properties, 1967
Mora-Monteros et al., in preparation
Notes: The measured k value is the value measured by deCavis using laser flash.

## Slide 50: Morphology
Tomography and image processing
δ = 0
δ = 4
δ = 8
δ = 12
δ = 0
δ = 8
Akolkar et al., IJHMT, 2011
Alkokar et al, TPM, 2012
Haussener et al., Materials, 2012
ε = 0.87 ε = 0.72 ε = 0.58 ε = 0.42

## Slide 51: Results
Morphological characterization
  Porosity: voxel statistics
  Specific surface area: two-point correlation function
  Pore size distribution: mathematical morphology operations 0.85%
Suter et al., IJHMT, 2014

## Slide 52: Results
Heat transfer:
  Convection: constant solid temperature
Gunn et al., IJHMT, 1978
Kuwahara et al, IJHMT, 2008
Notes: Gunn: experimental fit to packed bed
Kuwahara: simplified, 2D structure and fit to Wakaos model

## Slide 53: Optimization of structure
Various base morphology
ε = 0.84 0.73 0.59 0.45
Suter et al., JOM, 65, 2013

## Slide 54: Optimization of structure
Morphology influence for solar power example application:
DLR
Original foam
Fiber: Solid line
Foam: Dotted line
Shrunk foam: dashed
Suter et al., JOM, 65, 2013
→ Proper numerical optimization with machine learning
Notes: Energy and momentum equations fo rlocal thermoal non-equilibrium, quasi 1D
The fibrous samples reached the maximal absorptance for slab thicknesses of several hundred microns,
and the highest efficiency was achieved for samples with highest porosities as their reflectance were the smallest.
The shrunken foam-like samples reached their maximum efficiencies within the first 100 lm due to the larger extinction coefficients; however, a higher
reflectance for low porosity led to slightly lower maximum values.
Increasing the sample thickness led to a decrease in efficiency because the pressure losses through the slab became significant. The influence of the pump work onto the efficiency of the fibrous samples was less significant but still apparent. In contrast, the original foam-like samples showed no decrease in efficiency with increasing
thickness.
The original foam samples at comparable porosity required larger sample thicknesses to reach the maximal efficiency due to significantly lower extinction coefficients. The maximum efficiency of a fibrous sample and the shrunk foam-like samples was always larger compared to the original foam-like sample with the same porosity mainly due to their larger specific surface area and enhanced convective heat transfer.

## Slide 55: Application 2 – Partially aligned fibers
Anisotropic morphology:
Fiber diameter: 1mm
Computational volume: 183 mm3
Porosity of sample: 0.76
Anisotropy based on MIL:
Fiber diameter: 1mm
Computational volume: 183 mm3
Porosity of sample: 0.86
Anisotropy based on MIL:
x
z
y

## Slide 56: Application 2 – Partially aligned fibers
Continuum-scale radiative properties assuming anisotropic medium:
Less strong peaks

## Slide 57: Innovation in Application: Global South
Fredy Nandjou
Fridolin Tchouante
Matthieu Jonin
Unpublished
Stefan Troendle

## Slide 58: Model
Well studied catalytic hydrogen combustion chemistry mechanisms over different supports (Pt, Ru, Pd, Ni, …)
  We implemented different multi-steps mechanisms, but computational burden increases
  Simple step mechanisms (second order in O2 and H2) wins
Model
Chemistry: Single step heterogenous and homogeneous with rate constants
Porous media: Brinkman equation with Forchheimer correction
Species conservation: Fickian diffusion with Smidt number for temperature deviation
Turbulent flow
GRI-mech 3 and NASA for species transport and constitutive properties
Solved in Comsol

## Slide 59
560°C auto-ignition temperature
The more PPI, the hotter and the more radiative power, but the more likely to flashback due to back conduction in the porous medium and in side walls
More volume radiates more and have less convective loss due to enhanced porous conduction
560°C
30PPI
50PPI
80PPI
Simulation results : Hydrogen combustion – porous PPI

## Slide 60
SiC
Al2O3
SS
490 [W/(m*K)]
45 [W/(m*K)]
27 [W/(m*K)]
Flashback is delayed with lower conductivity
  Conductivity value to reach spatial steady state of «flame front» ?
Simulation results : Hydrogen combustion – time resolved flashback

## Slide 61
Simulation results : Hydrogen combustion – porous thickness
Parameters:
Vitroceramics cover
Insulated side
SiC porous material
1.5kW power
Increase of porous depth
  Reduction of overall temperature and
  Reduction of useful heat
2 cm
3 cm
4 cm
5 cm
Porous thickness
(cm) | (kW) | (degC) | (%) | (%) | (%) | (%) | (degC) | (%) | (%)
2.0000 | 0.78723 | 628.26 | 23.072 | 29.028 | 54.215 | 13.379 | 371.03 | 19.534 | 10.167
 | 1.5807 | 724.12 | 15.264 | 19.108 | 56.541 | 7.9053 | 446.77 | 14.170 | 8.0433
3.0000 | 0.78727 | 618.59 | 19.345 | 22.260 | 57.223 | 18.080 | 371.23 | 19.427 | 10.108
 | 1.5804 | 686.71 | 13.232 | 16.299 | 61.104 | 10.788 | 422.69 | 12.592 | 7.0047
4.0000 | 0.78748 | 597.45 | 17.741 | 20.552 | 57.012 | 22.126 | 355.26 | 17.577 | 9.1829
 | 1.5808 | 648.12 | 10.368 | 12.421 | 64.369 | 12.704 | 413.28 | 12.255 | 6.5655
5.0000 | 0.79065 | 664.44 | 16.295 | 18.904 | 55.196 | 25.592 | 343.43 | 16.990 | 8.5390
 | 1.5873 | 609.03 | 6.7238 | 6.9355 | 65.452 | 13.566 | 387.66 | 10.669 | 5.6469
2.0000 | 0.78723 | 628.26 | 23.072 | 29.028 | 54.215 | 13.379 | 371.03 | 19.534 | 10.167
 | 1.5807 | 724.12 | 15.264 | 19.108 | 56.541 | 7.9053 | 446.77 | 14.170 | 8.0433
3.0000 | 0.78727 | 618.59 | 19.345 | 22.260 | 57.223 | 18.080 | 371.23 | 19.427 | 10.108
 | 1.5804 | 686.71 | 13.232 | 16.299 | 61.104 | 10.788 | 422.69 | 12.592 | 7.0047
4.0000 | 0.78748 | 597.45 | 17.741 | 20.552 | 57.012 | 22.126 | 355.26 | 17.577 | 9.1829
 | 1.5808 | 648.12 | 10.368 | 12.421 | 64.369 | 12.704 | 413.28 | 12.255 | 6.5655
5.0000 | 0.79065 | 664.44 | 16.295 | 18.904 | 55.196 | 25.592 | 343.43 | 16.990 | 8.5390
 | 1.5873 | 609.03 | 6.7238 | 6.9355 | 65.452 | 13.566 | 387.66 | 10.669 | 5.6469

## Slide 62
Cases
  CO2 reduction
  Photoelectrochemical water splitting
  Solar thermochemical
  Thermal storage
  Hydrogen combustion
  Inverse property determination