## Slide 1: Designing the nanoremediation of contaminated aquifers: from laboratory tests to field implementation
Tiziana Tosco, Rajandrea Sethi & Groundwater Engineering Group
Department of Environment, Land and Infrastructure Engineering (DIATI)
Politecnico di Torino
Nantes, 22nd May 2026

## Slide 2: Nanoremediation
Subsurface injection of reactive micro- or nanomaterials for in-situ removal of contaminants:
Ability to treat secondary sources of contamination or create a PRB for plume treatment.
Flexibility and higher depths compared to PRBs
Wide spectrum of reactive materials
Does not impact site activities
Carbo Iron
FeOx
nZVI
mZVI

## Slide 3: Main ingredients for a successful nanoremediation project
Subsurface delivery
Environmental compatibility
Reactivity against pollutants
Use of reactive nanomaterials and additives having low environmental impact
Small size  High SSA  faster degradation kinetics
Surface modification tunes nZVI/mZVI reactivity
Targeted injection to form a controlled reactive zone

## Slide 4: Main ingredients for a successful nanoremediation project
Subsurface delivery
Environmental compatibility
Reactivity against pollutants
Targeted injection to form a controlled reactive zone

## Slide 5: Optimizing delivery using permeation injection
Poorly stable particles
low mobility
minimal ROI
 Need: improve stability
Very stable particles
- high mobility
- poorly controlled migration
 Need: control stability
nZVI
FeOx
mZVI
Colloidal stability directly affects injection and mobility
Colloidal stability must be controlled and tuned to achieve the desired mobility
Modeling tools to simulate particle transport and PM clogging are needed to design field-scale injection based on lab-scale data

## Slide 6: Nanoparticle transport in porous media: modeling across scales
    Pore-scale
    µCT
    Laboratory
    Column tests, flumes…
    Large-scale lab & Field

## Slide 7: Integrated experimental and modelling approach
Column injection tests
x N
BTC fitting
Site-specific colloid transport parameters
Pilot simulations
Field-scale simulations
Bianco et al. (2016). Journal of Contaminant Hydrology 193, pp. 10-20

## Slide 8: MNMs/MNM3D: modeling approach
Particle transport in saturated porous media
Polymer transport
Porous medium clogging
Fluid rheology
Linear deposition
Straining
Blocking
Ripening
Particle transport mechanisms
Dependendance of attachment/detachment on fluid properties
  Tosco et al. (2014) Journal of Contaminant Hydrology 166, 34-51

## Slide 9: Optimizing delivery using permeation injection
Poorly stable particles
low mobility
minimal ROI
 Need: improve stability
Very stable particles
- high mobility
- poorly controlled migration
 Need: control stability
nZVI
FeOx
mZVI

## Slide 10: Case study 1 - validation of the integrated experimental-modeling approach
Target: validate the up-scaling approach from column tests to radial injection modeling
Reference problem: permeation injection of mZVI in wells
Column tests run at different injection rates to obtain velocity-dependent particle transport parameters
Column tests
Radial lab-scale test
Validation of radial simulations against experimental data

## Slide 11: Case study 1 - injected mZVI suspension
mZVI slurry
  Particles: Superfine Iron Powder (Sagwell, Cina), d10 – d90 = 1.13 – 4.2 μm
  Concentration: C0 = 20 g/L
  Fluid: Polymeric biodegradable gel  XG+GG 1.75 g/L (shear thinning)
High viscosity at low shear rate
↓
Reduced sedimentation
& aggregation
Low viscosity at high shear rate
↓
Easily injected

## Slide 12: Case study 1 - experimental setup
  Column tests setup
  Geometry: column length: 40 cm, column diameter: 2.4 cm
  Porous medium: silica sand, d50 = 0.28 mm
  Monitored parameters:
  Concentration at column inlet and outlet (continuous)
  Concentration profile at different times
  Pressure build-up (continuous)
  Radial injection setup
  Geometry: R = 90 cm, H = 4 cm, f = 60°
  Monitored parameters:
  Photographic imaging (continuous)
  Injection pressure (continuous)
  Final particle distribution

## Slide 13: Case study 1 - column test results and modeling
Breakthrough curves
Concentration profiles
Pressure buildup
Modeled particle transport mechanisms: 2 interaction sites, blocking + straining
Trasport parameters depedent on fluid viscosity and flow velocity
(-)
0.6
0.4
0.2
0
(s-1)
0.00 0.01 0.02 0.03 0.04
(s-1)
, (s-1)
0.00 0.01 0.02 0.03 0.04
6x10-3
4x10-3
2x10-3
0

## Slide 14: Case study 1 - radial injection (tracer test)
  Bromophenol blue injection (C0 = 50 mg/L)
  Pre-flushing (water)
  Tracer solution: 6 l
  Flushing (water): 6 l
  Qradial= 7 L/h  Qwell =1 m3/h/m
  Comparion of images vs Visual Modflow simulation
  Visual limit detection @ 40 mg/l
  Hydrodynamic parameters (from column tests):
  Porosity 0.48
  Dispersivity 4.2x10-3 m
  Good match: hydrodynamic parameters confirmed
  PV = 7.75 l, advective front: L = 0.77 m
40 mg/l
50 mg/l
Tracer @ 50 mins
(end of injection)
Tracer @ 60 min
(+ 10min flushing)

## Slide 15: Case study 1 - radial injection (mZVI injection)
mZVI injection (C0 = 20 g/l)
  Pre-flushing: > 15 L (water)
  mZVI injection: 6 L (mZVI + XG:GG)
    Visual results:
    good mobility. L = 0.76 m
    Quantitative results:
    mZVI spatial distribution measured at the end of the test (sampling + magnetic susceptibility measurement)
-15°
0°
+15°
Spatial distribution of mZVI concentration

## Slide 16: Case study 1 - radial injection (mZVI injection)
mZVI injection (C0 = 20 g/l)
  Pre-flushing: > 15 L (water)
  mZVI injection: 6 L (mZVI + XG:GG)
    Visual results:
    good mobility. L = 0.76 m
    Numerical model validation:
    Radial injection was simulated in MNMs using the trasport and clogging parameters fitted from column tests
    Numerical simulation compared with experimental data good match
mZVI concentraton vs radial distance
Pressure buildup at injection point

## Slide 17: Case study 1 - field implementation
Contaminated site in the north of Italy
Contaminants: PCE up to 100.000 μg/L
nZVI injection for the treatment of the hot-spot of the contamination
Pilot injection performed in June 2024
Good ZVI distribution around the well
Max migration distance 9 m

## Slide 18: Optimizing delivery using permeation injection
Poorly stable particles
low mobility
minimal ROI
 Need: improve stability
Very stable particles
- high mobility
- poorly controlled migration
 Need: control stability
nZVI
FeOx
mZVI

## Slide 19: nFeOx particles for heavy metal sorption
Mode of action: injected to form a barrier to adsorb heavy metals (contaminated plume)
Particles’ characteristics:
  Non magnetic particles, humic-acid coated
  Very high colloidal stability
  Very high mobility in column tests  Possible bypass of the target delivery zone!
Source: Reground Project
Tiraferri et al. J Nanopart Res (2017) 19: 107. DOI 10.1007/s11051-017-3814-x

## Slide 20: Case study 2 - Pilot injection of Goethite NPs
Nitrastur site
Asturias (Spain)
Former use: Nitrogen-based fertilizer production
Heavy metal contamination from the backfill
Tiraferri et al. J Nanopart Res (2017) 19: 107. DOI 10.1007/s11051-017-3814-x
Goal:
  Installation of an in-situ reactive barrier
  Heavy metal adsorption
  Treatment of the contamination plume

## Slide 21: Case study 2 - Site characterization and suspension design
Site characterization
  Darcy velocity = 1.15 m/d
  Porosity = 0.15
  K = 4 x 10-3 m/s
  Dispersivity = 5 cm
  d10 = 0.16 mm
Tiraferri et al. J Nanopart Res (2017) 19: 107. DOI 10.1007/s11051-017-3814-x
Suspension design:
  FeOx NPs (10 g/L, 200 nm)
  High colloidal stability in concentrated suspension (dispersant: DI water)
  Expected aggregation when diluted in GW
Ca2: Tap water 0.7 mM Groundwater 5.8 mM

## Slide 22: Case study 2 – Column tests
Column tests on site material:
  Column preconditioning with groundwater
  Pre-flushing with tap water (2 PVs)
  Injection of FeOx 10 g/L in tap water (5 PVs)
  Flushing with tap water (5 PVs)
Modeling:
  Fitting model: 1 site with irreversible attachment
  No particle detachment
  Good transport expected

## Slide 23: Case study 2 – Pilot injection test

## Slide 24: Case study 2 – Pilot injection test
Goethite injection simulation:
  Q = 30 L/min
  Time = 11 hours
  C = 10 g/L
End of the injection
ROI ~ 5x5 m
Particles still in suspension
4 days after injection
reactive zone: 7.5x 4m
all particles deposited
Prediction from column tests modeling
CW3 field monitoring
Re-calibrated model
Chart: Time (h)
CW3_monitored | 0.0011003 | 0.51765 | 0.54976 | 0.59604 | 0.66286 | 0.76686 | 0.63686 | 0.56146 | 0.59214 | 0.028716 | 0.00056472 | 0.0018517 | 0.00092222 | 0.0067462 | 0.003861 | 0.00096047 | 0.00032028 | 0.0005346 | 0.0002016

## Slide 25: Case study 2 – Large scale simulation: injection strategies
Modeling tool: Modified Visual Modflow + MNM3D
  Grid: min. 1m x 1m, max 1m x 2.5m
  Groundwater flow model calibrated against static and dynamic water level measurements

## Slide 26: Case study 2 – Large scale simulation: injection strategies
GOAL: Identify the best injection strategy to:
  Obtain a wide and homogeneous reactive barrier
  Minimize the risk of suspension daylighting
DAY 1
DAY 2
DAY 3
DAY 4
DAY 5
SCENARIO 1
SCENARIO 2
SCENARIO 3
SCENARIO 4
SCENARIO 5
10 hour injection from 2 wells
Q = 30 l/min
14 hour stop
CONSTRAINTS:
  Injection in maximum 2 wells in parallel, per day
  Maximum injection rate 30 l/min per well

## Slide 27: Case study 2 – Large scale simulation: scenario 4
Solid phase
12 g/l
10
8
56
4
2
1
0.05
0.4 g/g
0.35
0.3
0.25
0.2
0.15
0.1
0.05
Liquid phase
End of injection
30 days after injection

## Slide 28: Case study 2 – Full scale injection
INJECTION PLAN
Day 1: IW1
Day 2: IW5,IW7
Day 3: P7, P8, P9 (NanoTune)
Day 4: IW2,IW4
Day 5: IW6,IW8
Day 6: IW3,IW9
Tot: 1260 kg of NP
V = 14 m3 per well
Q = 40 L/min
C = 10 g/L
Chart: Time (d)
| -6.0118055555576575 | 0.17638888888905058 | 1.1069444444437977 | 1.2611111111109494 | 3.0597222222204437 | 3.2312499999970896 | 4.0006944444467081 | 4.2249999999985448 | 4.9861111111094942 | 5.1131944444423425 | 7.9881944444423425 | 13.988194444442343 | 35.988194444442343 | 64.988194444442343 | 126.98819444444234 | 188.98819444444234
P7 | 0.17202 | 0.20661 | 0.20835 | 0.18148 | 0.18321 | 0.19795 | 0.14941 | 0.14508 | 0.13218 | 0.12081 | 0.1287 | 0.08528 | 0.14587 | 0.038454 | 0.027746 | 0.032952
P8 | 0.01938 | 0.0104 | 0.066387 | 0.22655 | 0.018893 | 0.075573 | 0.0364 | 0.048187 | 0.067167 | 0.021233 | 0.047112 | 0.016248 | 0.024072 | 0.02244 | 0.0042858 | 0.00177
P9 | 0.01938 | 0.0429 | 0.97708 | 1.6002 | 0.55155 | 0.82975 | 0.36955 | 0.34268 | 0.037274 | 0.32708 | 0.00678 | 0.009942 | 0.013122 | 0.009564 | 0.0082698 | 0.007548
P10 | 0.00954 | 0.0046453 | 0.39641 | 0.92161 | 1.4 | 1.2648 | 0.34147 | 0.41635 | 0.065867 | 0.37908 | 0.004827 | 0.0019584 | 0.008874 | 0.009078 | 0.0064218 | 0.005532
Iniezione AR | 0 | 2
Mohammadian et al (2021). Journal of Contaminant Hydrology 237, 103741

## Slide 29: Case study 2 – Monitoring results: Zinc
Mohammadiam et al (2021). Journal of Contaminant Hydrology 237, 103741

## Slide 30: Beyond particle injection: in-situ synthesis of metallic nanopartices for groundwater remediation
  Solute injection, wide ROI
  It is not necessary to improve the colloidal stability of nZVI/mZVI particles
  Potentially applicable also in low permeability aquifers

## Slide 31: In-situ synthesis of metallic nanoparticles for GW remediation

## Slide 32: Case study 3 - in-situ synthesis in a 3D homogeneous tank
Experimental 3D apparatus:
  L = 70 cm
  W = 55 cm
  H = 50 cm
  Homogeneously packed with mean silica sand (K = 7 · 10-4 m/s)
  Reconstruction of 3D particle distribution after synthesis with tomographic approach
Gallo et al. (2026). Communications Earth & Environment. Accepted manuscript

## Slide 33: Case study 3 - in-situ synthesis in a 3D homogeneous tank
Formation of a homogenous reactive zone close to injection well and along the vertical direction
No evidence of preferential migration pathways
Efficiency of precursor conversion ≈ 77%
Gallo et al. (2026). Communications Earth & Environment. Accepted manuscript

## Slide 34: Case study 3 - in-situ synthesis in a heterogenous 2D flume
Experimental 2D setup:
L = 40 cm, H = 20 cm, s = 2 cm
  Heterogeneously packed with lenses of:
  Gravel (K = 10-2 m/s)
  Mean sand (K = 7 · 10-4 m/s)
  Fine sand (K = 5 · 10-6 m/s)
Gallo et al. (2026). Communications Earth & Environment. Accepted manuscript

## Slide 35: Case study 3 - in-situ synthesis in a heterogenous 2D flume
nZVI direct injection
In-situ synthesis
L
4.5 x L
vs
Gallo et al. (2026). Communications Earth & Environment. Accepted manuscript

## Slide 36: Conclusions
Nanoremediation can be a successful strategy in many applications
The injection of reactive nano- and micro-particles for the formation of in situ reactive zones is highly affected by the colloidal stability of the suspensions
  Integrating tests and numerical modeling at different scales allows correct prediction of particle mobility during and after injection and consequently of the formed reactive zone
  Transport models must be validated and re-calibrated at the different scales
A novel approach to nanoremediation is based on the in situ synthesis of reactive particles via injection of eco-compatible precursors
  Problems associated with poor colloidal stability and particle mobility are overcome
  Particles can be formed also in low permeability zones
  Approach validated at lab scale, field application needed

## Slide 37: Acknowledgements
Groundwater Engineering Group @ POLITO
  Rajandrea Sethi, Full Professor
  Alessandro Casasso, Associate Professor
  Carlo Bianco, Assistant Professor
  >10 Assistant Researchers and PhD students

## Slide 38
Thank you for your attention
tiziana.tosco@polito.it
www.polito.it/groundwater
38