## Slide 1
Interpore2026 – Nantes – 20th May 2026
Fluid-calcite interface tracking by X-ray micro-tomography of bio-cemented sand samples exposed to acidic conditions
M. la Bella1,4, L. Schröer2, V. Cnudde2, F. Emeriault1, C. Geindreau1 , C. Noiriel3 and A. Naillon1
1 Univ. Grenoble Alpes, CNRS, Grenoble INP, 3SR, Grenoble, F-38000 France
2 UGCT, Department of Physics, Ghent University, Ghent, Belgiumn
3 Géosciences Environnement Toulouse, Observatoire Midi-Pyrénées, Université de Toulouse CNRS, IRD, CNES, Toulouse, France
4 Department of Physics, Technical University of Denmark, Kongens Lyngby, 2800 Denmark

## Slide 2: Motivations for new reinforcement technics
Manufacturing of construction materials
Ex. building blocks
Classical technics
  Use of high carbon foot print materials
  Some toxic materials
  Energy consuming technics
Late 20th : emergence of bio-cementation
+ environmental friendly
- low energy consumption
↗ mechanical properties
✓ permeabilities
Prevention of natural hazard
Ex. soil liquefaction
Dike reinforcement
Ex. Internal erosion [L. Peyras]
Heritage conservation
Ex. Tours cathedral

## Slide 3: How does bio-cementation work ?
100 µm
Reactant
Urea CO(NH2)2)
Calcium source (CaCl2)
Bacteria (S. Pasteurii)
injection
Sand
injection
A low fraction of calcite is sufficient
Mechanical properties depend on the contacts

## Slide 4: Global project : micromechanical characterization of biocemented contacts to predict macroscopic mechanical properties
[La Bella et al. 2025 Collaboration M. Sarkis (ESRF), C. Noiriel (GET), ESRF ID11, ]
[Collaborations TUGent, C. Noiriel (GET Toulouse)]
[Sarkis et al. 2023]
[Dumas - stage 2023]
[Sarkis et al. 2024]
[Sarkis et al. 2025]
200 µm
[Collab. B. Chareyre (YADE)]
How do biocalcite distribution and mechanical properties evolve under acidic conditions?

## Slide 5: Two scale experiments
Granular columns
  Biocementation in the fluid cell
  Dissolution with buffered acetic acid with :
    pH = 4, 5, and 6.4
    Q = 50 ml/h, and 2 ml/h
  Tracking of pH and conductivity
  Flushing with water before taking tomography scan
  Acquisition of several dissolution timesteps
  Vx size = 73 µm3 (3.53 µm3 binned x2)
Two-grain and crystal experiments
  Same solution and pH as in granular columns
  Comparison between
    Biocalcite
    Abiogenic calcite
  Vx size = 1.33 µm3
Sand D = 0.18 – 0.35 mm
Filter 60 µm
Outlet
9.1 mm
18 mm
Inlet

## Slide 6: Granular column: target indicators
  Porosity :
  Calcite volume fraction :
  Active calcite volume fraction :
  Fraction of grain without cohesive contact
  Fraction of cohesive contact surface area :
  Contact orientation : : singular value decomposition on the point cloud of the contact surface
  Fabric Tensor :
Inactive crystal
Active crystal

## Slide 7: Granular column: image analysis flowchart

## Slide 8: Granular column: results at pH5
t = 18h
100
80
60
40
20
0
t = 4h
FCC : Acohesive / Asand
t = 2.5h
t = 1h
t = 0h
1 mm
Even after 50% of the calcite has dissolved, 98% of grains have cohesive contacts
When of the grains have cohesive contacts

## Slide 9: Granular column: results at pH5
Heterogeneity develop in the material.
Dissolution occurs mainly from the inlet to the outlet but fingering patterns develop.
Anisotropy develop in the material.
Contacts whose normal vectors are parallel to the flow dissolve last.

## Slide 10: Two-grain and crystal experiments
Target indicators:
  Dissolution rate:
  Comparison between biogenic and abiogenic calcite
  Preferential dissolution sites in two-grain experiments
Flow chart
Distance map inside
the crystal at t0
Location of the crystal liquide interface at t1
Determination of

## Slide 11: Two-grain and crystal experiments : results in batch
Surface retreat with time
pH 4 :
20min
40min
1h20
2h
2h45
20min
40min
1h20
2h
2h45
pH 5 :
100 µm
500 µm
Dissolution of calcite monocrystal proceeds with rounding the edges and the corners
Calcite is more persistent at the contact due to reduced fluid accessibility to the surface area (transport advective vs diffusive)
pH 4
pH 5
Dissolution only at the contact
20min
40min
1h20
2h
2h45
20min
40min
1h20
pH 4 :
pH 5 :
  30 times greater than in HCl

## Slide 12: Conclusion
Methods :
  We performed experiments to track the dissolution kinetics and patterns at crystal scale and granular column scale
  We have designed experiments and algorithm that allows extracting the evolution of the microstructural properties in a granular column during dissolution.
Dissolution
  Dissolution rate decreases with pH increase, but not in orders of magnitude :
  Dissolution rate with acetic acid (weak acid) is 30 times greater than in HCl (strong acid)
  Apparent biogenic calcite dissolution rate seems faster at short time but slowler at long time because its difficult access to flow.
  Most the grains maintain cohesive contact until
  An anisotropy appears in the material due to the late dissolution of the contacts whose normal align with the flow.
Perspectives
  Use results from other flow conditions in the analysis.
  Start with smaller
  Use the microstructural evolution as input for DEM to predict the evolution of the mechanical properties of biocement sand.

## Slide 13: Thank you for you attention